## Slide 1: Biodegradable polymeric microcapsule for drug delivery system
Prepared by:
Afif Hithnawi Lubna Ashayer
Nuha Abu Zahra Sundus Aghbar
Co-Superviser:
Dr. Mohyedine Assali
Superviser:
Dr.Hassan Sawalha

## Slide 2: Drug problems
Side effects, immune system reactions.
Patient compliance and convenience problems to the repeated doses .
low extended period of time at desired release rate of drug.
weak achieving for drug targeting in cancer treatment.
Biodegradability and biocompatibility.

## Slide 3
Objectives.
Introduction.
Experimental work.
Results.
Conclusion.
Outlines:

## Slide 4
Objective :
The main objective of the current study was investigate the effect of the type of polymers on the drug release behavior from biodegradable microcapsules for drug delivery applications.

## Slide 5: Introduction
Polymers: many small molecules that can be linked together by covalent bonds to form long chains.

## Slide 6: Introduction
Polymers can be classified into several categories:
Basis of their occurrence:
natural polymers:
e.g: proteins , carbohydrates , and quartz.

## Slide 7: Introduction
synethetic polymers:
e.g: Nylon, polystyrene, rubber.
Semisynthytic:
silicones, polyacrylamide

## Slide 8: Introduction
Behavior toward temperature:
Thermoplastic.
Thermoset.
Other basis:
Based on line structure.
Based on tacticity.
Based on morphology.
Based of polymerization of reactions.

## Slide 9: Introduction
Biodegradable polymers:
are polymers that do not have resistance to degradation that take place through action of enzymes and chemical deterioration associated with living organism.
e.g. poly caprolactone (PCL), and Poly(esters) like poly D and L lactide(PLLA)(PDLLA).

## Slide 10: Introduction
Poly-Caprolactone:
PCL is a synthetic, biodegradable and semi-crystalline polymer is prepared using ring-opening polymerization of ε- Caprolactone.

## Slide 11: Introduction
Polylactic Acid:
PLA is a biodegradable poly ester and semi-crystalline thermoplastic polymer. it's hydrophobic polymer and unstable in wet conditions.

## Slide 12: Experimental work
8g water
+
+
3g PVA
+
1g DCM
+
10mg Carvedilol
0.5g polymer solution
+

## Slide 13: Experimental work

## Slide 14
CRV
CRV
CRV
CRV
MICROCAPSULE
(1μ)
TARGETING
CONTROLLED RELEASE
CRV

## Slide 15
Release process description:
Dialysis membrane
Washing the membrane
Saline buffer, pH=7.4
Then
Microcapsule
dissolved in
5ml buffer
Inserting the sample in the washed membrane.
The membrane was clamped by tongs and dip in buffer .

## Slide 17
* After a certain periods of time, (5ml) from the buffer which contained the released drug was withdrawn.
* The absorbance of withdrawn sample was measured by using U.V. Spectrophotometer.

## Slide 18: Result And Discussion
Drug Loading :
Freeze drying Conditions | %loading | Drug added (in preparation) | Biodegradable polymer
-87°C/5mTorr | 482.00% | 10 mg | PDLLA
-87°C/5mTorr | 389.00% | 10 mg | PCL
-87°C/5mTorr | 105.92% | 5 mg | PLLA

## Slide 19
Conditions(Temp./Pressure) | %loading | Drug added(in preparation) | Biodegradable polymer
-79 °C/6mTorr | 44.11% | 5mg | 50% PLLA- 50%PCL
-79 °C/6mTorr | 38.14% | 5mg | 50%PDLLA-50%PCL
Drug Loading :

## Slide 20: Drug release studying
The drug release system of neat polymers :
Chart: Time(hrs)
| 0 | 0.25 | 0.5 | 0.75000000000000022 | 1 | 2 | 20 | 21 | 23 | 24 | 25 | 26 | 27 | 46 | 47
PCL | 0 | 0 | 6.4516 | 25.641 | 25.641 | 27.5 | 67.7778 | 67.7778 | 69.7917 | 72.8972 | 72.8972 | 73.1481 | 73.1481 | 73.1481 | 73.1481
PDLLA | 0 | 0 | 50 | 51.5152 | 51.5152 | 58.9744 | 62.7907 | 69.8113 | 69.8113 | 69.8113 | 70.3704 | 70.3704 | 71.4286 | 71.4286 | 71.4286
PLLA | 0 | 0 | 41.1765 | 56.5217 | 62.963 | 73.6842 | 75 | 84.8485 | 86.4865 | 86.6667 | 86.6667 | 87.013 | 87.1795 | 87.1795 | 87.1795
Carvedilol | 0 | 31.8 | 46.2 | 64.4 | 78.2 | 90.6 | 96.2 | 98.2 | 99.4 | 99.2 | 99.4 | 99.4

## Slide 21: Drug release studying
The drug release system of PCL-PDLLA Blend:
Chart: 
| 0 | 0.25 | 0.5 | 0.75000000000000411 | 1 | 2 | 20 | 21 | 23 | 24 | 25 | 26 | 27 | 46 | 47
PCL | 0 | 0 | 6.4516 | 25.641 | 25.641 | 27.5 | 67.7778 | 67.7778 | 69.7917 | 72.8972 | 72.8972 | 73.1481 | 73.1481 | 73.1481 | 73.1481
PDLLA | 0 | 0 | 50 | 51.5152 | 51.5152 | 58.9744 | 62.7907 | 69.8113 | 69.8113 | 69.8113 | 70.3704 | 70.3704 | 71.4286 | 71.4286 | 71.4286
50% PDLLA,50%PCL | 0 | 0 | 64 | 77.5 | 78.5714 | 80.8511 | 90.3226 | 91.3462 | 91.4286 | 91.4286
PCL

## Slide 22
Chart: Time(hrs)
| 0 | 0.25 | 0.5 | 0.75000000000000022 | 1 | 2 | 20 | 21 | 23 | 24 | 25 | 26 | 27 | 46 | 47
PCL | 0 | 0 | 6.4516 | 25.641 | 25.641 | 27.5 | 67.7778 | 67.7778 | 69.7917 | 72.8972 | 72.8972 | 73.1481 | 73.1481 | 73.1481 | 73.1481
PLLA | 0 | 0 | 41.1765 | 56.5217 | 62.963 | 73.6842 | 75 | 84.8485 | 86.4865 | 86.6667 | 86.6667 | 87.013 | 87.1795 | 87.1795 | 87.1795
50% PCL,50%PLLA | 0 | 0 | 0 | 16.6667 | 32.4324 | 39.0244 | 46.8085 | 59.0164 | 82.0144 | 82.1429 | 82.2695 | 82.6389 | 82.6389 | 82.6389
Drug release studying
The drug release system of PCL-PLLA Blend:
PCL

## Slide 23: DSC test
DSC curve for PDLLA and PCL sample:

## Slide 24: DSC test
DSC curve for50% PCL/50%PDLLA and 50% PCL/50%PLLA samples:

## Slide 25: AFM test
The atomic force microscope for the sample of PDLLA, PLLA and PCL microcapsules.
Average size=0.46
Average size=0.75
Average size=0.0.50
PDLLA
PLLA
PCL

## Slide 26: AFM test
Average size=0.41
The atomic force microscope for the sample of PCL-PDLLA blend and PCL-PLLA blend microcapsules.
Average size=0.74
PCL-PDLLA Blend
PCL-PLLA Blend

## Slide 27: Conclusion
In this study CRV (active drug) was encapsulated inside biodegradable polymeric microcapsules(PCL, PLLA, and PDLLA).
The prepared microcapsules were fairly uniform with an average size of 0.5 -0.8µm.
Higher loaded amount of CRV was found with PDLLA microcapsules.
Higher accumulative release percentage of drug was obtained with PLLA microcapsules.
(50%PDLLA-50%PCl) blend system which most favorable system since it has the highest percentage of release with the most long period of time.

## Slide 29
The
Time
Of
Questions

## Slide 30
Congratulation us.
Currently , We Are .........Engineers