## Slide 1
Naheel
Abed Rabbo
Shurouq
Al-Wawi
Munya
Mas’oud
Maram
Kilani
Characterization of Wood Ash and Potential Applications
Supervisor:
Dr. Hamdallah Bearat

## Slide 2
Outlines:
Introduction.
pH and solubility characterization.
Experimental work of products.
Determination of elements concentration in ash.
Results.
Conclusions.

## Slide 3
Wood Ash
Glass
Ceramic
Soap
Cement
Fertilizer

## Slide 4
Wood Ash
Definition: residue from burning of wood or its products such as: chips, saw dust, bark, etc. It consists of organic and inorganic compounds.
Factors affecting ash properties:
Constituents of the wood.
The burning method (temperature, oven’s efficiency, fuels).
Soil and irrigation water chemistry.
Wood ash in this project is used as ingredient in industrial applications including: glass, ceramic, soap, cement and fertilizer.

## Slide 5
Glass
Definition: an amorphous substance, inorganic product which obtained either as a solid from the melt or by other methods in a compact form, or as a thin coherent films, wires, or fibers.
Glass in this project:
Soda-Lime-Silica Glass at °1000 C.
Quenching from the melt.

## Slide 6
Ceramic
Definition: inorganic, non-metallic material of crystalline nature, insoluble in water and formed by heating to high temperatures.
Ceramic in this project:
- Traditional ceramic using clay and sand.
- Hand-forming method by adding ash to improve strength.

## Slide 7
Soap
Definition: any salt of fatty acid and usually made by saponification of fatty oil with caustic soda.
Soap in this project:
Hard olive-oil soap using soluble part of ash.
Using hot method.

## Slide 8
Cement
Definition: is a material which binds together solid bodies by hardening from a plastic state. It is a fine powder produced by grinding Portland cement clinker.
Cement in this project:
Portland cement using ash to improve strength.
Preparation from powder at 1000 °C.

## Slide 9
Fertilizer
Definition: is a material for plant growth and development by providing essential plant nutrient elements, such as: nitrogen, phosphorus, and potassium.
Fertilizer in this project:
Using the soluble part of ash.
Using total part of ash.

## Slide 10
Solubility & pH Tests

## Slide 11
5 g of ash
100 mL water
Vacuum Filtration
Drying insoluble part
Insoluble part
Solubility & pH Test in Cold Water
pH Test
Soluble Part

## Slide 12
5 g of ash
Vacuum Filtration
Drying insoluble part
Insoluble part
Solubility & pH Test in Hot Water
pH Test
Soluble Part
100 mL water

## Slide 13
Experimental
Work of
products

## Slide 14
Glass Work
Almonds Ash
Silica Sand
Sodium Carbonate
Limestone

## Slide 15
Ceramic Work
Almonds Ash
Silica Sand
Clay
15 % water
25 % water
Drying !
2 Days
Oven (90 °C)

## Slide 16
Soap Work
NaOH
CaCO3
Olive Ash
CaCO3
Olive Ash
NaOH

## Slide 17
Cement Work
Citrus Ash
Clay
Limestone

## Slide 18
Fertilizer Work
100 g ash
1000 mL water
Citrus Ash
Citrus Ash
Olive-Olive cake Ash
5 mL
10 mL
5 mL
10 mL
10 g
10 g

## Slide 20
Hot Water Solubility (%) | Cold Water Solubility (%) | Ash Type
3.40 | 4.80 | Citrus Ash
9.60 | 8.80 | Almonds
17.60 | 19.20 | Olive
Solubility Results

## Slide 21
Solubilities of several inorganic and organic solids in water as a function of temperature

## Slide 22
pH | Ash Type
12.95 | Olive-Olive cake/Ramallah
12.90 | Olive
10.23 | Olive-Olive cake/Jenin
11.72 | Almonds
pH Results

## Slide 23
Glass Work Results
Kafr-Laqif silica sand
Limestone
Ash
Kafr-Laqif silica sand
Ash
Kafr-Laqif silica sand
Ash
Sodium Carbonate
40 %
30 %
30 %

## Slide 24
Desert Silica Sand
Ash
Sodium Carbonate
50 %
20 %
30 %
Sea Silica Sand
Ash
Sodium Carbonate
Purified Sea Silica Sand
Ash
Sodium Carbonate
1100 °C
40~45 %
27~30 %
27~30 %
Purified Sea Silica Sand
Ash
Sodium Carbonate

## Slide 25
Ceramic Work Results
Slip Casted Ceramics
Plastic Paste Ceramics
0 % Ash + 100 % (clay-sand)
10 % Ash + 90 % (clay-sand)
20 % Ash + 80 % (clay-sand)
30 % Ash + 70 % (clay-sand)
40 % Ash + 60 % (clay-sand)
50 % Ash + 50 % (clay-sand)

## Slide 26
10 % Ash
20 % Ash
0 % Ash
Comparison !
  Strength
Cracking
Color
Weight

## Slide 27
Soap Work Results
Ash
Calcium Hydroxide
Olive Oil
Caustic Soda + Water
Olive Oil
Ash
Calcium Hydroxide
Olive Oil
NaOH + Water
60 g
25 mL
7 g
30 g
30 g

## Slide 28
Cement Work Results
5 g Ash
10 g Ash
15 g Ash
20 g Ash
25 g Ash

## Slide 29
Fertilizer Work Results

## Slide 30
Elements’ Concentration Results

## Slide 31
Flame-photometry Analysis for Sodium
Sodium Concentration (ppm) | Ash Type
50 | Olive-cake
50 | Olive-Olive cake (Jenin)
300 | Almonds
550 | Olive
Effect on: Glass & Soap

## Slide 32
Potassium Concentration (ppm) | Ash Type
15 | Olive Cake
30 | Citrus
15000 | Almonds-Olive
15000 | Olive-Olive cake
Flame-photometry Analysis for Potassium
Effect on: Soap & Fertilizer

## Slide 33
Calcium Concentration (ppm) | Ash Type
42,000 | Olive cake
28,800 | Almonds-Olive
15,600 | Olive
12,000 | Olive-Olive cake/Ramallah
Titration Results for Calcium
Effect on: Glass

## Slide 34
Magnesium Concentration (ppm) | Ash Type
72,900 | Olive Cake
32,076 | Citrus
4,374 | Olive
7,290 | Almonds-Olive
Titration Results for Magnesium
Effect on: Glass

## Slide 35
Chlorine Concentration (ppm) | Ash Type
68,160 | Olive-Olive cake/Ramallah
58,575 | Olive-Olive cake/Jenin
20,235 | Citrus
36,210 | Almonds
Titration Results for Chlorine
Effect on: Soap & Ceramic

## Slide 36
Phosphorus Concentration (ppm) | Ash Type
22.61 | Olive-Olive cake/Ramallah
39.56 | Olive-Olive cake/Jenin
1,283 | Olive
424 | Olive Cake
Spectro-photometry Analysis for Phosphorus
Effect on: Fertilizer

## Slide 37
Conclusions
pH and solubility of ash ?
Using ash in glass preparation ?
Using ash in ceramic preparation ?
Using ash in soap making ?
Using ash in cement preparation ?
Using ash as fertilizer?
Chemical composition of ash and its effect ?