## Slide 1
Biochar Production and Characterization from Sesame Husk Waste for Environmental Application: Methylene Blue Adsorption
Faculty of Engineering
Chemical Engineering program
Graduation Project (2)
Prepared by:
Khalid Owies Sarah Al-Heeh Shayma’ Sulaiman
Supervised by:
Prof. Amer El-Hamouz

## Slide 2
Biochar Characterization
Contents
Problem Statement
What is Biochar?
Project Objectives
Why Sesame Husk?
Methodology
Adsorption Experiment
Activation
Results Analysis
Conclusions
2

## Slide 3
The Problem ?
3

## Slide 4
Biochar

## Slide 7
Why Sesame Husk ?
Agricultural Waste
Low Cost
Rich Lignocellulosic Compounds

## Slide 8
Transformation Journey
Sesame Husk
Adsorption
Activation
Biochar
Pyrolysis
Pretreatment

## Slide 9
  Pre- Treatment

## Slide 10
  Pre- Treatment of the Raw Husks

## Slide 11
  Pyrolysis

## Slide 12
  Physiochememical Characterizations

## Slide 13
pH =8.28
Ash Content = 49.3%
To predict the behavior of biochar with the pollutant in terms of charge.

## Slide 14
WHC = 268%
Wettability: Hydrophilic
It affects the accessibility of pollutants to adsorption sites and influence their retention within the pores.
It affects the ability of water and pollutants to enter the pores easily or not.

## Slide 16
Iodine Number =699 mg/g
I₂
It determines the number of accessible adsorption sites and thus significantly affects the adsorption performance.

## Slide 17
Biochar Chemiacl Activation

## Slide 19
Iodine Number

## Slide 21
Biochar
addition
Solution
Mixing
Sampling
Separation
Transfer
Analysis
Adsorption study
0.2 g

## Slide 22
Methylene Blue Concentration Reduction Over Time
Activated Biochar
Raw Biochar

## Slide 23
Comparison between raw biochar and activated biochar

## Slide 24
Adsorption Isotherm Models
Langmuir Model
Freundlich Model
Monolayer adsorption
Homogeneous surface
Uniform adsorption sites
Multilayer adsorption
Different adsorption
energies
Heterogeneous surface

## Slide 25
Adsorbent | Model | R² | RMSE
Raw Biochar | Langmuir | 0.9433 | 32.48
Raw Biochar | Freundlich | 0.9173 | 6.28
Activated Biochar | Langmuir | 0.9954 | 19.68
Activated Biochar | Freundlich | 0.9931 | 12.57
✓ Best Fit Model
Freundlich Isotherm

## Slide 26
Adsorption Kinetic Analysis
pseudo-first-order model
Pseudo-Second-Order model
Surface adsorption dominated
Surface interactions dominated

## Slide 27
Best Fit: Pseudo-Second-Order Model

## Slide 28
Intraparticle Diffusion Analysis
Activated biochar exhibited superior adsorption efficiency.
Rapid surface adsorption followed by pore diffusion.
The plot did not pass through the origin (C ≠ 0).

## Slide 29
Activated biochar showed enhanced diffusion and adsorption performance
Activated biochar
Raw biochar

## Slide 30
Recomendations & Future waork
  Investigations of the biochar performance with other types of dyes, as well as a mix of dyes.
  Testing the biochar adsorption on other types of pollutants (heavy metals, organic contaminants).
  Evaluation of the regeneration potential of the activated biochar.
  Exploring other activation methods and comparing them.

## Slide 31
  Sesame husk waste is an optimum feedstock for biochar production.
  KOH activation significantly improved the adsorbent properties of the biochar.
  Best described by the Freundlich isotherm and the Pseudo-Second Order kinetic model.
  Sesame husk waste has promising applications in wastewater treatment.
Conclusion

## Slide 32
Thank you