Faculty of Engineering & Information Technology

Chemical Engineering Department

Adsorptive removal of dyes from textile wastewater using nanoparticles (nanopyroxene)

Prepared by:

Aya Assaf

Huda Amer

Saja Ahmed

Yasmeen Sabbah

Supervisor:

Eng. Maryam Hmoudah

Presented in Partial Fulfillment of the Requirements for Bachelor

Degree in Chemical Engineering

May 2017

# Abstract

Textile wastewater consumes large quantities of water and produces large volumes of wastewater which is often rich in color, containing residues of reactive dyes and chemicals as well as much more hard-degradation materials. The presence of dyes in wastewater poses an environmental concern due to the existence of toxic components that may impact to aquatic and non-aquatic life. In this work, a new environmentally sound and low-cost, yet highly efficient nanopyroxene, (NaFeSi2O6) which is known as aegirine, will be used as an adsorbent for the removal of a model molecule dye from aqueous solutions and real textile wastewater by the batch-adsorption technique.

Different diluted samples (100%, 85%, 70%, 55%, 40%& 25%) for COD test and (100%, 80%, 60%, 40% & 20%) for the UV- spectrophotometer were prepared and adsorption was done at 25 oC, 35 oC and 45oC. The samples were put in the shaker for 24 hour and 150 rpm and separate by centrifuge at specific time and speed. The results were measured by COD and UV- Spectrophotometer devices.

The readings of COD must decrease but they were randomly changed maybe due to the high total suspended solid. Also for the UV- Spectrophotometer the results before adsorption were corrected as the dilution factor decrease the absorbance were decreased but for the samples after adsorption the absorbance were randomly changed and that unreasonable, this indicates that there is a specific metal in the water sample didn’t adsorb by nonopyroxene at wavelength equal approximately 281nm. According to the results the adsorption isotherm and thermodynamics study cannot applied.

Acknowledgment

First we thank Allah for granting us knowledge and patience to do this work. And we would like to express our special thanks of gratitude to our supervisor Eng. Maryam Hmoudah who gave us the golden opportunity to do this graduation project, which also helped us in doing a lot of research and we came to know about so many new things.

We really appreciate the help of all the staff members of the departments of chemical engineering, namely: Dr. Abdelraheem Abusafa for his assistance on the UV-Spectrophotometer, Mr. Yusuf Ratrout and Ms. Maha Fuqha for their help in the laboratory space.

Contents

Abstract	II

List of tables:	III

List of figures:	IV

Chapter 1: Introduction	1

Chapter 2: Adsorption	4

2.1 Adsorption definition	4

2.2 Adsorption mechanism	5

2.3 Adsorption in textile wastewater treatment	5

2.4 Adsorption Isotherm	6

Chapter 3: Literature Review	9

4.1 Adsorbate	13

4.2 Adsorbent	13

Chapter 5: Feasibility Study	19

Chapter 6: Results and discussion	21

6.1 COD results	21

6.2 UV-Spectrophotometer results	23

6.3 Regeneration and reuse	30

Chapter 7: Conclusion	30

Chapter 8: References	31

# List of tables:

Table 1: BET  surface  area,  particle  size  and  XRD  crystalline  size  of  different-sized  nanopyroxene nanoparticles	16

Table 2: the prices of raw materials	19

Table 3: the results of COD test at 250C	22

Table 4: the results of COD test at 350C	22

Table 5: the results of COD test at 450C	22

Table 6: the result of COD test at 250C	23

Table 7: the result of COD test from WESI	23

Table 8: The UV-spectrophotometer results before adsorption	24

Table 9: The UV-spectrophotometer results after adsorption	24

# List of figures:

Figure 1: Schematic representation of the report layout	3

Figure 2: adsorption occurs in liquid	5

Figure 3: XRD powder of nanopyroxene for particle size	15

Figure 4: SEM image for nanopyroxene	16

Figure 5: HRTEM images for size nanopyroxene	17

Figure 6: Infrared spectroscopy of the prepared pyroxene nanoparticles for the hydroxyl group region for nanopyroxene.	17

Figure 7: Abs vs. wavelength before adsorption for dilution 100%	25

Figure 8: Abs vs. wavelength after adsorption for dilution 100%	25

Figure 9: Abs vs. wavelength before adsorption for dilution 80%	26

Figure 10: Abs vs. wavelength after adsorption for dilution 80%	26

Figure 11: Abs vs. wavelength before adsorption for dilution 60%	27

Figure 12: Abs vs. wavelength after adsorption for dilution 60%	27

Figure 13: Abs vs. wavelength before adsorption for dilution 40%	28

Figure 14: Abs vs. wavelength before adsorption for dilution 40%	28

Figure 15: Abs vs. wavelength before adsorption for dilution 40%	29

Figure 16: Abs vs. wavelength before adsorption for dilution 20%	29

# Chapter 1: Introduction

Wastewater is any water that has been adversely contaminated by organic pollutants, bacteria and microorganisms, industrial effluent or any compound that deteriorated its initial quality.[1]It can be sub-divided into: first, municipal wastewater (liquid waste discharged by domestic residences and commercial properties), and second, industrial wastewater (liquid waste discharged by industrial and agricultural activities).[1]

# Textile industries very important sours of wastewater, because it release significant amount of colors or organic dyestuffs to fresh water that are used in various industrial processes, which contains a number of contaminants, including acidic or caustic dissolved solids, toxic compounds, and any different dyes.[2, 3]These dyes cause real environmental problems which affect human, plants and aquatic life, causing various diseases and disorders because of its high toxicity and possible accumulation in the environment.[4, 5]Many of these dyes are carcinogenic, mutagenic, and teratogenic; therefore, removing dyes from wastewater is essential before discharging effluents into the environment.[6, 7]Textile wastes sorted into four group by the USEPA (Environmental Protection Agency): dispersible, hard-to-treat, high-volume, and hazardous and toxic wastes.[8]

There is different complex chemical structure dyes which is based on aromatic, heterocyclic, and azo-compounds, such as aromatic amine (C6H5-NH2), phenyl(C6H5CH2), naphthyl(C10H7CH2), and azo(-N¼N-) groups, are known in literature.[9]These dyes and compounds are difficult to remove or treat with conventional treatment methods.[10] Various chemical and physical methods that have been employed for dye removal from wastewater, including coagulation-flocculation, precipitation, photocatalysis, membranes, electrochemical, biological (such as trickling filters), etc.[2, 3, 8, 11, 12] These technologies are cost prohibitive, and therefore are not viable options for treating wastewater streams.[12] Adsorption is popular technique for removal dyes due to simplicity and high efficiency of this process, and also for the availability of a wide range of adsorbents, including activated carbon, zeolites, etc.[1, 13] Adsorption is a phase transfer process it is used to remove substances from fluid phases (gases or liquids), and it also observed as natural process in different environmental compartments.[14]Nanoadsorbent technology is the best method to remove dyes from wastewater due to their properties such as large surface area, high reactivity, high specificity, which lead to high adsorption efficiency, high removal rate of contaminants, and easy and rapid separation of adsorbent from solution viamagnetic field.[15, 16] A new environmentally sound and low-cost, yet highly efficient nanopyroxene, (NaFeSi2O6) which is known as aegirine, will be used as an adsorbent for the removal of a model molecule dye from aqueous solutions and real textile wastewater effluents by the batch-adsorption technique.[17] Nanotechnology is the technology related to the utilization of materials at nanoscale, 1-100 nm .[18] The use of nanotechnology in the future is expected to expand into numerous industrial applications and help decrease production costs by reducing energy consumption, attenuate environmental pollution and increase the production efficiencies in developed countries.[19]With the latest developments in nanotechnology, various types of magnetic nanoparticles have also been successfully synthesized and have received considerable attention to solve environmental problems, such as accelerating the coagulation of sewage, removing radionuclides, adsorption of organic dyes, and remediation of contaminated soil.[20]Aluminum oxides(Al2O3), Magnesium oxide (MgO), Zirconium dioxide (ZrO2), Cerium oxides (CeO2), Titanium dioxide (TiO2), Zinc oxide(ZnO)and Fe and O form a number of phases, e.g., FeO (wustite); Fe3O8 (magnetite), α- Fe2O3 (hematite), γ-Fe2O3 (maghemite), and ε-Fe2O3 as an examples of nonmetal oxides.[21]

despite these advantages there are some of drawback such as high cost and ecotoxicological hazard of metal oxide nanoparticles.[22]

This study is aimed at investigating the effectiveness of nanopyroxene for the adsorptive removal of dyes from real textile wastewater effluents. The COD test and UV-Spectrophotometer were used for reading the results of the samples before and after adsorption.

Thisproject consists of eight chapters. It prepared by AyaAssaf, Huda Amer, Saja Ahmad and YasmeenSabbah. Eng. Maryam Hmoudah is the supervisor of the project. Chapter one gives an overview about nanoadsorbent technology, textile wastewater and the main objectives of this project. Chapter two presents adsorption definition, mechanisms and isotherms. Chapter three presents a literature review, isotherms, application. Chapter four presents the materials that will be used in this project. Chapter five presents the feasibility study and chapter six presents the results and discussion and chapter seven is about conclusion.

Figure1: Schematic representation of the report layout

# Chapter 2: Adsorption

## 2.1 Adsorption definition

Adsorption is the adhesion of atoms, ions, or molecules from a gas, liquid, or dissolved solid to a surface. This process creates a film of the adsorbate on the surface of the adsorbent. This process differs from absorption, in which a fluid (the adsorbate) permeates or is dissolved by a liquid or solid (the absorbent).[23] Adsorption has been proved as an efficient removal process for a multiplicity of solutes in water treatment.[14, 24] Adsorption can result either from the universal van der Waals interactions (physical adsorption, physisorption) or it can have the character of a chemical process (chemical adsorption or chemisorption). [25, 26] Contrary to physisorption, chemisorption occurs only as a monolayer.[25, 26]

Adsorption is surface phenomenon which may be defined in terms of an unit operation in the chemical engineering sense and that operation which deals primarily with the utilization of surface forces, and concentration of materials on the surface of solid bodies referred to as adsorption.[27, 28]Adsorption phenomena have been	 known to mankind for a very long time, and they are increasingly utilized to perform desired bulk separation or purification purposes.[29] The heart of an adsorption process is usually a porous solid medium.[14] The use of porous solid is simply that it provides a very high surface area or high micropore volume and it is this high surface area or micropore volume that high adsorptive capacity can be achieved.[29] Adsorption is present in many natural, physical, biological, and chemical systems, and is widely used in industrial applications such as activated charcoal, capturing and using waste heat to provide cold water for air conditioning and other process requirements (adsorption chillers), synthetic resins, increase storage capacity of carbide-derived carbons, and water purification.[23] Adsorption, ion exchange, and chromatography are sorption processes in which certain adsorbate are selectively transferred from the fluid phase to the surface of insoluble, rigid particles suspended in a vessel or packed in a column.[30]

The extent of adsorption depends upon the following factors: nature of adsorbate and adsorbent, the surface area of adsorbent, activation of adsorbent, experimental conditions such as temperature, pressure, PH, concentration, time, amount of adsorbent, to check the propensity of adsorption process.[31]

## 2.2 Adsorption mechanism

The process of adsorption arises due to presence of unbalanced or residual forces at the surface of liquid or solid phase. These unbalanced residual forces have tendency to attract and retain the molecular species with which it comes in contact with the surface.[14] Adsorption process involves two components Adsorbent and Adsorbate. Adsorbent is the substance on the surface of which adsorption takes place, Adsorbate is the substance which is being adsorbed on the surface of adsorbent.[29]

Adsorption from solutions is a competitive process where equilibrium is determined by many factors resulted from adsorbents, adsorbates, and solvent properties. The porous structure of a solid, its energetic heterogeneity, and surface chemical properties are the main factors influencing adsorption equilibria. For a given adsorbent, the adsorption of it towards different adsorbates is a function of the solubility, polarity, structure, mass, and size of the adsorbate molecules.[32, 33]

Adsorption can be understood by considering a simple example. In case of liquid state, water molecule presents on the surface is attracted inwards by the molecules of water present in the bulk. This gives rise to surface tension.[27] While the molecule of water present within the bulk is equally attracted from all the sides and the net force experienced by the water molecule in bulk is zero. This clearly shows that particles at surface and particles at the bulk are in different environment.[34, 35]

Figure 2: adsorption occurs in liquid

Water molecules on surface are experiencing unbalanced forces as compared to molecules inside, which experiences forces from all direction.[34, 35]

## 2.3 Adsorption in textile wastewater treatment

One of the most effective methods for removal of organic dye pollutant is by adsorption.[36]Adsorption process has been widely used in industrial dye wastewater treatment, because adsorption is a well-known equilibrium separation process and is effective in wastewater treatment.[37, 38]

Organic dyes released to surface waters during printing and dyeing of textiles and clothing may be toxic above certain threshold concentrations to aquatic organisms.[39]  In addition, dye-containing wastewaters are commonly characterized by high salt content and slow biodegradation which makes removal by conventional wastewater treatment processes difficult.[40] Adsorption of dyes onto low-cost adsorbents is largely dependent on dye properties such as molecular structure and type, number and position of substituent in the dye molecule, source of raw materials used, preparation and treatment conditions such as pyrolysis temperature and activation time, surface chemistry, surface charge, pore structure, and surface area of the adsorbent.[41, 42]

# 2.4 Adsorption Isotherm

Adsorption isotherms are applied to obtain the relationship between amount of a substance adsorbed at constant temperature and its concentration in the equilibrium solution and describe how adsorbate interact with adsorbents and are important in optimizing the use of an adsorbent in a real adsorption processes. Three of the most widely used isotherms were chosen to evaluate the equilibrium results: Langmuir, Freundlich and SIPS isotherms.[30, 43, 44]

- Freundlich Adsorption Isotherm

One of the most popular adsorption isotherms used for liquids to describe adsorption on a surface having heterogeneous energy distribution is Freundlich isotherm. The non-linearized form of Freundlich isotherm model is given as the following equation (2-4-1):

qe=kf*c1n  ……………………… (2-4-1)

Where, n is a constant related to adsorption efficiency and energy of adsorption, kf is a constant measuring adsorption capacity and qe is an amount of adsorbate adsorbed. It describes adsorption processes on surface sites that are energetically heterogeneous.[43, 45-47]

The logarithm form of the Freundlich equation can be written as the following equation (2-4-2):

Logqe=logKf+ 1n logCe  ………………………  (2-4-2)

Where qe (mg/g) is the amount of adsorbed per unit mass adsorbent, Ce (mg/L) is the equilibrium concentration. Kfand n are Freundlich constants which are related to the adsorption capacity and adsorption intensity, respectively.Generally n>1 suggests favorable adsorption of adsorbate on the adsorbent. The greater the value of n the more sturdy the adsorption strength.[43, 45-48]

- Langmuir Adsorption Isotherm

Langmuir (1918) was the first to propose a coherent theory of adsorption onto a flat surface based on a kinetic viewpoint, that is there is a continual process of bombardment of molecules onto the surface and a corresponding evaporation(desorption) of molecules from the surface to maintain zero rate of accumulation at the surface at equilibrium.[29, 48]

It is based on four assumptions:

1. Surface is homogeneous, that is adsorption energy is constant overall sites.

2. Adsorbed molecules do not interact.

3. All adsorption occurs through the same mechanism.

4. At the maximum adsorption, only a monolayer is formed: molecules of adsorbate do not deposit on other, already adsorbed, molecules of adsorbate, only on the free surface of the adsorbent.[29]

Langmuir isotherm, applicable for homogenous surface adsorption, the non-linearized form of Langmuir isotherm model can be described as the following equation

qe=KLCa0Ce1+ KLCe   ……………………… (2-4-3)

Where Ce (mg/L) is the equilibrium concentration, qe (mg/g) is the amount of adsorbed per unit mass adsorbent. ca (mg/g) and KL (L/mg) are Langmuir constants which are related to the adsorption capacity and rate of adsorption, respectively.[43, 45-47]

The term describing essential characteristics of the monolayer equation is referred to as dimensionless separation factor (RL), defined as equation (2-4-4)

RL= 11+ KLC0	 ……………………… (2- 4- 4)

Where KL is the Langmuir constant and Co is the highest initial concentration. The value of RL indicates whether it is unfavorable (RL> 1), linear (RL= 1), favorable (0 < RL< 1) or irreversible (RL= 0).[43, 45]

- SIPS  Adsorption Isotherm

SIPS isotherm, is a heterogeneous adsorption system, the non-linearized form of SIPS isotherm model can be described as the following equation

Qe=QmKsCens1+KsCens……………………… (2-4-5)

Where Qe is the number of moles of adsorbed per surface area of the dried nanoparticles (μmolm2), Ce is the equilibrium concentration of adsorbent in the supernatant (μmolL), Qm is the maximum adsorption capacity for complete monolayer coverage (μmolm2), Ks is the equilibrium constant of adsorption reaction related to the adsorption affinity (Lμmol), ns is the Sips constant related to the heterogeneity factor (unitless).[17]

# Chapter 3: Literature Review

(Nassar et.al.2015)[9] Investigated on synthetics and real textile wastewater treatment by using magnetic iron dioxide nanoparticle (γ-Fe2O3) with dye adsorption. They use this nanoparticle because it has good properties such as large specific surface area per mass. This study considers the effects of different experimental parameters on dye removal. Such as contact time, initial concentration, solution pH, and coexisting ions. The result of this study shows that that the dye adsorption was fast and equilibrium was achieved in less than 125 min for dye in real textile wastewater. (γ-Fe2O3) nanoparticle was successfully applied to remove dyes from textile wastewater.

(Hmoudah et.al.2016)[17] Showed the synthesis of nanopyroxene (NaFeSi2O6), they tried different sizes of nanopyroxene and surface and structural modified and that by replacing some of original atoms like Ce, Zr, H and Ca instead of Fe, Si and Na, also by adding Ni to NaFeSi2O6. All this functionalities were done to enhance their adsorption quality. Characterization techniques like XRD, BET, FTIR, TGA, TRD-Co2, XPS, and SEM were characterized to modify surface structure and different sizes of nanoparticles. The other aim of this study is to study the effect of nanopyroxene on Violantthrone -79 (Vo-79) which is a model molecule mimics behavior of asphaltenes. The result showed that the nanopyroxene (aegirine) has good properties such as high surface area and the adsorption capacity of these nanoparticles was in the range between 30 to 60 nm and doubled the adsorption capacity.

(Xiaolei Qu.et al.2013)[49] Talked about the importance of nanotechnology in advancing water and wastewater treatment. One of these nanomaterial is carbon based nano adsorbent (CNT) which shown higher efficiency than activated carbon on adsorption of various organic chemicals and this higher efficiency come from the large specific surface area and the diverse contaminate-CNT interactions including hydrophobic effect,π-π interaction, hydrogen bonding, covalent bonding and electrostatic interaction. The major drawback of activated carbon is its low adsorption affinity for low molecular weight polar organic compound adversely to CNT which strongly adsorb many of these polar organic compounds. Oxidized CNT is important for heavy metal removal, the surface functional group such as carboxyl, hydroxyl and phenol are the major adsorption sites for metal ions.

Another nanomaterial that studied is metal oxide such as iron oxide, titanium dioxide and alumina which are effective, low cost adsorbents for heavy metals and radionuclides. Dendrimers which are one of polymeric nano adsorbents are tailored adsorbents that are capable of removing both organic and heavy metals. Their interior shells can be hydrophobic for sorption of organic compounds while the exterior branches can be tailored for adsorption of heavy metals.

Among these studies on nanomaterial promise to show in full scale application in the near future because some of these nano still in the laboratory research stage and some have made their way to pilot testing or even commercialization.

(El-Qanni.et al, 2016)[50] Studied iron oxide nanoparticle applications for wastewater treatment primarily focused on applying nanoparticles as adsorbents for removal of contaminants, typically metal ions and ionic organic compounds (like dyes). They used iron oxide nanoparticles due to its unique features, such as high surface area to volume ratio, magnetism, biocompatibility, natural occurrence and catalytic oxidizing capabilities. According to environmental effect, iron oxide nanoparticles are considered to be inert, highly stable and naturally occurring.

In this study, they integrated the adsorption process as a non-classical technique for removing dyes, exemplified by methylene blue. The adsorption isotherms were determined and were described by the Freundlich and Langmuir isotherms and fit to Freundlich model.

(Mahapatra.et al, 2013)[51] Studied the nanocomposites composed of mixed iron and aluminum oxide (Fe2O3- Al2O3) as adsorbent for the adsorptive decolorization of Congo red dye from wastewater. They used these nanocomposites because of its advantages such as low cost, extensive availability, thermal stability and remarkable adsorption capacity. Effects of pH, contact time and initial concentration of adsorbate have been studied. So the result showed that adsorption equilibrium is attained within a short contact time of 15 min. and the adsorption capacity was found to be 498 mg/g in case of gamma mixed oxides, the optimum pH for maximum removal of Congo red was found to be 7 and the order of it was governed by pseudo-second-order kinetics.

(Ghaedi.et al, 2015)[52] Focused on removal of methylene blue and safranin-O, which are hazardous dyes, from wastewater by ultra-sonic-assisted adsorption onto the developed adsorbent that is Fe3O4 nanoparticles. Ultra sonic was used due to its high efficiency of water purification from chemically hazardous pollutants. The effects of variables such as pH, adsorbent dosage, methylene blue concentration, safranin-o concentration and contact time on dyes removal were examined and that values were found to be 6, 0.01g, 10 and 20 mg/l, respectively, and 2 min for contact time which showed a very rapid adsorption process. According to that, the removal percentage for each dye was predicted to be 99.9%.

(Gholivand.et al, 2015)[53] Studied the removal of tow anionic dyes from aqueous solutions by using the potential of polypyrrole-coated Fe3O4 nanoparticles. Adsorption has been considered as an effective method among many methods such as electrochemical degradation, ozonation, oxidation, photocatalysis, membrane filtration and biological treatment due to its low cost, simplicity of design, ease of operation without harmful residues and the possibility of regeneration of the adsorbent.

Polypyrrole-coated Fe3O4 used as adsorbent according to its high adsorption capacity and available at economical costs. Several parameters such as pH, sorbent amount and contact time were studied. This study showed that 0.1- 0.12 g/100ml of the adsorbent amount was achieved to remove dyes at pH 4-4.5 in 60 min, and the kinetic results showed that the pseudo-second-order equation was the best model.

(Nekouei.et al, 2015)[54] Showed the effective of removal acid blue 129 from liquids by using copper oxide nanoparticle-modified activated carbon as a novel adsorbent. Removal of this dye is necessary according to its harmful if there is contact to eyes, respiratory system and skin. The effects of pH, adsorbent dosage, initial dye concentration, contact time and temperature were examined and optimizing. So the investigation showed that the capacity adsorbent was 65.36 for the removal of acid blue 129 from aqueous solutions in a short time (<=25 min) and the maximum removal efficiency (around 100%) occurred at pH 2.

(Rajabi.et al, 2015)[55] Showed the application of cetyltrimethylammonium bromide (CTAB) coated magnetite nanoparticles (MNPs) as an adsorbent for removal of two types of disperse dyes, including disperse red 167 and disperse blue 183 from wastewater of textile companies. These dyes have most serious environmental problems and also affect the human health. The adsorbent which used in this study was selected due to its low cost and novel locally available.

In this study CTAB coated MNPs adsorbent were successfully applied to remove disperse dyes from wastewater and its efficiency was (>= 95%) at high concentration of the dyes. And the adsorbent capacity was 2000mg/g.

Chapter 4: Materials

## 4.1 Adsorbate

A real textile wastewater sample obtained from Al-Aqad Textile Company (Nablus) was used as   a source of real contaminants. The sample was light blue in color and free of suspended solid  particles .[9] We use simple dyes have different configurations and it that have been used in the textile industry such as methylene blue is Synonym: 3,7bis (Dimethylamino) phenazathionium chloride, Tetramethylthionine chloride, it is Empirical Formula (Hill Notation): C16H18ClN3S·xH2O, and it is Molecular Weight: 319.85 (anhydrous basis) Methylene blue was supplied by the university warehouse and it is a compound consisting of dark green crystals or crystalline powder, having a bronze-like luster.[5]  Solutions in water or alcohol have a deep blue color.  and has been used to treat cyanide poisoning and to lower levels of METHEMOGLOBIN.[6] As a model molecule for textile dyes, distilled water was employed for preparing  the solutions.[9] and   Methyl orange (4-[[(4-dimethylamino) phenyl]- azo] benzene sulfonic acid sodium salt) and all reagents.[56] Molecular formula is C14H14N3NaO3S as a model. molecule for textile and is an intensely colored compound used in dyeing and printing textiles.[7] Chemists use methyl orange as an indicator in the titration of weak bases with strong acids. Crystal violet C25H30ClN3 and Methyl black.

## 4.2 Adsorbent

Pyroxene is a term referring to a group of industrial minerals and materials include important elements of the Earth's crust and rocks lunar and Mars form.[57] It is environmentally friendly, where the general chemical formula of nanopyroxene is (M2M1T2O6) the  five-to eight-coordinated  M2cation  site  can  be  occupied  by elements like Na, K, Li, Ca, Ba , Fe2+, Mg and Sr while the six-coordinated M1site can be occupied by elements like Mg, Mn , Fe2+, Fe3+, Al, Cr, Ga, Zn, Ti3+, V, Sc, Cu, Co, Ni.[57] The nanopyroxene that contain silica which naturally exist constitute 25% of the size of Earth from the depths of 400 km. however, pyroxenes are produced by the mixture of oxides, hydroxides and carbonates  in  stoichiometric  ratios  and  heating  them  up  to high  temperatures  and pressures.[57] There are a series of industrial nanopyroxene possible to have the same chemical composition and is not possible. Nanopyroxene Synonym is NaFeSi2O6.[57]

Nano pyroxenes most commonly occur in intermediate to ultra-mafic igneous rocks, although they are also common in some medium-grade to high-grade metamorphic rocks. Pyroxene minerals share a similar crystal structure and their physical properties are so similar they are often only identified as ‘pyroxene’ in the field. All of them are harder than glass.[58] The nanopyroxene can be divided up into four subgroups, depending on whether they are relatively rich in calcium, magnesium, sodium or (more rarely) lithium ions.[58]Nanopyroxene nanoparticles with different surface and structural modifications:the atomic ratio of Si/Fe in pure nanopyroxene should always be fixed to 2.0. However, it is possible to artificially modify the structure of nanopyroxene by partially replacing Fe or Si during the synthesis by addition of other suitable elements, and in this way, an artificial modification of the Si/Fe atomic ratio can be carried out. To understand the effect of surface and structural modifications of PY nanoparticles on adsorption (hereinafter called functionalized PY nanoparticles).[17] Nanopyroxene for adsorption and catalytic thermal decomposition of visbroken residue asphaltenes.

X-ray diffraction (XRD):

Nanopyroxene nanoparticles (M2M1T2O6) were used as an adsorbent. The nanoparticles were used as received without further purification. The nanoparticles have a size of 10±2 nm structure and particle size was determined using an X-ray diffraction System.[9] The XRD  measurements  of  dried  powder  different-sized,  surface  and  structural-modified  nanopyroxene were  collected  at  room  temperature  using  X-ray  Ultima  III  Multi-Purpose Diffraction System (Rigaku Corp, The Woodlands, TX) with Cu KD radiation operating at 40 kV and 44 mA with a T-2Tgoniometer.[17] X-ray diffraction analysis of the different-sized nanopyroxene nanoparticles is shown in Figure1, which confirmed that the correct structure is nanopyroxene. The sharp peaks in the XRD patterns imply good crystallinity of all products.[17] The  identification  of  the  patterns  confirms  the material  to  be  nanopyroxene.[17] Noticeable  changes  in  the  signals  intensities  and  broadenings  are  produced .[17]Nanopyroxene nanoparticle produced the broad signals, indicating that this material has the small crystalline domain size.[17]

Figure 3:XRD powder of nanopyroxene for particle size

Textural properties:

The surface areas of the prepared different-sized, surface and structural-modified nanopyroxene nanoparticles were measured following the Brunauer-Emmett-Teller (BET) method. This was accomplished by performing nitrogen physisorption at 77 K using a surface area and porosity analyzer (TriStar II 213020, Micrometrics Corporate, norcross, GA). An estimation of the particle size (assuming spherical-like nanoparticles)  was  accomplished  by  using  the  measured  specific  surface  area  and  the derived  equation d =6000⁄(SAPnanopyroxene)  ;  where d is  the  particle  size  in  nm, SA is  the experimentally measured specific surface area (m2/g), and P the aegirine density (3.577 g/cm3) .[17]

When the particle size nanopyroxene significant deviation is observed in crystalline domain size obtained by XRD and the particle size obtained by BET as listed in Table 1. The ultrafine nanoregime, particle size and crystalline domain size are very similar.[17]

Table 1: BET  surface  area,  particle  size  and  XRD  crystalline  size  of  different-sized  nanopyroxene nanoparticles

| Sample | BET surface area (m2/g) | Particle size by BET (nm) | domain size by XRD (nm) |
| --- | --- | --- | --- |
| PY-10 (nanopyroxene) | 160 | 10 | 10±2 |

Scanning electron microscopy (SEM):

Scanning  electron  microscopy  was  performed  to  study  the  surface  morphology  of  the  different-sized nanopyroxene nanoparticles. A field emission Quanta 250 electron microscope manufactured by FEI was used, with an accelerating voltage of 20 kV and a spot size of 3.0. SEM image is important to investigate the surface morphology and the nanoparticles shape in the first place. The representative SEM image of the surface of the nanopyroxene showed morphology quite as seen in Figure 2 for the small crystalline domain size and nanopyroxene there in nature to form Fibers.[17]

Figure 4: SEM image for nanopyroxene

High resolution transmission electron microscopy (HRTEM):

Transmission electron microscopy images for different-sized nanopyroxene nanoparticles were obtained via FEI Tecnai F20 FEG TEM using an accelerating voltage of 200 kV to analyze the nanoparticle size   and   morphology. This   technique provides   atomic-resolution   real   space   imaging   for nanoparticles. In order to investigate the real shape of the nanoparticle HRTEM image, as seen in Figure3, nanoparticles are spherical in shape for nanopyroxene nanoparticles of size 10.[17]

Figure 5: HRTEM images for size nanopyroxene

FTIR analysis of sized nanopyroxene nanoparticles:

FTIR was employed to examine existing hydroxyl stretching bands. Therefore, hydroxyl density on the surface is needed to determine the amounts of OH moieties on each surface. Figure 4,shows the infrared spectra of the prepared sized nanopyroxene nanoparticles.[17]

Figure 6: Infrared spectroscopy of the prepared pyroxene nanoparticles for the hydroxyl group region for nanopyroxene.

X-ray Photoelectron Spectroscopy (XPS):

XPS  analysis  was  performed  to  confirm  the  elemental  and  the  surface  composition  for  the functionalized PY nanoparticles. XPS was carried out with a PHI Versa Probe 5000 spectrometer.[17]

Thermo gravimetric analysis (TGA):

TGA was used to determine the hydroxyl group density on the surface of the prepared different-sized PY nanoparticles.[17]

# Chapter 5: Feasibility Study

To check if the price of 1 kg is efficient or not, the prices of raw materials which entered in the preparation of nanopyroxene were taken from Eng. Majed Abu Kharmi and the prices were taken per 1 Kg.

The raw materials and there's amounts  that entered in the preparation of 2 g of nanopyroxene were 3.2g  NaOH,4.9g Sodium Silicate,2.4g  H2SO4 and 2.8g FeCl3. The prices of them shown in the following table (2)

Table 2: the prices of raw materials

| Raw material | Price(ILS/Kg) |
| --- | --- |
| Sodium hydroxide(NaOH ) | 5 |
| Sodium silicates | 4 |
| H2SO4 | 25 |
| FeCl3 | 11 |

The cost for 2 g of nanopyroxene:

The price of 1000 g NaOH = 5 ILS

The price or 3.2 g NaOH = 3.2*51000 = 0.016 ILS

The price of 1000 g Sodium Silicate = 4ILS

The price or 4.9 g Sodium Silicate = 4.9*41000 = 0.0196 ILS

The price of 1000 g H2SO4= 25ILS

The price or2.4 g Sodium Silicate = 2.4*251000 = 0.06 ILS

The price of 1000 FeCl3= 11ILS

The price or2.8 g Sodium Silicate = 2.8*111000 = 0.0308 ILS

So the cost of raw materials for 2g of nonopyroxene = 0.016 + 0.0196 + 0.06 + 0.0308 = 0.1264 ILS.

And the cost of raw materials to produce 1 Kg of nanopyroxene =1000g *0.1264NIS2=63.2 ILS

The price of electricity of the oven that needed to prepare 2 g of nonopyroxene was consumed from the oven for 72 hours. And the price of 1 KW of electricity = 0.67 ILS. So for 72 hour the price of electricity for produce nanopyroxene = 72 * 0.67 = 48.24 ILS.

And now the total cost of producing 1 Kg of nanopyroxene = 63.2 + 48.24 = 111.44 ILS.

The amount of adsorbate cannot be found due to problems in the concentration of the diluted samples so the price of the nonopyroxene cannot be decided if it efficient or not.

# Chapter 6: Results and discussion

Figure (7) show that the adsorption was occurred due to the removal of the color from water sample. To know how the mechanism of the adsorption occur the isotherm and thermo dynamic study should be done.

a)b)

.

Figure 7: The samples of textile wastewater: a) before testing. b) After testing with aegirine.

## 6.1 COD results

Firstly, 6 samples  prepared with  different dilution percent (100%, 85%, 70%, 55%, 40%  & 25%)   from the original sample . 5 ml from each dilution  were added to Viles which contain approximately 0.05g of nanopyroxen. Adsorption isotherm was done at 250C, 350C, 450C for 6 samples. These samples were put in the shaker for 24 h and 150 RPM. After that,the samples were settling out for another 24 hour to separate the nanoparticle from water samples. The concentration of the dilution samples before adsorption (without nanopyroxen) (C0) and after adsorption (C) were measured by COD and its result shown in the table 3, 4, 5.

Table 3: the results of COD test at 250C

| # sample | Dilution% | C0(PPM) | C(PPM) |
| --- | --- | --- | --- |
| 1 | 100 | 344 | 221 |
| 2 | 85 | 302 | 312 |
| 3 | 70 | 110 | 158 |
| 4 | 55 | 116 | 181 |
| 5 | 40 | 112 | 225 |
| 6 | 25 | 94 | 163 |

Table 4: the results of COD test at 350C

| # sample | Dilution% | C0(PPM) | C(PPM) |
| --- | --- | --- | --- |
| 1 | 100 | 344 | 81 |
| 2 | 85 | 302 | 251 |
| 3 | 70 | 110 | 109 |
| 4 | 55 | 116 | 148 |
| 5 | 40 | 112 | 160 |
| 6 | 25 | 94 | 171 |

Table 5: the results of COD test at 450C

| # sample | Dilution% | C0(PPM) | C(PPM) |
| --- | --- | --- | --- |
| 1 | 100 | 344 | 315 |
| 2 | 85 | 302 | 440 |
| 3 | 70 | 110 | 203 |
| 4 | 55 | 116 | 236 |
| 5 | 40 | 112 | 244 |
| 6 | 25 | 94 | 262 |

These results were randomly changed at the time they must decrease when the dilution decreased. Maybe there are problems in the procedure of running COD test.  The sample of water before and after adsorption weren’t done at the same condition, and also some nanoparticles of pyroxene may didn’t separate completely from water sample, so the adsorption for 6 samples were rebated at 25 0C for 24 h. Then centrifuge device was used to separate nanopyroxene completely for 5min at 2500 rpm.  After that the results were taken by COD device and table 6shows the results.

Table 6: the result of COD test at 250C

| # sample | Dilution% | C0(PPM) | C(PPM) |
| --- | --- | --- | --- |
| 1 | 100 | 44 | 530 |
| 2 | 85 | 30 | 63 |
| 3 | 70 | 37 | 289 |
| 4 | 55 | 22 | 30 |
| 5 | 40 | 18 | 754 |
| 6 | 25 | 0 | 256 |

Also these results are not reasonable so the samples were measured by using the COD device in water and environment studies institute (WESI)in the scientific centers building to check the reproducibility of the results if the problem from COD device or not. The following table (7) showing the results of COD for the original water samples before adsorption.

Table 7: the result of COD test from WESI

| # sample | Dilution % | C0(PPM) |
| --- | --- | --- |
| 1 | 100 | 46 |
| 2 | 85 | 16 |
| 3 | 70 | 7 |
| 4 | 55 | 0 |
| 5 | 40 | 19 |

Based on these results we consider that the COD device is not suitable for our experiment because COD is very sensitive to any very few particles and the wastewater have a high total suspended solid (TSS) and as dilution increase the error in readings will increase, so the isotherm study can't apply. And another technique is used which is UV spectrophotometer.

## 6.2 UV-Spectrophotometer results

Firstly, 5 samples prepared with different dilution percent (100%, 80%, 60%, 40% & 20%)   from the original sample. 5 ml from each dilution were added to Aviles which contain approximately 0.05g of nanopyroxen, and another 5 ml from each dilution were added to Aviles without nanopyroxen, all the samples were put in the shaker for 24 h and 150 RPM. After that, the centrifuge device was used to separate nanoparticle from water samples for 1 hour at 3000 rpm.  The absorbance of the dilution samples before adsorption (without nanopyroxen) and after adsorption were measured by UV-Spectrophotometer device and table 8 & table 9show the UV result

Table 8: The UV-spectrophotometer results before adsorption

| # samples | Dilution percent% | Peak(nm) | Absorbance |
| --- | --- | --- | --- |
| A1 | 100 | 277 | 0.229 |
| A2 | 80 | 281 | 0.148 |
| A3 | 60 | 281 | 0.103 |
| A4 | 40 | 281 | 0.101 |
| A5 | 20 | 287 | 0.069 |

Table 9: The UV-spectrophotometer results after adsorption

| # samples | Dilution percent% | Peak(nm) | Absorbance |
| --- | --- | --- | --- |
| A6 | 100 | 281 | 0.167 |
| A7 | 80 | 281 | 0.165 |
| A8 | 60 | 281 | 0.188 |
| A9 | 40 | 272 | 0.199 |
| A10 | 20 | 281 | 0.103 |

The following figures show the amount of absorbance vs. wavelength and specify the peaks

Figure 8: Abs vs. wavelength before adsorption for dilution 100%

Figure 9: Abs vs. wavelength after adsorption for dilution 100%

Figure 10: Abs vs. wavelength before adsorption for dilution 80%

Figure 11: Abs vs. wavelength after adsorption for dilution 80%

Figure 12: Abs vs. wavelength before adsorption for dilution 60%

Figure 13: Abs vs. wavelength after adsorption for dilution 60%

Figure 14: Abs vs. wavelength before adsorption for dilution 40%

Figure 15: Abs vs. wavelength before adsorption for dilution 40%

Figure 16: Abs vs. wavelength before adsorption for dilution 40%

Figure 17: Abs vs. wavelength before adsorption for dilution 20%

The results of UV for the diluted samples before adsorption were acceptable; when the percentage of diluted samples decreased the absorbance value decreased gradually but after adsorption the reading of the UV done randomly. This means that adsorption processes didn’t set correctly at 250C. This indicates that there is a specific metal in the water sample didn’t adsorbed by nanopyroxene at wavelength equal approximately 281nm.

## 6.3 Regeneration and reuse

The possible method for regeneration and reuse the nanopyroxene

1. High temperature calcination by setting the adsorbent in the furnace with air and calcined with different temperature at different time.[59]

2. Desorption by using acidic solution such as HCl.[60]

# Chapter 7: Conclusion

In this study, the adsorption of dyes from textile wastewater by using nanopyroxene as adsorbent was investigated. COD and UV-Spectrophotometer devices were used to found the results of diluted samples before and after adsorption which must indicate the efficiency of nanopyroxene for adsorption of dyes from textile wastewater.

Unfortunately the results for both devices were unreasonable because as the dilution factor increase the readings of COD must decrease. However they were randomly changed maybe due to the high total suspended solid. Also for the UV- Spectrophotometer the results before adsorption were corrected as the dilution factor decrease the absorbance were decreased but for the samples after adsorption the absorbance were randomly changed and that unreasonable, this indicates that there is a specific metal in the water sample didn’t adsorbed by nanopyroxene at wavelength equal approximately 281nm. According to the results the adsorption isotherm and thermodynamics study cannot applied.

# Chapter 8: References

1.	Tchobanoglous, G., et al., Wastewater engineering : treatment and reuse. 2003, Boston: McGraw-Hill.

2.	Utilization of Textile Effluent Waste Sludge in Brick Production. 2014.

3.	Salehi, R., et al., Novel biocompatible composite (Chitosan–zinc oxide nanoparticle): Preparation, characterization and dye adsorption properties. Colloids and Surfaces B: Biointerfaces, 2010. 80(1): p. 86-93.

4.	R Ananthashankar, A.E.G., Production, Characterization and Treatment of Textile Effluents: A Critical Review. Chem Eng Process Technol Journal of Chemical Engineering & Process Technology, 2013. 05(01).

5.	Tan, K.A., et al., Removal of Cationic Dye by Magnetic Nanoparticle (Fe3O4) Impregnated onto Activated Maize Cob Powder and Kinetic Study of Dye Waste Adsorption. APCBEE Procedia, 2012. 1: p. 83-89.

6.	Afkhami, A., M. Saber-Tehrani, and H. Bagheri, Modified maghemite nanoparticles as an efficient adsorbent for removing some cationic dyes from aqueous solution. Desalination, 2010. 263(1–3): p. 240-248.

7.	Emami, F., et al., Kinetic study of the factors controlling Fenton-promoted destruction of a non-biodegradable dye. Desalination, 2010. 257(1–3): p. 124-128.

8.	Tsui, L.S., W.R. Roy, and M.A. Cole, Removal of dissolved textile dyes from wastewater by a compost sorbent. Coloration Technol Coloration Technology, 2003. 119(1): p. 14-18.

9.	Nassar, N.N., et al., Adsorptive removal of dyes from synthetic and real textile wastewater using magnetic iron oxide nanoparticles: Thermodynamic and mechanistic insights. The Canadian Journal of Chemical Engineering, 2015. 93(11): p. 1965-1974.

10.	Zhu, H.-Y., et al., A novel magnetically separable γ-Fe 2 O 3/crosslinked chitosan adsorbent: preparation, characterization and adsorption application for removal of hazardous azo dye. Journal of Hazardous Materials, 2010. 179(1): p. 251-257.

11.	Nawaz, M.S. and M. Ahsan, Comparison of physico-chemical, advanced oxidation and biological techniques for the textile wastewater treatment. Alexandria Engineering Journal, 2014. 53(3): p. 717-722.

12.	Biological Treatment of a Synthetic Dye Water and an Industrial Textile Wastewater Containing Azo Dye Compounds. 2001.

13.	Afkhami, A. and R. Moosavi, Adsorptive removal of Congo red, a carcinogenic textile dye, from aqueous solutions by maghemite nanoparticles. Journal of Hazardous Materials, 2010. 174(1–3): p. 398-403.

14.	Worch, E., Adsorption technology in water treatment : fundamentals, processes, and modeling. 2012, Berlin; Boston: De Gruyter.

15.	Nassar, N.N., Kinetics, Mechanistic, Equilibrium, and Thermodynamic Studies on the Adsorption of Acid Red Dye from Wastewater by γ-Fe2O3 Nanoadsorbents. Separation Science and Technology, 2010. 45(8): p. 1092-1103.

16.	Oliveira, L.C.A., et al., Clay–iron oxide magnetic composites for the adsorption of contaminants in water. Applied Clay Science, 2003. 22(4): p. 169-177.

17.	Hmoudah, M., et al., Effect of nanosized and surface-structural-modified nano-pyroxene on adsorption of violanthrone-79. RSC Advances, 2016. 6(69): p. 64482-64493.

18.	Roco, M.C., Nanotechnology: convergence with modern biology and medicine. Current Opinion in Biotechnology, 2003. 14(3): p. 337-346.

19.	Fleischer, T. and A. Grunwald, Making nanotechnology developments sustainable. A role for technology assessment? Journal of Cleaner Production, 2008. 16(8–9): p. 889-898.

20.	Masciangioli, T. and W.-X. Zhang, Peer Reviewed: Environmental Technologies at the Nanoscale. Environmental Science & Technology, 2003. 37(5): p. 102A-108A.

21.	Fernández-García, M. and J.A. Rodriguez, Metal Oxide Nanoparticles, in Encyclopedia of Inorganic and Bioinorganic Chemistry. 2011, John Wiley & Sons, Ltd.

22.	Kahru, A., et al., Biotests and Biosensors for Ecotoxicology of Metal Oxide Nanoparticles: A Minireview. Sensors, 2008. 8(8): p. 5153.

23.	Dąbrowski, A., Adsorption — from theory to practice. Advances in Colloid and Interface Science, 2001. 93(1–3): p. 135-224.

24.	Brownfields and C. Land Revitalization Technology Support, Brownfields technology primer : vapor intrusion considerations for redevelopment. 2008, Washington DC: U.S. Environmental Protection Agency, Office of Solid Waste and Emergency Response, Brownfields and Land Revitalization Technology Support Center.

25.	Adamson, A.W. and A.P. Gast, Physical chemistry of surfaces. 1997.

26.	Sharma, S.K. and R. Sanghi, Advances in water treatment and pollution prevention. 2012.

27.	Roque-Malherbe, R.M.A., Adsorption and diffusion in nanoporous materials. 2007, Boca Raton: CRC Press.

28.	Lata, S., P.K. Singh, and S.R. Samadder, Regeneration of adsorbents and recovery of heavy metals: a review. Int. J. Environ. Sci. Technol. International Journal of Environmental Science and Technology, 2015. 12(4): p. 1461-1478.

29.	Duong, D.D., Adsorption analysis : equilibria and kinetics. 1998.

30.	Guimarães Gusmão, K.A., et al., Application of succinylated sugarcane bagasse as adsorbent to remove methylene blue and gentian violet from aqueous solutions – Kinetic and equilibrium studies. Dyes and Pigments, 2012. 92(3): p. 967-974.

31.	Mittal, A., L. Kurup, and J. Mittal, Freundlich and Langmuir adsorption isotherms and kinetics for the removal of Tartrazine from aqueous solutions using hen feathers. Journal of Hazardous Materials, 2007. 146(1–2): p. 243-248.

32.	Bhatnagar, A. and A.K. Minocha, Conventional and non-conventional adsorbents for removal of pollutants from water - A review. Indian journal of chemical technology., 2006. 13(3): p. 203-217.

33.	Wu, Z.j. and K. Lee, Adsorption Mechanisms of Mesoporous Adsorbents in Solutions. CHEMICAL RESEARCH IN CHINESE UNIVERSITIES, 2004. 20: p. 185-187.

34.	Jaroniec, M., Physical adsorption on heterogeneous solids. Advances in Colloid and Interface Science, 1983. 18(3): p. 149-225.

35.	Deryło-Marczewska, A. and A.W. Marczewski, Effect of adsorbate structure on adsorption from solutions. Applied Surface Science, 2002. 196(1–4): p. 264-272.

36.	Başar, C.A., Applicability of the various adsorption models of three dyes adsorption onto activated carbon prepared waste apricot. Journal of Hazardous Materials, 2006. 135(1–3): p. 232-241.

37.	Bansal, R.C. and M. Goyal, Activated carbon adsorption. 2005, Boca Raton: Taylor & Francis.

38.	Freeman, H.M., Standard handbook of hazardous waste treatment and disposal. 1989: New York, NY (US); McGraw-Hill Book Company; None. Medium: X; Size: Pages: (1036 p).

39.	A.S, A.L., Adsorption of methylene blue from aqueous solution onto a low-cost natural Jordanian Tripoli. Am. J. Appl. Sci. American Journal of Applied Sciences, 2009. 6(6): p. 1047-1058.

40.	Ouasif, H., et al., Removal of a cationic dye from wastewater by adsorption onto natural adsorbents. J. Mater. Environ. Sci. Journal of Materials and Environmental Science, 2013. 4(1): p. 1-10.

41.	Reife, A. and H.S. Freeman, Environmental chemistry of dyes and pigments. 1996, New York: Wiley.

42.	Rafatullah, M., et al., Adsorption of methylene blue on low-cost adsorbents: A review. HAZMAT Journal of Hazardous Materials, 2010. 177(1-3): p. 70-80.

43.	Garba, Z.N. and A.A. Rahim, Adsorption of 4-Chlorophenol onto optimum activated carbon from an agricultural waste. Internal journal of science and research (IJSR), 2015. 4(5).

44.	Alqaragully, M.B., Removal of textile dyes (Maxilon blue, and Methyl orange) by date stones activated carbon. International journal of advanced research in chemical science (IJARCS), 2014. 1(1): p. 48-59.

45.	S.E, A., et al., Equilibrium adsorption studies of methylene blue onto palm kernel shell-based activated carbon. International Refereed Journal of Engineering and Science, 2013. 2(5): p. 38-45.

46.	Chen, X., Modeling of Experimental Adsorption Isotherm Data. Information, 2015. 6(1): p. 14.

47.	Dalali, N., et al., Magnetic removal of acidic dyes from wastewaters using surfactant-coated magnetite nanoparticles: optimization of process by Taguchi method. International conference on environmental and agriculture engineering 2011. 15: p. 89-93.

48.	Liu, M., et al., Comparison of reverse osmosis and nanofiltration membranes in the treatment of biologically treated textile effluent for water reuse. Desalination, 2011. 281: p. 372-378.

49.	Qu, X., P.J.J. Alvarez, and Q. Li, Applications of nanotechnology in water and wastewater treatment. Water Research, 2013. 47(12): p. 3931-3946.

50.	El-Qanni, A., et al., Maghemite nanosorbcats for methylene blue adsorption and subsequent catalytic thermo-oxidative decomposition: Computational modeling and thermodynamics studies. Journal of Colloid and Interface Science, 2016. 461: p. 396-408.

51.	Mahapatra, A., B.G. Mishra, and G. Hota, Adsorptive removal of Congo red dye from wastewater by mixed iron oxide–alumina nanocomposites. Ceramics International, 2013. 39(5): p. 5443-5451.

52.	Ghaedi, M., et al., Modeling of competitive ultrasonic assisted removal of the dyes – Methylene blue and Safranin-O using Fe3O4 nanoparticles. Chemical Engineering Journal, 2015. 268: p. 28-37.

53.	Gholivand, M.B., et al., Adsorptive removal of alizarin red-S and alizarin yellow GG from aqueous solutions using polypyrrole-coated magnetic nanoparticles. Journal of Environmental Chemical Engineering, 2015. 3(1): p. 529-540.

54.	Nekouei, F., et al., Kinetic, thermodynamic and isotherm studies for acid blue 129 removal from liquids using copper oxide nanoparticle-modified activated carbon as a novel adsorbent. Journal of Molecular Liquids, 2015. 201: p. 124-133.

55.	Rajabi, A.A., et al., Modified magnetite nanoparticles with cetyltrimethylammonium bromide as

superior adsorbent for rapid removal of the disperse dyes from wastewater of textile

companies`. Journal of the iranian chemical society, 2015. 1: p. 49-56.

56.	Arabatzis, I.M., et al., Silver-modified titanium dioxide thin films for efficient photodegradation of methyl orange. Applied Catalysis B: Environmental, 2003. 42(2): p. 187-201.

57.	Iron Silicate Nano-Crystals as Potential Catalysts or Adsorbents for Heavy Hydrocarbons Upgrading. 2013.

58.	Morimoto, N., Nomenclature of Pyroxenes. Mineralogy and Petrology Mineralogy and Petrology, 1988. 39(1): p. 55-76.

59.	Wang, S., et al., Physical and chemical regeneration of zeolitic adsorbents for dye removal in wastewater treatment. Chemosphere, 2006. 65(1): p. 82-87.

60.	Zhang, J., et al., Pb(II) removal of Fe3O4@SiO2–NH2 core–shell nanomaterials prepared via a controllable sol–gel process. Chemical Engineering Journal, 2013. 215–216: p. 461-471.