## Slide 1
Synthesis of Watermelon Seed Husk Based Activated Carbon Ablated by Laser for Supercapacitor Electrode Material and Adsorption of Methylene Blue Dye
Graduation Project Defense
Supervisors: Amer El-Hamouz
Iyad Saad Al-Deen
Prepared by: Anas Draidi
Kareema Dababat Manal Tuffaha

## Slide 2
01
Significance
02
Introduction
03
Experimental Work
04
CONTENTS
Results
05
06
Future Work
Objectives

## Slide 3
01
Significance
01
Laser ablation
Synthesis
Properties
Usage
Laser ablation
Methylene blue
What is it
Effects on environment
Removal
Supercapacitor
Differs form traditional capacitor
Types
Material used

## Slide 4
02
Objectives
1
2
3
Synthesize activated carbon.
Enhance AC via laser ablation.
Fabricate SC electrodes from CC, AC and LAC.
Perform electrochemical tests and FTIR.
4
5
Test CC, AC and LAC as methylene blue adsorbents.
Compare the latter’s performance.
6
02

## Slide 5
Experimental Work
04

## Slide 6
Pretreatment of watermelon seed husks
RSH
05

## Slide 7
2 Hrs
500 ℃
N2
Carbonization
Through
Pyrolysis
CC
06

## Slide 8
Soaking
Washing
100℃
Washing with boiling deionized water
Soaking in zinc chloride
24 hours
Preparation Pre-activation
ZnCl2
07

## Slide 9
AC
Activation
08

## Slide 10
  Laser Ablation
LAC
09

## Slide 11
SC
10

## Slide 12
CC
AC
LAC
CC
AC
LAC
Methylene
Blue
Adsorption
Adsorbents were inserted
Samples were put in the shaker
Withdrawn every 10 minutes and filtered
Color fading was observed
Batch
Experiment
11

## Slide 13
Results and Discussion
MB
FTIR
GCD
CV
EIS
SC
12

## Slide 14
Chart: Potential (v)
CC
LCC
Cyclic Voltammetry
13

## Slide 15
Galvanostatic Charge-Discharge
14

## Slide 16
Electrochemical Impedance Spectroscopy
15

## Slide 17
Electrochemical Tests Results
Cs (F/g)
Specific Capacitance Values
16

## Slide 18
CC
R%=0.08%
LAC
R%=99.1%
AC
R%=64.9%
MB
Adsorption
Results
At 40 minutes
17

## Slide 19
FTIR
RSH
AC
CC
RSH
CC
AC
LAC
LAC
18

## Slide 20
AC
LAC
CC
Cs: 190.9 F/g
R%: 99.1%
Approximated Surface Area: 2247 m2/g
Cs: 160.1 F/g
R%: 64.9%
Approximated Surface Area: 1473 m2/g
Cs: 91.06 F/g
R%: 0.08%
Overall Results
19

## Slide 21
Study the adsorption
kinetics of MB dye
SEM, TEM, XRD, and BET
Optimize the synthesis parameters
Optimize the laser ablation parameters
Explore different activation methods
Composite materials for SC electrodes.
Explore different post-treatment methods
Conduct long-term cyclic stability tests
Evaluate the economic feasibility
Include the desorption of MB
05
Future Work
20

## Slide 22
THANK YOU!