## Slide 1: An- Najah National University Faculty of Engineering Chemical Engineering Department Graduation project 2
Experimental Investigation on the Performance of phase change material (PCM)-Incorporated With Solar Water Heating System.
Supervisor: Dr. Abdelrahim AbuSafa
Prepared by:
Obada Dwekat
Taha Karaki
Ali Musmar
May, 2019

## Slide 2: Table of content
Introduction
Objectives
Methodology
Results
Conclusion and recommendations
Acknowledgment
References

## Slide 3: Introduction
In Palestine, people suffer from scarcity of energy resources for many reasons. Mainly because of the great population growth with bad economic situation, as well as weak infrastructure and Israeli occupational policies.
Energy storage is considered one of the most efficient methods for minimizing this problem. So that PCM is studied as an application of thermal energy storage as shown in figure (1).
Solar energy
Potential solar energy about 3000 sunshine hours per year.[1]
Average solar radiation 5.4 kW h/m2.day on horizontal surface. [1]
These values show the efficiency of utilization solar energy in solar water heaters (SWH) in Palestine; due to the high number in solar radiation and sunshine hours. As shown in (figure2) 65% of water heating depend on solar energy.
Figure (1) : Latent heat storage for solid –liquid phase change [2]
Figure (2) : Distribution of energy consumption for water heating, 2013

## Slide 4: Objectives
Design and construct a new solar water heater tank, integrated with PCM storage in the aim of reduce the solar water heater tank size.
Simulate the charging and discharging behavior of the constructed system using variable power electrical heater tank, coupled with the PCM storage tank.

## Slide 5: Methodology
The main units of the system as shown in figure(3) are :
Hot water storage tank ( Galvanized steel )
Electric heater (Variable power)
Thermocouples
Pipe and Fittings
PCM storage tank (stainless steel 304 L)
Figure (3): Pilot System-P&ID
Hydrocarbons paraffin wax was selected due to its,
Availability and low price
Unchanged thermal properties
Suitable melting and solidification prop rites
Melting temperature (C) : 55
Latent heat of fusion (kJ/kg]) : 190

## Slide 6: Methodology
Rig Tests
(Charging and discharging with and without PCM)
Batch wise system
Continuous system
Design Constrains
PCM mass/ water volume not less than 30%
Flow Rate : 0.25 – 0.3 L/min.
Heater Power : 500, 700 and 900 W.
Experimental Outcomes :
1- Hot water supply ( Time and temperature ).
2- Effect of Using PCM in the system.
3- Charging and Discharging Time.
Chart: hour
 | 0.1 | 2.5 | 1.2 | 1 | 1.1 | 2 | 6.5 | 15.5 | 17.5 | 15.9 | 13.5 | 11.6 | 9.5 | 8 | 7 | 6.2 | 6.3 | 7.7 | 10.1 | 12 | 12.1 | 11 | 9.7 | 7.8
Household water consumption [3].
Suitable water temperature for each type of uses [3].
Application | Temperature (oC)
Sink, Hand washing | 40
Showers | 43
Dish washing and laundry | 48-60
Therapeutic baths | 53
Figure 4: Daily load profile of the domestic hot water system
Table 1: The water temperature for different applications

## Slide 7: Batchwise System Results
Batchwise test at 500 watt with and without PCM:
The PCM started to melt after 250 minutes and it took 360 min to completely melt.
Without PCM, shows a sharp decrease in output water temperature during discharging, unlike with PCM system.
Figure 5: PCM Temperature at 500 watt in Batchwise system
Figure 6: Water Output Temperature at 500 Watt in Batchwise with and without PCM

## Slide 8: Batchwise System Results
Batchwise test at 500 watt with and without PCM:
The results show 33% addition of hot water supply time, system with PCM saved 2855 kJ more than conventional system which supplied an amount of approx. 22 litter of hot water.
Discharging time Without PCM : 150 min.
Discharging time With PCM : 225 min.
Chart: Time [min]
| 0 | 10 | 20 | 30 | 40 | 60 | 70 | 90 | 105 | 120 | 135 | 150 | 165 | 180 | 200 | 225
Output Temp with PCM | 68 | 65.5 | 63.5 | 61.7 | 58.4 | 57 | 56 | 55 | 53.5 | 52.8 | 51.3 | 49 | 46.5 | 44 | 41 | 39
Output Temp Without PCM | 67 | 62 | 57 | 51 | 46 | 40
Figure 7: Water Output Temperature during discharging in Batchwise at 500 watt

## Slide 9: Batchwise System Results
Batchwise test at 700 watt with and without PCM:
The PCM started to melt after 40 minutes and it took 170 min to completely melt.
Without PCM, took 165 min to increase the output water temperature 26 C during charging. Unlike with PCM it took 180 min
Chart: Time [min]
| 0 | 5 | 15 | 30 | 45 | 75 | 105 | 120 | 135 | 150 | 165 | 195 | 225 | 255 | 285 | 315 | 345 | 375
Output Temp without PCM | 47.5 | 52.5 | 54 | 56 | 58 | 59.9 | 67.5 | 67.9 | 69.9 | 72.5 | 74.5 | 70 | 67 | 62 | 57 | 51 | 46 | 40
Output Temp with PCM | 50 | 51 | 52 | 55 | 59 | 63 | 69 | 72 | 72 | 72 | 70 | 68 | 65.5 | 63.5 | 61.7 | 58.4 | 57 | 56 | 55 | 53.5 | 52.8 | 51.3 | 49 | 46.5 | 44 | 41 | 39
Figure 8: PCM Temperature at 700-Watt in Batchwise system.
Figure 9: Water Output Temperature at 700 Watt in Batchwise with and without PCM.

## Slide 10: Batchwise System Results
Batchwise test at 700 watt with and without PCM:
The results show 27% addition of hot water supply time, system with PCM saved 2283 kJ more than conventional system which supplied an amount of approx. 22 litter of hot water.
Discharging time Without PCM : 210 min.
Discharging time With PCM : 290 min.
Figure 10: Water Output Temperature during discharging in Batchwise at 700 watt
Chart: Time [min]
| 0 | 10 | 20 | 40 | 50 | 70 | 85 | 100 | 115 | 130 | 145 | 160 | 180 | 205 | 220 | 240 | 260 | 290
Output Temp with PCM | 72 | 70 | 68 | 65.5 | 63.5 | 61.7 | 58.4 | 57 | 56 | 55 | 53.5 | 52.8 | 51.3 | 49 | 46.5 | 44 | 41 | 39
Output Temp Without PCM | 74 | 70 | 67 | 62 | 57 | 51 | 46 | 40

## Slide 11: Batchwise System Results
Batchwise test at 900 watt with and without PCM:
The PCM started to melt after 120 minutes and it took 240 min to completely melt.
Without PCM, took 180 min to increase the output water temperature 43 C during charging. Unlike with PCM it took 240 min to increase 53 C
Figure 11: PCM Temperature at 900-Watt in Batchwise system.
Figure 12: Water Output Temperature at 900 Watt in Batchwise with and without PCM.
Chart: Time [min]
| 0 | 20 | 30 | 45 | 60 | 75 | 90 | 105 | 120 | 135 | 150 | 165 | 180 | 210 | 240 | 270 | 300 | 330 | 360 | 390
Output Temp without PCM | 30 | 34 | 36.5 | 41 | 44.5 | 49 | 53 | 57 | 60.5 | 64 | 67.5 | 71 | 74 | 70 | 67 | 62 | 57 | 51 | 46 | 40
Output Temp with PCM | 19.6 | 25.5 | 34.4 | 50.3 | 50 | 51.4 | 55.4 | 55 | 56.7 | 56 | 55.6 | 61 | 65.6 | 68 | 71 | 69 | 73.5 | 72 | 70 | 68 | 65.5 | 63.5 | 61.7 | 58.4 | 57 | 56 | 55 | 53.5 | 52.8 | 51.3 | 49 | 46.5 | 44 | 41 | 39

## Slide 12: Batchwise System Results
Batchwise test at 900 watt with and without PCM:
The results show 30% addition of hot water supply time, system with PCM saved 3100 kJ more than conventional system which supplied an amount of approx. 26 litter of hot water.
The results above show 30% addition of hot water supply time. In comparison with Mohammad. F. A[4] configuration, that increased the hot water supply by 25%.
Figure 13: Water Output Temperature during discharging in Batchwise at 900 watt
Chart: Time [min]
| 0 | 30 | 60 | 90 | 120 | 150 | 180 | 210
Output Temp without PCM | 74 | 70 | 67 | 62 | 57 | 51 | 46 | 40
Output Temp with PCM | 73.5 | 72 | 70 | 68 | 65.5 | 63.5 | 61.7 | 58.4 | 57 | 56 | 55 | 53.5 | 52.8 | 51.3 | 49 | 46.5 | 44 | 41 | 39

## Slide 13: Continuous System Results
Continuous test at 700 watt with and without PCM:
The PCM started to melt after 210 minutes and it took 660 min to completely melt.
In comparison with the batchwise system at 700 watts, PCM took 165 minutes to completely melt, unlike continuous system at 700 watt which, took 530 minutes to completely melt.
Figure 14 PCM Temperature at 700-Watt in Continuous system.

## Slide 14: Continuous System Results
Continuous test at 700 watt with and without PCM:
Without PCM, took 410 min to increase the output water temperature 48 C during charging. Unlike with PCM it took 530 min to increase 56 C
Time to reach the charging period with PCM higher than without PCM system at the same power due to, heat loss for the PCM and the stainless steel PCM tank.
Figure 15: Water Output Temperature at 700 Watt in Continuous with and without PCM.
Chart: Time [min]
| 0 | 30 | 45 | 105 | 165 | 210 | 225 | 255 | 285 | 315 | 360 | 410 | 440 | 470 | 500 | 530 | 560 | 590 | 620
Output Temp Without PCM | 26 | 43 | 45 | 55 | 62 | 63 | 64 | 65 | 64 | 67 | 68 | 73 | 70 | 67 | 62 | 57 | 51 | 46 | 40
Output Temp With PCM | 16 | 32 | 39 | 46 | 48 | 50 | 52 | 56 | 58 | 58 | 59 | 60 | 62 | 62 | 64 | 63 | 66 | 69 | 73 | 72 | 72 | 72 | 70 | 68 | 65.5 | 63.5 | 61.7 | 58.4 | 58 | 57 | 55 | 55 | 52.8 | 52 | 50 | 46.5 | 44 | 41 | 39

## Slide 15: Continuous System Results
Continuous test at 900 watt with and without PCM:
The PCM started to melt after 170 minutes and it took 540 min to completely melt.
The period of releasing the latent heat from 540 to 650 min (110 min) which is used in heating water in case of no power supply
In comparison with the batchwise system at 900 watts, PCM took 240 minutes to completely melt, unlike continuous system at 900 watt which, took 420 minutes to completely melt.
Figure 16: PCM Temperature at 900-Watt in Continuous system.

## Slide 16: Continuous System Results
Continuous test at 900 watt with and without PCM:
Without PCM, took 410 min to increase the output water temperature 46 C during charging. Unlike with PCM it took 440 min to increase 56 C
These results show an effective PCM configuration which give a high heat transfer rate and efficient energy storage in compression with Mongibello and M. Atrigna configuration[5]at Literature Review which show that not all of the PCM has undergone melting.
Figure 17: Water Output Temperature at 900 Watt in Continuous with and without PCM.
Chart: Time [min]
| 0 | 25 | 55 | 85 | 115 | 145 | 175 | 190 | 205 | 235 | 265 | 280 | 295 | 325 | 340 | 370 | 395 | 415 | 415 | 425 | 435 | 445 | 455 | 475 | 485 | 505 | 520 | 535 | 550 | 565 | 580 | 595 | 615 | 640 | 655 | 675 | 695 | 715
Output Temp with PCM | 19 | 31 | 41 | 47 | 51 | 53 | 56 | 58 | 61 | 64 | 65 | 66 | 65 | 67 | 68 | 70 | 71.5 | 72 | 72 | 72 | 72 | 70 | 68 | 65.5 | 63.5 | 61.7 | 58.4 | 57 | 56 | 55 | 53.5 | 52.8 | 51.3 | 49 | 46.5 | 44 | 41 | 39
Output Temp without PCM | 26 | 43 | 45 | 55 | 62 | 63 | 64 | 65 | 64 | 67 | 68 | 73 | 70 | 67 | 62 | 57 | 51 | 46 | 40

## Slide 17: PCM and output water temperature behavior after discharging period
After the output water temperature become less than 40 C, water flow rate stopped to study the performance of PCM configuration, which show a high heat transfer rate because no heat remain to increase the output water temperature.
Chart: Time [min]
| 0 | 30 | 60 | 90
PCM Temp | 45 | 43 | 42 | 40
Water Output Temp | 39 | 40 | 41 | 40
Figure 18: PCM and output water temperature behavior after discharging period

## Slide 18: Temperature profiles along the TES tank
Chart: time [min]
| 0 | 10 | 20 | 30 | 40 | 60 | 70 | 90 | 105 | 120 | 135 | 150 | 165 | 180 | 200 | 225 | 240 | 260 | 280 | 300
Ta | 73 | 72 | 72 | 70 | 68 | 65.5 | 63.5 | 61.7 | 58.4 | 57 | 56 | 55 | 53.5 | 52.8 | 51.3 | 49 | 46.5 | 44 | 41 | 39
Tb | 70 | 69.5 | 69 | 67.5 | 66 | 63.5 | 63 | 60 | 57 | 55.5 | 53.5 | 51 | 48.5 | 46.8 | 43 | 39.3 | 36.5 | 33.5 | 31 | 29
Tc | 65 | 64.5 | 64 | 64 | 63 | 60.5 | 57.5 | 48 | 42 | 38 | 36 | 33 | 31.5 | 29.7 | 28.2 | 27 | 25.3 | 24 | 23 | 22
Figure 19: Temperature Distribution along tank at discharging period with PCM
It’s observed from figure 19, that top temperature decreases 5 oC each 60 min until all the PCM solidified, where bottom temperature decreased 5 oC During the first 60 min but after 120 min it decreases around 30 oC
Ta: Water temperature oC, at the surface of the TES tank.
Tb: Water temperature oC, at 28 cm below the surface.
Tc: Water temperature oC, at 55 cm below the surface.

## Slide 19: Effect of nozzle position for hot water withdrawn
Its observed from the figure (20), that T5 is lower than Ta during discharging because of, water from the inserted pipe is passing throw the storage tank.
Water density difference and low water flowrate; cold water will be at the lower half which will cause heat losses and decreasing the temperature of output water.
Chart: time [min]
| 0 | 10 | 20 | 30 | 40 | 60 | 70 | 90 | 105 | 120 | 135 | 150 | 165 | 180 | 200 | 225 | 240 | 260 | 280 | 300
T5 | 65 | 63 | 63 | 61 | 58 | 54 | 52 | 49 | 47 | 45 | 44 | 43 | 42 | 41 | 40 | 39 | 38 | 36 | 35 | 33
Ta | 73 | 72 | 72 | 70 | 68 | 65.5 | 63.5 | 61.7 | 58.4 | 57 | 56 | 55 | 53.5 | 52.8 | 51.3 | 49 | 46.5 | 44 | 41 | 39
Figure 20: Effect of nozzle position for hot water withdrawn.

## Slide 20: Effect of flowrate on output water temperature during discharging
it’s observed from the figure below, that whenever the flowrate increase, the output water temperature will decrease faster due to the large cold water input the system.
Chart: Time [min]
| 0 | 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 75 | 100 | 125 | 135 | 145 | 155
T out 0.45 L/min | 74 | 73.8 | 71.9 | 69.9 | 67.7 | 66 | 64.5 | 63.5 | 62.2 | 60.9 | 59.4 | 58.5 | 56.8 | 56 | 50.1 | 43 | 41.3 | 40.5 | 38.5
T out 0.27 L/min | 73 | 72 | 72 | 70 | 68 | 65.5 | 63.5 | 61.7 | 58.4 | 57 | 56 | 55 | 53.5 | 52.8 | 51.3 | 49 | 46.5 | 44 | 41 | 39
Figure 21: Effect of flowrate on output water temperature during discharging.

## Slide 21: Conclusion and recommendations
PCM increases the time of hot water supply at specified temperature between 27-33%.
PCM supplied between 22-27 litter of hot water more than conventional system.
PCM configuration shows an effective heat transfer rate, in which all the PCM was melt during charging.
Withdrawn the hot water from the top of the tank to reduce heat losses.
The recommendations for any future work:
Study the system with different types of PCM or by using eutectic PCM mixture.
Use a solar simulator instead of the solid state relay .
Study the suggested system by using flat plate collector or evacuated tubes instead of the electric heater.

## Slide 22: Acknowledgment
Our Team Would like to thanks :
Our Supervisor: Dr. Abdelrahim AbuSafa and Chemical engineering department at an najah national university
Our partners
Palestinian Incubator for Energy
Higher council for innovation & Excellence

## Slide 23: References
[1]: Juaidi, A., Montoya, F. G., Ibrik, I. H., & Manzano-Agugliaro, F. (2016). An overview of renewable energy potential in Palestine. Renewable and Sustainable Energy Reviews, 65, 943–960. doi:10.1016/j.rser.2016.07.052.
[2]: SavEnrg, 2019, Phase Change Energy Storage Technology, available at https://rgees.com/technology.php
[3]: Balalta Deema, Habayeb Lama, Assaf Nida, 2017. Thermal Energy Storage Using PCM in Domestic Solar Water Heaters, Nablus: An-Najah National university.
[4]: Mohammad Ali Fazilati and Ali Akbar Alemrajabi, 2013. Phase change material for enhancing solar water heater, an experimental approach. Energy conversion and management. 71(138-145)
[5]: Mongibello, L., 2017. Experimental test of a hot water storage system including a macro-encapsulated phase change material (PCM). Journal of Physics: Conference Series, 796(1).