## Slide 1
SELF-HEALING CONCRETE
2024

## Slide 2
ACKNOWLEDGEMENTS
We express our deepest gratitude to all who contributed to our civil engineering graduation project. Special thanks to our project advisor, Dr. Mohammad Samaaneh, for his invaluable guidance and support, and to Eng. Sameer Halaweh for his assistance in the experimental process. We are also grateful to Dr. Abd al-Fatah Al-Mallah for his constructive feedback. Finally, we thank our families and friends for their unwavering encouragement. Your support has been instrumental in our success. Thank you.
An-Najah National University

## Slide 3
ABSTRACT
  Self-healing concrete aims to reduce cracks, minimize crack width, and maintain structural integrity without compromising strength, thereby extending the lifespan and reducing maintenance costs.
  In this study, we used wastewater containing bacteria from a WWTP in Nablus, Palestine, in various mixing percentages in our concrete samples. We conducted tests on compressive and tensile strength, flexural strength, and abrasion, comparing results with standard specifications.
  Our goal is to induce cracks and observe the self-healing process over time.
An-Najah National University

## Slide 4
INTRODUCTION TO SELF-HEALING CONCRETE
  Concrete is widely used in construction for its strength, durability, and versatility.
  Cracks are a common problem in concrete, potentially leading to larger failures.
  Cracks develop during the hardening phase and over decades, especially in damp environments.
  This project aims to create a self-healing concrete mix.
  We use treated wastewater in the mix to achieve self-healing properties.
An-Najah National University

## Slide 5
MATERILAS
Water
Aggregates
Cement
An-Najah National University

## Slide 6
CEMENT
  The cement used in the experimental work is Composed Portland cement (CEM I 42.5 N).
An-Najah National University

## Slide 7
  Fine and coarse aggregates were used according to the ASTM C136 reference. Crushed limestone aggregates with a maximum 25 mm.
AGGREGATES
An-Najah National University

## Slide 8
  Potable tap water was used for the sample either completely or with different proportions with WW.
WATER
An-Najah National University

## Slide 9
WASTE WATER
  In our project, we develop self-healing concrete using treated water and we will study the effect of wastewater on concrete
  We collected around 60 liters of treated water from the Nablus West treatment plant.
  To study the effect of treated water on this type of concrete we make three concrete mixes (100% of pure water, 100% of treated water, and 50% treated 50% pure)
An-Najah National University

## Slide 10
PROPERITIES OF WATER WE USED
  We take these results from the Nablus West treatment plant
  The pH for water Equals 7.35
  In this project COD/BOD = 16/3.2 = 5
An-Najah National University

## Slide 11
MATERIALS PREPARATION
An-Najah National University

## Slide 12
MATERIALS PREPARATION
An-Najah National University
  Sieve analysis:

## Slide 13
MATERIALS PREPARATION
An-Najah National University
  Sieve analysis:

## Slide 14
MATERIALS PREPARATION
An-Najah National University
  Sieve analysis:

## Slide 15
MATERIALS PREPARATION
An-Najah National University
  Absorption rate:

## Slide 16
MATERIALS PREPARATION
An-Najah National University
  Absorption rate:

## Slide 17
MIX PROPORTIONS OF CONCRETE MIX
An-Najah National University

## Slide 18
TESTING METHODOLOGY
An-Najah National University
  The following table illustrates the details of tests operated on samples :

## Slide 19
TESTING METHODOLOGY
  The slump test.
An-Najah National University

## Slide 20
TESTING METHODOLOGY
  Test of compressive strength following 7 days.
  Test of compressive strength following 28 days.
An-Najah National University

## Slide 21
TESTING METHODOLOGY
  Test for tensile strength.
An-Najah National University

## Slide 22
TESTING METHODOLOGY
  Flexural strength test.
An-Najah National University

## Slide 23
TESTING METHODOLOGY
  Self-healing monitor samples
An-Najah National University

## Slide 24
  Ingredients of B300:
METHODOLGY AND ANALYSIS
An-Najah National University

## Slide 25
  Ingredients of B350 :
METHODOLGY AND ANALYSIS
An-Najah National University

## Slide 26
  Ingredients of B400:
METHODOLGY AND ANALYSIS
An-Najah National University

## Slide 27
RESULTS

## Slide 28
B300 MIX TESTS RESULTS
An-Najah National University
  B300 (0% WW):

## Slide 29
B300 MIX TESTS RESULTS
An-Najah National University
  B300 (50% WW):

## Slide 30
B300 MIX TESTS RESULTS
An-Najah National University
  B300 (100% WW):

## Slide 31
B350 MIX TESTS RESULTS
An-Najah National University
  B350 (0% WW):

## Slide 32
B350 MIX TESTS RESULTS
An-Najah National University
  B350 (50% WW):

## Slide 33
B350 MIX TESTS RESULTS
An-Najah National University
  B350 (100% WW):

## Slide 34
B400 MIX TESTS RESULTS
An-Najah National University
  B400 (0% WW):

## Slide 35
B400 MIX TESTS RESULTS
An-Najah National University
  B400 (50% WW):

## Slide 36
B400 MIX TESTS RESULTS
An-Najah National University
  B400 (100% WW):

## Slide 37
DISCUSSION

## Slide 38
OUTCOMES AND DISCUSSION
  Density: Treated Waste Water (WW) has no impact on the density values of fresh concrete
  Slump Values: WW does not affect slump values differently than ordinary water; the amount of added water is the key factor
An-Najah National University

## Slide 39
OUTCOMES AND DISCUSSION
  Compression Strength (7 Days): WW affects the early reaction of concrete, notably decreasing compressive strength in high-strength designs (B350 and B400 mixes).
  Compression Strength (28 Days): Mixed results; some samples showed increased strength with 50% WW, while others showed decreased strength. The same variability was observed with 100% WW.
An-Najah National University

## Slide 40
OUTCOMES AND DISCUSSION
  Tensile Strength: WW tends to decrease tensile strength, especially at a 50% WW mixing ratio.
  Flexural Strength: No major differences were observed in the flexural strength of concrete due to the addition of WW.
An-Najah National University

## Slide 41
SELF-HEALING PROGRESS OBSERVATION
  Regarding cracks case in concrete, we observed an inverse relationship between the amount of WW added to the mixtures, and the number of cracks occurring in the healed samples, the more WW added to mixtures, the less cracks occur.
An-Najah National University

## Slide 42
SELF-HEALING PROGRESS OBSERVATION
An-Najah National University
100 % WW

## Slide 43
SELF-HEALING PROGRESS OBSERVATION
An-Najah National University
50 % WW

## Slide 44
SELF-HEALING PROGRESS OBSERVATION
An-Najah National University
0 % WW

## Slide 45
  Based on the results of previous experiments, we found that replacing pure water with wastewater is feasible, especially from an economic standpoint. The price of a cubic meter of pure water is about 11-12 shekels, while wastewater is 2-3 shekels. Also from a political standpoint, due to the presence of the occupation and the difficulty of extracting groundwater, it can be used. As an alternative in other construction matters
  As for self-healing, we did not notice any change in the samples due to the short time for the project
CONCLUSION
An-Najah National University

## Slide 46
RECOMMENDATIONS
  Conduct more experiments with different percentages, such as 25% and 75%, to obtain more accurate results.
  Monitoring self-healing samples over a period ranging from one to six months.
  Treated water can be used in mortar.
  Study of the environmental impact of concrete after using treated water.
An-Najah National University

## Slide 47
THANK YOU
“Brick by brick, stone by stone, every great thing was built by those who believed they could.”
Tom “The Mason” Mitchell
An-Najah National University