## Slide 1: Production and Characterization of Nanocomposites composed of Polyvinyl alcohol and synthesized silver nanoparticles
Prepared by:
Abeer Bsharat Shahed Salameh Sondos Soboh
Supervisor :
Dr.Shadi Sawalha
Graduation project 2

## Slide 2: Introduction 01 Opjectiv 03 Methodology 04 Charactaresation 05 Results 06 Conclusions 07 Table of contents
02
Problem statement

## Slide 3: Introduction 01

## Slide 4: Nanotechnology
Nanotechnology explores unique material interactions on a nanoscale (1-100 nanometers),offering diverse possibilities. Nanocomposites, integrating particles of varying scales into matrices, excel in mechanical and electrical enhancements, contributing to modern technological advancements.

## Slide 5: Problem statement 02

## Slide 6
Synthesizing silver nanoparticles faces challenges in achieving precise control over size and shape, and most manufacturing methods require a long time. They also face challenges related to toxicity, stability, and chemical reactivity. In addition to several problems with its properties .
PVA properties like thermal ,electrical, and other properties are not sufficient to use them for applications.
Some food packages are not resistant to bacteria. It causes contamination of food with bacteria.

## Slide 7: Opjective 03

## Slide 8
Synthesis of Ag-NPs using rapid method (microwave assisted method).
Studying the effect of the power on Ag-NPs properties like optical, electrical properties.
Enhance a properties of PVA films properties such as electrical, thermal and anti-microbial.

## Slide 9: Methodology 04

## Slide 10: Material
Silver Nitrate (AgNO3)
Ethylene glycol
Polyvinylpyrrolidone (PVP)
Polyvinyl alcohol (PVA)
distilled water

## Slide 11: Synthesis of Ag-NPs
Weight of
0.17g of AgNO3 and
0.34g of PVP
Add 40ml of
Ethylene glycol
While stirring, we add
0.34g of PVP Gradually, after
completely dissolved
We add 0.17g
of AgNO3
different
powers
90s
microwave
Ag-NPs
solution
The product yield for Ag-NPs was 22.11%

## Slide 12: Synthesis of PVA/Ag nanocomposites
Weight
1.0g of PVA
Add 50ml of
distilled water
While stirring, we add
1.0g of PVP Gradually, after
dissolved completely, we add different
amount of Ag-NPs
90C°
20 min
poured onto a
dry, leveled surface
Dry
PVA/Ag nanocomposite film

## Slide 13: Characterization 05

## Slide 14
UV-vis spectra
AFM Microscopy
Vector network analyzer
Differential ScanninCalorimetry (DSC)

## Slide 15: Results 06
Synthesis
Characterization Results

## Slide 16: UV-VIS SPECTROSCOPY
(a) UV-vis absorption spectra of synthesized Ag-NPs at different power (b) Tauc plot of Ag-NPs at different power.

## Slide 17: UV-VIS SPECTROSCOPY
(a) UV-vis absorption spectra of synthesized PVA / Ag nano composite (b) Tauc plot of PVA / Ag nano composite at medium high power.

## Slide 18: Vector network analyzer
(a) the conductivity of synthesized Ag-NPs (b) the conductivity of synthesized PVA / Ag nano composite with different volume Ag-NPs.

## Slide 19: AFM Microscopy
(a) The morphology and size for Ag-NPs at medium power (b) The morphology and size for Ag-NPs at medium high power.

## Slide 20: Differential Scanning Calorimetry (DSC)
DSC results for Ag/PVA nanocomposites film containing different wt% of Ag-NPs .
Wt% Ag | Xc %
0.0Pure PVA | 14.047
0.11 Ag-NPs | 14.204
0.22Ag-NPs | 18.331

## Slide 21: Antibacterial Activity.
ATCC Number | microbe Strain | Gram type | L | M-L | Power M | M-H | H
DPC 5645 | MRSA | + ve | 20 | 17 | 18 | 183 | 330
ATCC 25923 | S. aureus | + ve | 20 | 17 | 18 | 183 | 330
ATCC 25922 | E. coli | - ve | 10 | 8.6 | 18 | 91 | 330
ATCC 13883 | Klebsiella pneumoniae | - ve | 5 | 4.3 | 4.6 | 45 | 330
ATCC 8427 | Proteus vulgaris | - ve | 20 | 8.6 | 18 | 45 | 160
ATCC 9027 | Pseudomonas aeruginosa | - ve | 5 | 4.3 | 4.6 | 45 | 330
Microbial and Fungal Growth Inhibition MIC values (μg/mL) of different powers.
Number of colony | from36to6
Kills | 84%
Bacteria | E.Coli

## Slide 22: Conclusions 08

## Slide 23
Microwave-assisted method.
Effect of Power Levels on Ag-NPs.
Ag/PVA Nanocomposite Film Formation.
Properties of Ag/PVA Nanocomposite.
The Ag/PVA nanocomposite film significantly reduced colony-forming units of E. coli bacteria.
Ag-NPs, enhancing antibacterial activity.

## Slide 24: Thanks
Do you have any questions?