## Slide 1: Synthesis of Carbon Nanodots from Smoked Tobacco Molasses via Chemical Oxidation and Extraction
Presented by
Amal Yaseen
Aya Ataya
Leena Rifai
Prepared to
Dr. Shadi Sawalha

## Slide 2
Introduction
Sensing Application
Project Objectives
Synthesis of CNDs
Results and Discussion
Summary Of The Project
Content

## Slide 3
Resources of CNDs
Natural
Man made
Waste
CNDs have many important properties such as optical quanta small size uniform shape and composition fluorescence emission, low toxicity and biocompatibility and low cost in preparation.
Over the past decade, carbon dots have received a great deal of attention and extensive research.
Carbon NanoDots(CNDs)

## Slide 4
Top-Down
Chemical Oxidation
Laser ablation
Electrochemical oxidation
Sonication
Bottom-Up
Thermal Carbonization
Plasma Treatment
Hydrothermal Treatment
Microwave
Synthesis Methods to Prepare CNDs

## Slide 5
Using CNDs In Sensing
CNDs are suitable for use in Nano sensors due to a variety of their characteristics .
Adjustable Fluorescence
Superior Stability
Strong Water Solubility

## Slide 6
Project Objectives
.
.
Synthesis of carbon nanodots from tobacco molasses waste by two methods extraction and chemical oxidation, to use them in sensing based on fluorescence metals mainly iron ions in the water will be an optimal solution for the problem of water pollutants, especially that CNDs are synthesized from tobacco molasses waste, which is available and recycle for the waste.

## Slide 7
Smoked Tobacco Molasses (STM)
Residual of STM Water
Residual of STM 𝐇_𝟐 𝐎_𝟐+Water
5g STM soaked in 120 ml water
D-CNDs
Florescence D-CNDs
O-CNDs
Oxidation
90 min
Florescence O-CNDs
Smoked Tobacco Molasses (STM)
5g STM soaked in 120 ml water
D-CNDs
Florescence D-CNDs
O-CNDs
Oxidation
90 min
Florescence O-CNDs
Synthesis of CNDs

## Slide 8
Morphology and Chemical Composition
AFM Image
Height Profile
Distribution Histogram
D-CNDs show a wide range of particle size from 2.9 to 33 nm with an average of 10.7 nm
Characterizations of CNDs

## Slide 9
AFM Image
Height Profile
Distribution Histogram
O-CNDs show narrow range of particle size from 0.93 to 5.9 with an average of 2.7 nm
Morphology and Chemical Composition

## Slide 10
FTIR Spectra of Synthesized CNDs
The existence of oxygen group in both CNDs (O-CNDs and D-CNDs) was confirmed by PAIS 𝜀-Potential measurement illustrating higher negative value for O-CNDs (-15.2) than D-CNDs (-10.24).

## Slide 11
The absorption spectra of prepared D-CNDs
Tauc plot of D-CNDs
Optical properties
Band gap of D-CNDs has been calculated and giving a value of (2.25 eV)

## Slide 12
Optical properties
Tauc plot of O-CNDs
The absorption spectra of prepared O-CNDs
Band gap of O-CNDs has been calculated and giving a value of (3 eV)

## Slide 13
Photoluminescence (PL) Intensity
D-CNDs
O-CNDs
O-CNDs exhibit a higher Q.Y which was 3.1% while D-CNDs have a quantum yield of 1.55%

## Slide 14
Metal Ions Solution
Sample
CNDs
Deionized Water
Selectivity Test

## Slide 15
Metal Salts
〖𝐹𝑒𝐶𝑙〗_3
〖𝑀𝑛𝐶𝑙〗_2
〖𝐻𝑔𝐶𝑙〗_2
〖𝑁𝑖(𝑃𝑂_3)〗_2
〖𝐹𝑒𝐶𝑙〗_2
𝑃𝑏(𝑁𝑂3)2
𝐶𝑢𝐶𝑙2.2𝐻2𝑂
Metal Salts

## Slide 16
Results of Selectivity Test for D-CNDs
D-CNDs Fluorescence Quenching Upon Cation Ions Spiking
D-CNDs Selectivity of Different Cations

## Slide 17
Results of Selectivity Test for O-CNDs
O-CNDs Fluorescence Quenching Upon Cation Ions Spiking
O-CNDs Selectivity of Different Cations

## Slide 18
PL Intensity at Different Excitation Wavelengths
D-CNDs
O-CNDs

## Slide 19
CNDs | Linear Range (μM) | Sensitivity (μM-1) | LOD (μM) | LOQ (μM) | Efficiency @ 400 μM
D-CNDs | 0 - 50 | 0.0029 | 7.2 | 24 | 65%
O-CNDs | 0 - 50 | 0.0045 | 3.9 | 13 | 76.6%
Comparing The Sensing Parameter For Both CNDs

## Slide 20
Quenching Efficiency Curves for D-CNDs and O-CNDs
Fitted Calibration Curves

## Slide 21
Sample | CNDs Type | Spiked (µM) | Measured (µM) (n=3) | %RSD | Recovery %
Tap water | D-CNDs | 50 | 49.42 | 0.615 | 98.84
 |  | 20 | 18.53 | 2.73 | 92.66
 | O-CNDs | 50 | 49.51 | 3.34 | 99.03
 |  | 20 | 20.89 | 1.93 | 104.48
Rain Water | D-CNDs | 50 | 51.84 | 1.060 | 103.68
 |  | 20 | 20.48 | 2.58 | 102.43
 | O-CNDs | 50 | 51.05 | 2.48 | 102.10
 |  | 20 | 20.50 | 0.418 | 102.50
Drink Water | D-CNDs | 50 | 47.85 | 0.232 | 95.70
 |  | 20 | 18.88 | 0.264 | 94.41
 | O-CNDs | 50 | 52.42 | 6.819 | 104.8
 |  | 20 | 19.56 | 2.075 | 97.80
Fe+3 Sensing With CNDs In Real Water Samples

## Slide 22
Static
Dynamic
Combined
Stern Volmer Plot
Fluorescence Quenching Mechanism

## Slide 23
O- CNDs
D-CNDs
Quenching Mechanism of CNDs with Fe+3 (Stern Volmer Plot)

## Slide 24
Summary
Of The
Project
Pollutants Found In Water Cause Different Types of Diseases
Water Sensors are Expansive & Needs Complicated Instrumental Techniques
Sensing Application Using O-CNDs and D-CNDS
Synthesis of Carbon Nanodots From Tobacco Molasses Waste
Based on Fluorescence Metals Iron Ions
Based on Fluorescence Metals Iron Ions 〖𝐹𝑒〗^(3+)
An Available Feasible Solution!
Pollutants Found In Water Cause Different Types of Diseases
Water Sensors are Expansive & Needs Complicated Instrumental Techniques
Sensing Application Using O-CNDs and D-CNDS
Synthesis of Carbon Nanodots From Tobacco Molasses Waste
An Available Feasible Solution!

## Slide 25
Thank You For Your Attention!