## Slide 1
Conservation of the Material Cultural Heritage in Al-Aqsa Mosque
Prepared by:
Isra’a Maraabeh – Chemical Engineering
Hadeel Qawariq – Materials Engineering
Omaila Taweel – Materials Engineering
Supervisor:
Dr. Hamdallah Bearat

## Slide 2
Content:
Introduction
Objective
Methodology and Results for:
- Kashani
- Wood
- Marble
- Lead
Conclusion and Recommendation
Constrains

## Slide 3
Introduction
- Conservation-Restoration of cultural heritage.
- Historic and Islamic sites in Palestine.
- Al-Aqsa Mosque is one of the most important landmarks.

## Slide 4
Objective:
Continuing efforts in restoration and preservation of the material Islamic heritage in Al-Aqsa mosque through the scientific study of materials and their degradation processes

## Slide 5
Methodology and Results:
Kashani
Description of the sample:

## Slide 6
Sample preparation:

## Slide 7
Experimental part (with result):
Optical microscope:

## Slide 8
- SEM/EDX:

## Slide 9
- SEM/EDX results:
Three layers in kashani sample was clearly visible (A, B and C)
A- Kashani paste (ceramic substrate): The EDX analyses shows that the layer contains those elements; Si > Al >> Na > Mg > Cl > K .
B- Kashani intermediate zone (next to glaze): The EDX analyses shows that the layer contains those elements; Si >> Al >> Mg > Na > Cl > Ca > K .
C-Kashani-glaze: The EDX analyses shows that the layer contains those elements; Si > Pb > Zn > Al > Cl > Ca

## Slide 10
- XRD:

## Slide 11
XRD (results):
XRD results for Kashani was plotted, But there is No database to compare with.
Chart: Faience

## Slide 12
Lead
Description of the sample

## Slide 13
Sample preparation:

## Slide 14
Experimental part (with results)
Optical microscope

## Slide 15
SEM/EDX

## Slide 16
XRD:

## Slide 17
IR:

## Slide 18
Marble
Description of the sample:

## Slide 19
Sample preparation:

## Slide 20
Experimental part:
Optical microscope

## Slide 21
SEM/EDX
The EDX shows that the marble is almost pure calcium carbonate (CaCO3)

## Slide 22
IR:

## Slide 23
Chemical treatment:
H2O2
Aceton

## Slide 24
Thermal treatment:
The sample was put at oven at 412֯֯C
Before
After

## Slide 25
Wood
Description of the sample

## Slide 26
Sample preparation:

## Slide 27
Experimental part (with result):
Optical microscope

## Slide 28
SEM/EDX
SEM picture shows that there is black hole in the sample, we believe that microorganisms are the cause. These tunnels may be made while passing through the sample or because of their waste.

## Slide 29
Conclusion and Recommendation:
Our focus in this preliminary work is on the Al-Aqsa Mosque, which is an important religious and historical landmark. Samples were taken from three different locations in the Al-Aqsa Mosque (the Dome of the Rock and Al-Qibili mosques) , These samples suffered deterioration of different and nature levels. The anticipated objectives of this project have been to identify the causes and mechanism of degradation in each type of these archeomaterial and to propose some remedies for each problem.

## Slide 30
Constrains
Delay in obtaining the samples.
Difficulty to visit and observe the location of samples, since the Israel occupation put obstacles to visit of Jerusalem city.
Difficulty to know the exact age of the samples.
Limited information available on sample manufacturing.
Our laboratories lack the necessary equipment for sample preparation, characterization, and testing.
The high price of epoxy and the lack of it in the market and the inability of laboratories to provide it on time.
Lack of specialized programs (software) to analyze the results of microscopic and XRD examinations.
Short time available to interpret analytical results, since most of tests were done in the last month at the Arab-American University in Jenin.

## Slide 31
Thanks For Listening
Any Question?