## Slide 1: Chemical Engineering Program 2024-2023
Preparation, Characterization and Applications of Zinc Oxide/Carbon Nanodots Hybrid

## Slide 2: Contents
Overview
Objectives
Materials and methodology
Result
Application
Conclusion

## Slide 3: Overview
Nano Particles
Carbon Nanodots
The hybrid
Photodegradation

## Slide 4: Objectives
MICROWAVE SYNTHESIS METHOD:
Develop a rapid microwave-based synthesis for high-yield ZnO NPs and CNDs.
Investigate a one-pot approach for simultaneous ZnO-CNDs hybrid synthesis.
PHOTODEGRADATION APPLICATION:
Explore ZnO and ZnO-CNDs hybrid electrodes for methylene blue photodegradation.
Emphasize effectiveness, degradation efficiency, and stability through multiple cycles.

## Slide 5: Objectives
WATER PURIFICATION APPLICATIONS:
Assess ZnO/CND hybrids as electrodes for practical water purification.
Focus on diverse pollutant removal, particularly dyes, via a photocatalytic process
MATERIAL CHARACTERIZATION:
Utilize UV–vis spectrophotometry to analyze optical properties.
Identify chemical functional groups through FT-IR spectroscopy.
Examine surface topography with SEM and AFM.

## Slide 6: MATERIALS AND METHODOLOGY
MATERIALS USED
SYNTHESIS PROCEDURES
CHARACTERIZATION TECHNIQUES

## Slide 7: Materials Used
Distilled Water
Isopropanol
Sodium Hydroxide
Ammonia Hydroxide
Zinc Salt
D-Glucose

## Slide 8: THE PROCESS OF MANUFACTURING

## Slide 9: CHARACTERIZATION TECHNIQUES
UV-vis Absorption spectra
Fourier Transform Infrared (FT-IR)
Photolinmineneacence
Scanning electron Microscopy (SEM)
Atomic Force Microscopy (AFM)

## Slide 10: RESULTS
Synthesis
Characterization Results

## Slide 11: Synthesis Results
 | Without NH4OH | With NH4OH
Zinc Oxide (ZnO Nps) | 17.3% | 27.7%
Carbon Nanodots (CNDs) | 9.5% | 17.5%
ZnO-CNDs Hybrid | 13.5% | 24.4%

## Slide 12: FLUORESCENCE MEASUREMENTS

## Slide 13: UV-VIS SPECTROSCOPY

## Slide 14: UV-VIS SPECTROSCOPY

## Slide 15: FT-IR SPECTRA

## Slide 16: SEM MICROSCOPY

## Slide 17: AFM MICROSCOPY

## Slide 18: APPLICATION
PHOTODEGRADATION
Photocatalyst

## Slide 19: ELECTRODE MANUFACTURING METHOD

## Slide 20: PHOTODEGRADATION OF DYE USING ELECTRODE

## Slide 21: ANALYSES OF THE METHYLENE BLUE DEGRADATION

## Slide 22: ELECTRODE STABILITIES

## Slide 23: AFM MICROSCOPY

## Slide 24: Conclusions
Microwave Method
Potential of Ammonia as Reducing Agent
Thin Film Stability
Characterization Analysis
Application in Photodegradation
Successful Hybridization

## Slide 25
Thank You
Do You Have Any Questions ?