## Slide 1: Pavement condition index calculation

## Slide 2: Data Collection
Data for the project has been collected through conducting accurate condition assessment process of the existing pavement surface distresses

## Slide 3: Purposes of Using Pavement Condition Data
Establishing Project Priorities
Establishing Options
Forecasting Performance
This information is useful for preparing long-range budget estimates of the cost to maintain the highway system at a minimum standard of performance.

## Slide 4: Pavement defects types
Cracking
Patching and Potholes
deformations
Disintegration and wear

## Slide 5: Some types of distresses on Ring Road Alligator Cracks

## Slide 6: Transverse Crack

## Slide 7: Raveling & Polished aggregate

## Slide 8: Example on calculation of (PCI)

## Slide 9: Deduct Value curve of Alligator Crack

## Slide 10: Correct Deduct Value curve (CDV)

## Slide 11: Paser Rating System

## Slide 12: Treatment and Cost
When defects occur in surface of pavement, it is preferred to make the proper maintenance to extend the life of the road
Some Types of treatments:
1- crack sealing:
Crack sealing is the process of cleaning and sealing or resealing of cracks in AC pavement to prevent the intrusion of water into cracks.

## Slide 14
2- Full-Depth Patching :
This technique involves replacing the full depth of the AC layer and may include replacement of the base and subbase layers.
3- AC Overlay :
This technique involves adding one or more AC layers to an existing

## Slide 15
4- Reconstruction :
Is the removal and replacement of existing pavement structure.
5- Cold Milling:
Cold milling is the removal of a given thickness of the surface layer using a machine containing a rotary drum with teeth.

## Slide 16: Unit price / maintenance efficiency
The unit price is an important element
in the priority of
determining maintenance.
Unit Price US($) | Unit | Description of treatment
0 | - | Do nothing
3 | m2 | routine crack filling
5 | m2 | sealcoat
110 | ton | surface batching/deep
12 | m2 | structural overlay
14 | m2 | Structural asphalt layer without milling
16 | m2 | major overlay, Milling and removal of deterioration
16 | m2 | reconstruction with extensive base repair
30 | m2 | Total Reconstruction

## Slide 17: PCI, Rating ,Treatments and Price
Total Price($) | Unit price($) | Area(m2) | General condition/ treatment measures | Surface Rating | PCI | Section
3250 | 5 | 650 | Shows signs of aging. Sound structural condition. Needs sealcoat to extend the life of overlay | Good | 64 | 0+000 - 0+100
2050 | 5 | 410 | Shows signs of aging. Sound structural condition. Needs sealcoat to extend the life of overlay | Good | 60 | 0+100 - 0+200
5160 | 12 | 430 | Significant aging and first signs of need for strengthening. Would benefit from a structural overlay (2” or more). | Fair | 44 | 0+200 - 0+300
1260 | 3 | 420 | First signs of aging. Needs to maintain with routine crack filling | Good | 75 | 0+300 - 0+400
1110 | 3 | 370 | First signs of aging. Needs to maintain with routine crack filling | Good | 74 | 0+400 - 0+500
1850 | 5 | 370 | Shows signs of aging. Sound structural condition. Needs sealcoat to extend the life of overlay | Fair | 54 | 0+500 - 0+600
2200 | 5 | 440 | Shows signs of aging. Sound structural condition. Needs sealcoat to extend the life of overlay | Fair | 54 | 0+600 - 0+700
0 | 0 | 410 | Sealcoat or new cold mix. little or no maintenance required | Very good | 88 | 0+700 - 0+800
0 | 0 | 380 | New construction, No need to treatment | Excellent | 92 | 0+800 - 0+900

## Slide 18
0 | 0 | 330 | New construction, No need to treatment | Excellent | 90 | 0+900 - 1+000
0 | 0 | 340 | New construction, No need to treatment | Excellent | 96 | 1+000 - 1+100
1800 | 5 | 360 | Needs sealcoat to extend the life of overlay. | Fair | 51 | 1+100 - 1+200
1200 | 3 | 400 | First signs of aging. Needs to maintain with routine crack filling | Good | 71 | 1+200 - 1+300
1900 | 5 | 380 | Shows signs of aging. Sound structural condition. Needs sealcoat to extend the life of overlay | Fair | 57 | 1+300 - 1+400
1080 | 3 | 360 | First signs of aging. Needs to maintain with routine crack filling | Good | 70 | 1+400 - 1+500
5440 | 16 | 340 | Severe deterioration. Needs reconstruction with extensive base repair | Very Poor | 22 | 1+500 - 1+600
1750 | 5 | 350 | Shows signs of aging. Sound structural condition. Needs sealcoat to extend the life of overlay | Fair | 56 | 1+600 - 1+700
6400 | 16 | 400 | Needs Patching and repair prior to major overlay, Milling and removal of deterioration extend the life of overlay | Poor | 33 | 1+700 - 1+800
6080 | 16 | 380 | Needs Patching and repair prior to major overlay | Poor | 36 | 1+800 - 1+900
9900 | 30 | 330 | Total Reconstruction | Failed | 18 | 1+900 - 2+000
1650 | 5 | 330 | Shows signs of aging. Sound structural condition. Needs sealcoat to extend the life of overlay | Good | 62 | 2+000 - 2+100
5440 | 16 | 340 | Needs Patching and repair prior to major overlay, Milling and removal of deterioration extend the life of overlay | Poor | 38 | 2+100 - 2+200

## Slide 19
4200 | 12 | 350 | Significant aging and first signs of need for strengthening. Would benefit from a structural overlay (2” or more). | Fair | 40 | 2+200 - 2+300
9900 | 30 | 330 | Total Reconstruction | Failed | 0 | 2+300 - 2+400
9900 | 30 | 330 | Total Reconstruction | Failed | 18 | 2+400 - 2+500

## Slide 20
Station | PCI | Surface Rating | General condition/ treatment measures | Area(m2) | Unit Price($) | Total Price
2+500 – 2+600 | 34 | Poor | Needs Patching and repair prior to major overlay, Milling and removal of deterioration extend the life of overlay | 650 | 16 | 10400
2+600 – 2+700 | 20 | Very Poor | Severe deterioration. Needs reconstruction with extensive base repair | 470 | 16 | 7520
2+700 – 2+800 | 58 | Fair | Surface aging. Sound structural condition. Needs sealcoat or thin non-structural overlay (less than 2”) | 340 | 5 | 17000
2+800 – 2+900 | 85 | Very Good | Sealcoat or new cold mix. little or no maintenance required | 400 | 0 | 0
2+900 – 3+000 | 59 | Fair | Shows signs of aging. Sound structural condition. Needs sealcoat to extend the life of overlay. | 370 | 5 | 1850
3+000 – 3+100 | 69 | Good | Shows signs of aging. Sound structural condition. Needs sealcoat to extend the life of overlay | 430 | 5 | 2150
3+100 – 3+200 | 50 | Fair | Surface aging. Sound structural condition. Needs sealcoat or thin non-structural overlay (less than 2”) | 360 | 5 | 1800

## Slide 21
3+200 – 3+300 | 72 | Good | First signs of aging. Needs to maintain with routine crack filling | 410 | 3 | 1230
3+300 – 3+400 | 83 | Very Good | Sealcoat or new cold mix. little or no maintenance required | 380 | 0 | 0
3+400 – 3+500 | 84 | Very Good | Sealcoat or new cold mix. little or no maintenance required | 400 | 0 | 0
3+500 – 3+600 | 98 | Excellent | New construction, no need for treatment | 360 | 0 | 0
3+600 – 3+700 | 77 | Good | First signs of aging. Needs to maintain with routine crack filling | 390 | 3 | 1170
3+700 – 3+800 | 56 | Fair | Shows signs of aging. Sound structural condition. Needs sealcoat to extend the life of overlay. | 350 | 5 | 1750
3+800 – 3+900 | 91 | Excellent | New construction , no need to treatment | 400 | 0 | 0
3+900 – 4+000 | `94 | Excellent | New construction , no need to treatment | 400 | 0 | 0
4+000 – 4+100 | 29 | Very Poor | Severe deterioration. Needs reconstruction with extensive base repair. | 380 | 16 | 6080
4+100 – 4+200 | 82 | Very Good | Sealcoat or new cold mix. little or no maintenance required | 360 | 0 | 0
4+200 – 4+300 | 48 | Fair | Significant aging and first signs of need for strengthening. Would benefit from a structural overlay (2” or more). | 380 | 12 | 4560

## Slide 22
4+300 – 4+400 | 62 | Good | Sound structural condition. Needs sealcoat to extend the life of overlay | 400 | 5 | 2000
4+400 – 4+500 | 49 | Fair | Significant aging and first signs of need for strengthening. Would benefit from a structural overlay (2” or more). | 350 | 12 | 4200
4+500 – 4+600 | 62 | Good | Shows signs of aging. Sound structural condition. Needs sealcoat to extend the life of overlay | 350 | 5 | 1750
4+600 – 4+700 | 42 | Fair | Significant aging and first signs of need for strengthening. Would benefit from a structural overlay (2” or more). | 360 | 12 | 4320
4+700 – 4+800 | 54 | Fair | Shows signs of aging. Sound structural condition. Needs sealcoat to extend the life of overlay | 350 | 5 | 1750
4+800 – 4+900 | 72 | Good | First signs of aging. Needs to maintain with routine crack filling | 370 | 3 | 1110
4+900 – 5+000 | 37 | Poor | Needs Patching and repair prior to major overlay, Milling and removal of deterioration extend the life of overlay | 330 | 16 | 5280

## Slide 23
Total cost for all treatments and sections= 159,440$
Based on PCI values in this project, most of sections range from (40-65) which is corresponding to Preventive maintenance actions and Corrective action location

## Slide 24: Pavement Deterioration Chart