## Slide 1: Deep drawing and Rolling Process using Finite Element Analysis
Prepared by:
Mohammad Alawni
Bilal Abdelrazeq
Supervisor:
Dr. Iyad Assaf

## Slide 2: Rolling and Deep drawing process
Rolling process:

## Slide 3: The Rolling process:
The force calculated:
F= LWYavg
The type of rolling process :

## Slide 4: Some types of rolling process

## Slide 5: Hot and cold work the rolling process

## Slide 6: Deep drawing process
The forces calculated:
Fmax= πDp t (UTS)[(Db/Dp)-0.7]

## Slide 7: Finite Element Analysis the flat rolling process
:

## Slide 8: Create parts
3D→Deformable→solid→extrusion 3D →discreate shell→solid→extrusion

## Slide 9: Define material

## Slide 10: Assign the define material to the deformable part

## Slide 11: Create Assembly

## Slide 12: Define step
Explicit .dynamic
Time period =0.089 sec

## Slide 13: Interaction Model

## Slide 14: Mesh
the Element Library was Explicit

## Slide 15: Load and Boundary condition
workpieces (ENCASTRE →U2=0)., U3=UR1=UR2=0
ROLLER → U1=U2=U3=UR1=UR2=0,UR3)

## Slide 16: Define job
Job-1 was created and submitted.
.

## Slide 17: The Visualization

## Slide 19: Force-time

## Slide 20: Deep drawing process using finite element analysis
Create parts

## Slide 21: Define material and assign Aluminum-killed steel properties
 | Young’s Modulus (GPa) | Poisson’s ratio
Elastic | 210 | 0.3
 | Yield stress (MPa) | Plastic strain
Plastic | 91 | 0
 | 181 | 0.0085618
 | 281 | 0.066236
 | 381 | 0.26252
 | 481 | 0.7489
 | 521 | 1.0721

## Slide 22: Create Assembly

## Slide 23: Define Step and BC
Static  standard, General.

## Slide 24: Define step

## Slide 25: Define step

## Slide 26: Define interactions

## Slide 27: Mesh

## Slide 28: Define jops and results

## Slide 30: Force_time and Displacement_time curves

## Slide 31: Force_displacement curves

## Slide 32: Flat rolling limitation:
Maximum draft possible: ho – hf = µ 2R= dmax
final width:
The strip thickness is reduced at each rolling pass and the strip width increases slightly (around 2%)  h0V0W0 = hfVfWf .
wf = 1.02 w0.
3) Contact length:
L=√(R(h0-hf)) .

## Slide 33: Calculate the force
4) Final thickness:
Vo/Vf =hf/ho
5)Slip of strip:
s=(Vf-Vr)/Vr
R2 = L2 +(R-((ho-hf)/2)2
1702 = L2+(170-((40-30)/2)2
L = 40.9 mm
yavg== 308.585MPa
F = 305.58 (40)(40.9) = 504k N
for the force in ABAQUS equal = 275 KN

## Slide 34: Deep drawing limitation
Where:
Db = 0.2 m.
Dp = 0.1 m.
t = 0.0082m.
Then:
1) r = = 0.5
2) DR =
3) c= 1.1×t = 0.009

## Slide 35: Force calculation
Where:
UTS=521 Mpa
Fmax= πDp t (UTS)[()-0.7] = 174.3KN

## Slide 36
Thank you