## Slide 1: Thermal Efficiency of Buildings
Motaz H. Othman
Mohammad S. Humaidi
Supervised by: Dr. Salameh Abdul Fattah

## Slide 2: Outline
Introduction.
Thermal insulation.
Heat losses.
Environmental effects.
New thermal insulation
procedure
Experimental results
Conclusion
Recommendation

## Slide 3
Reinforced concrete is widely used in construction sector due to its several features, such as:
  workability
  better appearance
  fire resistance
  economical issues
  high durability and ability to be molded to any complex shape using suitable form work.
Introduction

## Slide 4
Deficiencies can be found with reinforced concrete usage, such as:
  high thermal conductivity
  high heat losses
  problems with humidity.
Introduction

## Slide 5: Considerations for Increasing Thermal Efficiency
Thermal insulation.
Vapor barriers.
Heat Losses.
Environmental Effects.
Solar Solutions.

## Slide 6: Thermal insulation
What is Thermal Insulation?
Insulation is defined as a material or combination of materials, which retard the flow of heat.

## Slide 7
Characteristics of Thermal Insulation:
  Thermal Resistance (R)
  Water Vapor Permeability
  Weather Resistance
  Corrosion Resistance
  Fire Resistance Density (lb/ft3) (kg/m3)
Thermal insulation

## Slide 8
Temperature range | Applications | Properties | R value
Polystyrene |  |  | 
low temperatures (-167 C to 82 C) | cool rooms, refrigeration piping | Rigid, lightweight | R-5.00
Polyurethane |  |  | 
low temperatures (-178C to 4oC) | cool rooms, refrigeration piping and floor and foundation insulation | low density, high mechanical strength | R-7–R-8
Insulation Types:
Thermal insulation

## Slide 9
Temperature range | Applications | Properties | R value
Rockwool |  |  | 
temperatures up to 820 C | insulate industrial, heat exchangers, boilers | maintains mechanical strength during handling | R-2.5–R-3.7
Fiber glass |  |  | 
temperatures up to 540oC | heat exchangers , boilers | It should not promote or accelerate the corrosion of steel, provide it is protected from external contamination | R-3.1–R-4.3
Insulation Types:
Thermal insulation

## Slide 10
Forms of Insulation Board
  Block
  Sheet
  Foam
  Spray
  Cements
Thermal insulation

## Slide 11
What is Vapor barriers?
It is defined as the ability of a material to retard the diffusion of water vapor and measured in units known as "perms" or permeability.
Vapor barriers

## Slide 12
Temperature range | Thermal conductivity | (permeability) | Applications
CELLULAR GLASS |  |  | 
-260 to 430°C | 0.040 | zero | Industrial: tank bases, vessels, piping and equipment . Buildings: roofs, floors, walls
GLASS MINERAL WOOL |  |  | 
-200 to 450°C | 0.040 | zero | in the HAC V sector and insulation in transport, shipping, building and industrial applications.
Vapor barriers Types:
Vapor barriers

## Slide 13
Temperature range | Thermal conductivity | (permeability) | Applications
NITRILE RUBBER EXPANDED |  |  | 
-40 to 116°C | 0.037 | 0.25 μgm/Nh | used for and energy conservation on domestic heating, and hot and cold-water pipe work.
PHENOLIC FOAM |  |  | 
-180 to 120°C | 0.018-0.022 | 10 μgm/Nh | Construction – floor, wall, roof insulation in domestic, commercial and industrial buildings.
Vapor barriers Types:
1 kg/(m×s×Pa) = µgm/(Nh) × 2.778 × 10
13
Vapor barriers

## Slide 14: Heat Losses
What is heat loss?
It is defined as the heat that flows from the building interior, through the building envelope to the outside environment .

## Slide 15
The heat loss can be calculated as :
Ht = A U (ti - to)
Ht = transmission heat loss (W)
ti = inside air temperature (oC)
U = overall heat transmission coefficient (W/m2K)
ti = inside air temperature (oC)
to= outside air temperature (oC)
Floors
Windows
Draughts
Walls
Roofs
Heat Losses

## Slide 16
Overall Heat Transmission Coefficient (U-value)
Heat Losses

## Slide 17
Heat loss by Ventilation:
The heat loss by ventilation can be calculated as:
Hv = cp ρ qv (ti - to)
Hv = ventilation heat loss (W)
cp = specific heat capacity of air (J/kg K)
ρ = density of air (kg/m3)
qv = air volume flow (m3/s)
ti = inside air temperature (oC)
to = outside air temperature (oC)
Heat Losses

## Slide 18
Environmental Effects

## Slide 19
Orientation for Visual Comfort:
Environmental Effects

## Slide 20
Orientation for Thermal Comfort: wind
Environmental Effects

## Slide 21
Using Ecotect

## Slide 22: Shading device

## Slide 23
Surface Color and Cool Roofs
Environmental Effects

## Slide 24
New Insulation Material

## Slide 25
Project description:
The project is about making new insulation material from local simple ones, with high thermal resistance at low price.

## Slide 26
New thermal insulation material consists of three components:
  Limestone: :
k-value: Theoretical: 0.15-1.1 W/(m.K)
  Uses: Limestone is very common in architecture, especially in Europe and North America. Many landmarks across the world, including the Great Pyramid .
Limestone Characteristics

## Slide 27: Advantages:
Available in Palestine.
It is not expensive in the local market.
Relatively easy to cut into blocks or more elaborate carving.
Long lasting.
Stands up well to exposure.
  Disadvantages:
  Heavy weight
Limestone Characteristics

## Slide 28
Straw:
K-value: 0.09 W/(m.K)
Uses:
Straw-bale construction is a building method that uses bales of straw (commonly wheat, rice, rye and oats straw)
as structural elements, building, or both.
Straw Characteristics

## Slide 29: Advantages:
Lightweight.
Few in the heat conduction.
Disadvantage:
Non-fire-resistant
Unable to withstand stress
Straw Characteristics
Fire ashes:

## Slide 30: The Procedure

## Slide 31
1-The sample was put into molds that fit testing apparatus used.
2-Samples were exposed to heat until they have dried.
Procedure

## Slide 32
3-The samples were ready to test
4-Sample were put one after one between the phases of the apparatus.
Procedure

## Slide 33
5-Cold water was allowed to flow through the heat unit.
6-The apparatus was turned on at 10w heat flux, and then wait for half an hour to reach steady state.
Procedure

## Slide 34
7-The temperature was recorded at all six sensors.
8-Step 6 was repeated at 20w.
9-The temperature was recorded at all six sensors.
10-Step 6 was repeated at 30w.
11-The temperature was recorded at all six sensors.
12-The test was repeated to the other samples.
Procedure

## Slide 35
Experiment Results

## Slide 36
x(mm) |  |  |  |  |  |  |  |  |  |  | 
Q (w) | 5 | 15 | 25 | 30 | 40 | 50 | 55 | 65 | 75 | slope | k (w/k.m)
10 | 78.7 | 78.7 | 78.6 |  |  |  | 18.1 | 18.8 | 0.3536 | 0.3536 | 0.3536
20 | 97.2 | 97.2 | 97.1 |  |  |  | 18.7 | 19.5 | 0.568 | 0.568 | 0.568
30 | 139.4 | 139.4 | 139.3 |  |  |  | 19.2 | 20 | 0.4367 | 0.4367 | 0.4367
Area=0.0037 |  | r=.015 |  |  |  |  |  |  |  | kavg | 0.452767
Chart: X
| 5 | 15 | 25
10 W | 78.7 | 78.7 | 78.6
10w | 18.1 | 18.8 | 18.7
10 W | 78.6 | 18.1
20 W | 97.2 | 97.2 | 97.1
20 W | 97.1 | 18.7
20 W | 18.7 | 19.5 | 19.4
30 W | 139.4 | 139.4 | 139.3
30 W | 139.3 | 19.2
30 W | 19.2 | 20 | 19.9
Sample 1 :

## Slide 37
Sample 2 :
x(mm) |  |  |  |  |  |  |  |  |  |  | 
Q (w) | 5 | 15 | 25 | 30 | 40 | 50 | 55 | 65 | 75 | slope | k (w/k.m)
10 | 79 | 78.9 | 78.9 |  |  |  | 17 | 17 | 17 | -2.0633 | 0.336
20 | 99.2 | 99.2 | 99.1 |  |  |  | 17.4 | 17.3 | 17 | -2.7233 | 0.552
30 | 143.4 | 143.4 | 143 |  |  |  | 17.9 | 17.8 | 18 | -4.18 | 0.4023
Area=0.0037 |  | R=.015 |  |  |  |  |  |  |  | kavg | 0.336241
Chart: X
| 5 | 15 | 25
10 W | 79 | 78.9 | 78.9
10w | 17 | 17 | 16.9
10 W | 78.9 | 17
20 W | 99.2 | 99.2 | 99.1
20 W | 99.1 | 17.4
20 W | 17.4 | 17.3 | 17.2
30 W | 143.4 | 143.4 | 143.3
30 W | 143.3 | 17.9
30 W | 17.9 | 17.8 | 17.8

## Slide 38
x(mm) |  |  |  |  |  |  |  |  |  |  | 
Q (w) | 5 | 15 | 25 | 30 | 40 | 50 | 55 | 65 | 75 | slope | k (w/k.m)
10 | 79 | 78.9 | 78.9 |  |  |  | 16.2 | 16.2 | 16 | -2.09 | 0.3205
20 | 99.2 | 99.2 | 99.1 |  |  |  | 16.4 | 16.4 | 16.5 | -2.7567 | 0.5782
30 | 143.4 | 143.4 | 143.3 |  |  |  | 16.7 | 16.6 | 17.6 | -4.22 | 0.3762
Area=.0037 |  | R=.015 |  |  |  |  |  |  |  | kavg | 0.324007
Chart: X
| 5 | 15 | 25
10 W | 79 | 78.9 | 78.9
10w | 16.2 | 16.2 | 16
10 W | 78.9 | 16.2
20 W | 99.2 | 99.2 | 99.1
20 W | 99.1 | 16.4
20 W | 16.4 | 16.4 | 16.5
30 W | 143.4 | 143.4 | 143.3
30 W | 143.3 | 16.7
30 W | 16.7 | 16.6 | 17.6
Sample 3 :

## Slide 39
Experiment Calculation

## Slide 40
0.3536
0.452767
Sample1:
Sample 2:
Experiment Calculation

## Slide 41
Sample 3:
Experiment Calculation

## Slide 42
The new material that we have made from local raw material (limestone, straw and fire ashes) proves theoretical is good insulation material.
It give us k-value (sample 1 k-value=0.452767 sample 2 k-value=0.4301, sample 3 k-value=0.424907) with acceptable error.
The theoretical value of the insulation material is good, but the error of the apparatus is too large so the practical value is not accurate.
Conclusion:

## Slide 43: Recommendation

## Slide 44
The idea of ​​the project is to increase the thermal efficiency of buildings in order to reduce the loss of thermal energy in the cases of heating and cooling, therefore, we proposed several solutions, as stated at the previous chapters. For the fundamental idea, which is making a new thermal insulation material from local materials found in the Palestinian environment.
The new material is characterized by several features, including:
Its thermal insulation is very good,
samples were tested using apparatus and it gives – k- value (0.424967)
Its low cost because it is widely available.
Ease of formation and use
The possibility of development on it to be moisture proof.
Recommendation :

## Slide 45
Through that, the new material could be more common, it needs more development to produce products that are easy to use, thus increasing the thermal efficiency of buildings, which in turn reduces energy consumption.
Recommendation :

## Slide 46
Thank You