Faculty of Engineering & Information Technology

Chemical Engineering Department

Adsorption of Phenol from Aqueous Solution by Activated Carbon Derived from the Pyrolysis of Waste Tires

Prepared by:

Diana Thabalih

Enas Abu Saif

Hala Abu Shanab

Tahani Qteishat

Supervisor:

Dr. Abdelrahim Abusafa

Presented in Partial Fulfillment of the Requirements for Bachelor Degree in Chemical Engineering

December 2016

الإھداء

لعيون قررت السهر فبعثرتِ الزمن ، لسنوات خمس وبعض خمس،

لطابق كلّيتنا الأول، للقاعة ٢٣٠، لأدوات المختبر التي كنّا نحرص

عليها كحرص أمٍ على وليدها، للقاعة ١٩١، لأحلامنا المعلقة على درج الطوارئ،

لدعوات أمهاتنا التي رصصنا بها مشروعنا هذا، ولأموال آبائنا التي أوصلتنا

إلى هذه الصفحة الآن ، لتلافيف أدمغتنا المنهكة لأقلامنا لدفاترنا لأمانينا..

وأخيرا، للوطن الذي ننتظر منه وظيفة وينتظر منا التحرير.. وكلانا ينتظر...

- Abstract

The production of activated carbon from waste tires and evaluate its ability for the removal of phenol from aqueous solutions in batch process is the aim of our study. The activation process was carried out by washing carbon by KOH then heated at 550°C for 2 hour under nitrogen flow rate after that washing with HCl and dried. The adsorption capacity performances of prepared carbon that washed by two solutions (water and HCl) of different particles size in this work were investigated using phenol. The kinetic adsorption study was carried out at initial concentration of phenol (30 ppm) at room temperature (25ºC) for 48 h with 0.5g carbon. The adsorption capacity was found to increase with decreasing the particle size. The results obtained show that the pseudo-second order model was the best to describe adsorption kinetic data for phenol adsorption by activated carbon with R2 value of 0.993 and adsorption capacity qm was 9.091 (mg/g), for carbon washed by water for (0.425 – 2 mm and 2 – 4 mm) particles size with R2 value of 0.998 and 0.992 and adsorption capacity qm was 7.634 and 7.194 (mg/g), respectively, and for carbon washed by HCl for (0.425–2 and 2– 4 mm) particles size with R2 value of 0.994 and 0.982 and adsorption capacity qm was 8.0645 and 6.6667 (mg/g), respectively. For phenol isotherm adsorption, the adsorption data were fitted to Langmuir isotherm for phenol adsorption by activated carbon with R2 value of 0.957 and adsorption capacity qm was 4.281 (mg/g), for carbon washed by water for (0.425 – 2 mm and 2 – 4 mm) particles size with R2 value of 0.99 and 0.979 and adsorption capacity qm was 1.889 and 1.7006 (mg/g), respectively, and for carbon washed by HCl for (0.425–2 and 2– 4 mm) particles size with R2 value of 0.976 and 0.983 and adsorption capacity qm was 3.937 and 3.597 (mg/g), respectively. From adsorption capacity data, the carbon washed with HCl is better than the carbon washed with water but in a slightly small different which is means the washing solution has no effect on adsorption of phenol. The acetic acid adsorption was Freundlich isotherm so it is a multilayer adsorption which means the surface area measurement is hard to measured by this method. The result in this research indicated that activated carbon from waste tires was an attractive adsorbent for removal of  phenol from aqueous solutions.

- Table of contents

Abstract	i

List of tables	v

List of figures	vii

Chapter 1.	Introduction	1

Chapter 2.	Activated carbon	3

2.1	Definition of activated carbon	3

2.2	Raw materials of the activated carbon	3

2.3	Characteristics of activated carbon and how it works	3

2.4	Types of activated carbon and its classifications	4

2.5	Properties of the activated carbon	5

2.6	Estimation of surface area of activated carbon	7

2.7	Preparation of activated carbon from steam and chemical activation	10

2.8	Production of activated carbon	11

(a)	Pyrolysis of waste tires	12

2.9	Application usage of activated carbon	13

2.10	Activated Carbon Efficiency	14

2.11	Quality assurance and test of activated carbon	15

Chapter 3.	Adsorption	16

3.1	Definition of Adsorption	16

3.2	Adsorption Mechanisms	16

3.3	Types of Adsorption	17

(a)	Energetic Considerations	18

3.4	Differentiating physical and chemical adsorption	19

3.5	Common Adsorbents and it’s applications	20

3.6	Factors affecting adsorption	21

3.7	Effects of Adsorption on the Nature of the Solid Surface	21

(a)	Adsorption at the solid-vapor interface	22

3.8	Isotherms	22

(a)	Types of adsorption isotherms	22

(b)	Kinetics of  isotherm	25

(c)	Classification of Adsorption Isotherm	29

3.9	Different modes of operation	29

Chapter 4.	Literature Review	32

Chapter 5.	Experiment work	35

5.1	Preparation of pyrolyzed carbon	35

(a)	Preparation of  pyrolyzed carbon washed with HCl	35

(b)	Preparation of  pyrolyzed carbon washed with water:	36

5.2	The activation	36

Chemical activation with KOH	37

5.3	Phenol adsorption	37

(a)	Phenol preparation	37

5.4	Batch adsorption	37

5.5	Surface area measurement	38

Acetic acid	38

Chapter 6.	Result and Dissection	39

6.1	Calibration Curve	39

6.2	Equilibrium study	39

(a)	The Langmuir isotherm	40

(b)	The Freundlich isotherm	42

6.3	Kinetic  Study	46

6.4	Surface area measurement	52

Chapter 7.	Conclusion	53

Chapter 8.	Recommendations	54

Chapter 9.	Reference	55

Chapter 10.	Appendix	59

- List of tables

Table ‎3-1 : Langmuir forms.	24

Table ‎6-1 : Langmuir phenol adsorption and Freundlich phenol adsorption isotherm.	43

Table ‎6-2: Pseudo first order and pseudo second order of phenol kinetic adsorption.	49

Table 4: Calibration data of Phenol concentration.	59

Table 5: Kinetic adsorption phenol data adsorbed on carbon washed by water of (0.425 – 2 mm) particle size.	60

Table 6: Kinetic adsorption phenol data adsorbed on carbon washed by water of ( 2 – 4  mm) particle size.	61

Table 7: Kinetic adsorption phenol data adsorbed on carbon washed by HCl of ( 0.425 – 2  mm) particle size.	62

Table 8: Kinetic adsorption phenol data adsorbed on carbon washed by HCl of ( 2 – 4  mm)  particle size.	63

Table 9: Kinetic adsorption phenol data adsorbed on activated carbon washed by HCl of ( 0.425 – 2 mm) particle size.	64

Table 10: Isotherm  adsorption phenol data adsorbed on carbon washed by water of (0.425 – 2 mm) particle size.	65

Table 11: Isotherm adsorption phenol data adsorbed on carbon washed by water of ( 2 – 4  mm) particle size.	65

Table 12: Isotherm  adsorption phenol data adsorbed on carbon washed by HCl of ( 0.425 – 2  mm) particle size.	66

Table 13: Isotherm  adsorption phenol data adsorbed on carbon washed by HCl of ( 2 – 4  mm)  particle size.	66

Table 14: Isotherm  adsorption phenol data adsorbed on activated carbon washed by HCl of ( 0.425 – 2 mm) particle size.	67

Table 15:  Acetic acid adsorption data adsorbed on carbon washed by water of ( 0.425 – 2 mm) particle size.	67

Table 16: Acetic acid adsorption data adsorbed on carbon washed by water of ( 2 – 4 mm) particle size.	68

Table 17: Acetic acid adsorption data adsorbed on carbon washed by HCl of (0.425 – 2 mm) particle size.	68

Table 18: Acetic acid adsorption data adsorbed on carbon washed by HCl of ( 2 – 4 mm) particle size.	69

Table 19: Acetic acid adsorption data adsorbed on activated carbon washed by HCl of ( 0.425 – 2 mm) particle size.	69

- List of figures

Figure ‎2-1 : Contaminated water and air through the Activated Carbon.	4

Figure ‎2-2 : Langmuir Linear plots of MB on the produced A.Cs.	8

Figure ‎2-3 : Freundlich Linear plots of MB on the produced ACs.	9

Figure ‎3-1 : Physical Adsorption Vs. Temperature graph.	18

Figure ‎3-2 : Chemical Adsorption Vs. Temperature graph.	18

Figure ‎3-3 : Basic Adsorption Isotherm.	22

Figure ‎3-4 : Monolayer adsorption type 1 isotherm.	25

Figure ‎3-5 : Type II Adsorption isotherm.	26

Figure ‎3-6 : Type III Adsorption isotherm.	27

Figure ‎3-7: Type IV adsorption isotherm.	28

Figure ‎3-8 : Type V adsorption isotherm.	28

Figure ‎3-9:Breakthrough curve.	30

Figure ‎3-10: Favorable isotherm of the Langmuir or Freundlich type.	31

Figure ‎5-1: The steps that was followed in this work.	35

Figure ‎5-2 : Two-dimensional representation of carbon activation.	36

Figure ‎6-1: Calibration Curve of phenol solution.	39

Figure ‎6-2: Langmuir Adsorption Isotherm for phenol adsorption on carbon washed by water for two particles size.	41

Figure ‎6-3: Langmuir Adsorption Isotherm for phenol adsorption on carbon washed by HCl for two particles size.	41

Figure ‎6-4: Langmuir Adsorption Isotherm for phenol adsorption on activated carbon washed by HCl for particle size (0.425 – 2 mm).	42

Figure ‎6-5 : Effect of particles size on isotherm adsorption of phenol on carbon washed by water.	43

Figure ‎6-6: Effect of particles size on isotherm adsorption of phenol on carbon washed by HCl.	44

Figure ‎6-7: Effect of washed solution on isotherm adsorption of phenol for particle size of (2-0.425 mm).	45

Figure ‎6-8: Effect of washed solution on isotherm adsorption of phenol for particle size of  (2 - 4 mm).	45

Figure ‎6-9: Effect of washed solution on isotherm adsorption of phenol on carbon washed by HCl, water and A.C for particle size of (2-0.425 mm).	46

Figure ‎6-10: Pseudo second order for phenol adsorption on carbon washed by water for two particles size.	47

Figure ‎6-11: Pseudo second order for Pseudo second order for phenol adsorption on carbon washed by HCl for two particles size.	48

Figure ‎6-12: Pseudo second order for phenol adsorption on activated carbon washed by HCl for particle size (0.425 – 2 mm).	49

Figure ‎6-13: Effect of particles size on kinetic adsorption of phenol on carbon washed by water.	50

Figure ‎6-14: Effect of particles size on kinetic adsorption of phenol on carbon washed by HCl.	50

Figure ‎6-15: Effect of washed solution on kinetic adsorption of phenol for particle size of (2-0.425 mm).	51

Figure ‎6-16: Effect of washed solution on kinetic adsorption of phenol for particle size of (2 -4 mm).	51

Figure ‎6-17: Effect of washed solution on kinetic adsorption of phenol on carbon washed by HCl, water and A.C for particle size of (2-0.425 mm).	52

- Introduction

Water is a source of life and energy, although millions of people worldwide are suffering with the shortage of fresh and clean drinking water. Industrial development has led to major problems of environmental pollution level. Large amounts of pollutants are released into bodies of water such as VOCs, metal ions, and large amount of phenol and its derivatives, among others. This rapid pace of industrialization, population expansion, and unplanned urbanization has contributed largely to the severe water pollution and surrounding soils. Each of these contaminants is highly detrimental to ecosystems and human health. [1]

Phenol is an important chemical which is used in the manufacture of many products such as dyes, synthetic resins, pesticides, tanning materials, perfumes and medicinal products, lubricants, essential oils, solvents, etc. It is very toxic even present as traces in industrial waste water effluents. It may constitute a potential pollution source of ground waters and hence it has to be eliminated. [2]

Hazards associated with scrap tires can cause both health and environmental problems. The accumulation of scrap tires results in large spaces occupied and wastage of a valuable energy resource. The huge amount and high stability of scrap tires have made their disposal is a serious environmental problem. Although pyrolysis is considered as an eﬀective and environmentally friendly disposal method, a proper utilization for the residues generated is still a problem to be solved. The production of pyro-oil from tire pyrolysis as a fuel source has generated considerable interest. However, most research emphasis has been focused on the identiﬁcation of the pyro-oil components. During the past 10–15 years, several fundamental studies have reported that carefully controlled tire pyrolysis can produce a number of valuable products. However, several studies have reported the production of char and activated carbons from waste tires. The potential of these products as possible adsorbents for various pollutants has been assessed and found to be very successful, thus stimulating a serious research interest. These active carbons have been used to adsorb phenols, basic dyes, metals, p-chlorophenols, butane and natural gas.

The treatment processes for phenolic wastewater can be classified into two basic categories :

a) Destructive process such as destructive oxidation with ozone, hydrogen peroxide or manganese oxides.

b) Recuperative processes such as adsorption into porous solids, membrane separation and solvent extraction. [3]

Hence activated carbon is the most suitable material to be used to adsorb this harmful chemical because of their larger surface area. The pyrolysis of waste tires is rich carbonaceous material which remains after separation of oil from the waste tires and because it do not readily degrade in the environment.

The main objective of this work is to produce activated carbon from waste tires and to evaluate its ability for the removal of phenol from aqueous solutions in batch and continuous processes. Equilibrium studies will be conducted in the different concentration ranges. The effect of temperature, pH will be investigated. The experimental data will be analyzed by the Langmuir, Freundlich, Temkin and Dubinin–Radushkevich isotherm models. The kinetic data will also modeled by suitable first or second order kinetic models. The specific objectives can be summarized as:

- Produce activated carbon from waste tires.

- Investigate the properties of the prepared activated carbon.

- Test the produce carbon for phenol removal.

- Model the result with necessary equilibrium and kinetic model.

Activated carbon

Definition of activated carbon

Activated carbon, also called activated charcoal or activated coal, is a carbon material widely used not only as adsorbent but also as catalyst and as a support for catalysts is a form of a solid, porous, carbonaceous material prepared by carbonizing and activating organic substances that has been processed to make it extremely porous and thus to have a very large surface area available for adsorption or chemical reactions and its subjected to thermal treatment with oxidizing gases, vapors or a mixture of both (steam) to increase its adsorptive properties. [4]

Raw materials of the activated carbon

The raw materials which include saw dust, peat, lignite, coal, cellulose residues, coconut shells, petroleum coke, may be carbonized and activated at high temperature with or without the addition of inorganic salts in a stream of activating gases such as steam or carbon dioxide, woods, fruit stones, and synthetic macromolecular systems are used also.

AC can be made out of wood, but coconut shell is a cheaper and widely available raw material considered as farm waste by-product. [5]

Many agricultural by-products were used for activated carbon preparation such as; peach stones, apricot stones, cherry stones, dates stones and pits, waste apple pulp, nut shells, pecan shell, walnut shells, almond shells, oil palm waste, rice husks, tea waste, coffee bean, grounds corncob, cotton stalks and olive waste. Olive wastes are available in large amounts in many countries at very low cost. [6]

Characteristics of activated carbon and how it works

The characteristics of activated carbon are:

- Solubility: activated carbon insoluble in water and organic solvents.

- Burning: when heated to redness it burns slowly without a flame.

- Ignition: when ignite a portion of the sample in air, carbon monoxide and carbon dioxide are produced, and an ash remains. [5]

How the activated carbon work

Contaminated water or air flows through the AC, the contaminants sorbs to the outer and inner surfaces of the granules as shown in the figure (2-1). The water and air exiting the container will be cleaner. Regular testing of exiting water or air used to check contaminant levels. If testing shows that some contaminants remain, the water or air may need to be treated again to meet the treatment levels. The AC will need to be replaced when the available surfaces on the activated carbon are taken up by contaminants and additional contaminants can no longer adsorb to them. [7]

Figure ‎2-1 : Contaminated water and air through the Activated Carbon.

Types of activated carbon and its classifications

Some broad classification is made for general purpose based on their physical characteristics:

- Powdered activated carbon (PAC): Active carbons are made in particular form as powders or fine granules less than 1.0 mm in size with an average diameter between 0.15 and 0.25 mm. Thus they present a large surface to volume ratio with a small diffusion distance.

- Granular activated carbon (GAC): It has a relatively larger particle size compared to powdered activated carbon. These carbons are therefore preferred for all adsorption of gases and vapors as their rate of diffusion are faster. The most popular aqueous phase carbons are the 12×40 and 8×30 size, because they have a good balance of size, surface area, and head loss characteristics.

- Extruded activated carbon (EAC):It combines powdered activated carbon with a binder which are fused together and extruded into a cylindrical shaped activated carbon block with diameters from 0.8 to 130 mm.

- Bead activated carbon (BAC).

- Impregnated carbon.

- Porous carbon containing several types of inorganic impregnated such as iodine, silver, and cations such as Al, Mn, Zn, Fe and Li.

- Polymer coated carbon: This is a process by which a porous carbon can be coated with a biocompatible polymer to give a smooth and permeable coat without blocking the pores. The resulting carbon is useful for him perfusion. [8]

- Other Uncategorized: Activated carbon is also available in special forms such as cloths and fibers. [6]

Properties of the activated carbon

- Porosity and surface area:

Carbon adsorbents have a porous carbon structure, which contains small amounts of different heteroatom such as Oxygen and Hydrogen. Some activated carbons also contain variable amounts of mineral matter (ash content) depending on the nature of the raw material used as precursor. The porous structure is perhaps the main physical property that characterizes activated carbons. This is formed by pores of different sizes which according to IUPAC recommendations can be classified into three major groups:

• Micro pores with a pore width of less than 2×10-9m.

• Meso pores with widths from 0.2 to 50×10-9 m.

• Macro pores with a pore width larger than 50×10-9 m.

A high surface area and an adequate pore size distribution are necessary conditions for a carbon adsorbent to perform well in a particular application. In particular activated carbons (non-graphitizable carbons) have a relatively large edge area, which results in a strong propensity for Oxygen chemisorptions. Thus, molecular Oxygen can dissociate into atoms that react chemically with atoms of carbon to form Oxygen surface compounds. This oxidation process is particularly significant as the temperature of the reaction increases. [6]

- Apparent density: Higher density provides greater volume activity and normally indicates better quality activated carbon.

- Hardness/abrasion number: It is a measure of the activated carbon’s resistance to attrition.

- Ash content: It reduces the overall activity of activated carbon.

- Carbon tetrachloride activity: Measurement of the porosity of an activated carbon by the adsorption of saturated carbon tetrachloride vapor.

- Particle size distribution: The finer particle size of an activated carbon, the better access to the surface area and the faster rate of adsorption kinetics.[6]

- Iodine number: Iodine number is the most fundamental parameter used to characterize activated carbon performance often reported in mg/g (typical range 500-1200 mg/g).

- Molasses: Molasses number or molasses efficiency is a measure of the mesopore content of the activated carbon (greater than 20 Å or larger than 2 nm) by adsorption of molasses from solution. [5]

- Ethylene blue: Some carbons have a mesopore (20-50 Å or 2-5 nm) structure which adsorbs medium size molecules, such as the dye ethylene.

- Dechlorination: Some carbons are evaluated based on the dechlorination half-value length, which measures the chlorine-removal efficiency of activated carbon. [9]

Estimation of surface area of activated carbon

We can determine the surface area (SA) by the following methods:

- Determination of activated carbon surface area (SA)  related to dye adsorption in (m2/g) after the equilibrium occurs in the adsorption process between solutions of different concentrations of iodine I2 and  methyl blue MB dye respectively that will contacting with amount of the AC  the following equation:

SADye= Qm×σ×10-20×Nn		 (2-6-1)

Where,

σ  is the cross sectional area of solute in (m2/g), N is Avogadro’s number, and n is the aggregation factor. Qm is the amount adsorbed per mass unit of adsorbent corresponding to complete monolayer coverage on the surface which we determine it by:

- By using the linear form of Langmuir equation, which is valid for monolayer adsorption on the surface as expressed in equation (2-6-2):

CeQe= 1KL×Qm+CeQm			 (2-6-2)

Where

KLis the Langmuir constant, Qe is the adsorbed quantity of dye that can be find by using The following equation which used for determining the adsorbed amount of dye:

Qe=(C0-Ce)×VW			(2-6-3)

Where C0 and Ce are the initial and the equilibrium liquid phase concentrations, respectively (mg/L), V is the volume of the solution, and W is the weight of the carbon used (g).

The values of Qm and Langmuir constants KL of   I2and MB dye adsorption on the produced ACs will found from the linear Langmuir plots of the Qe in (mg/g) Vs. Cein (mg/L)as shown in figure (‎2-2).

Figure ‎2-2 : Langmuir Linear plots of MB on the produced A.Cs.

- Or by using the linear form of a Freundlich isotherm equation, which is valid for monolayer adsorption on the surface as expressed in equation (2-6-4):

lnQe=lnK+1n* 1lnCe	(2-6-4)

Where:

- Ce is equilibrium concentration of the sorbet in (mg/L), Qe is the amount adsorbed in (mg/g) of AC, K is the unit capacity factor, and n is an empirical parameter that represents the heterogeneity of the site energies or the affinity of the adsorbate to the carbon surface, while Freundlich constants are given from Freundlich Linear plots of the relationship between lnQe in (mg/g) and lnCe (mg/l) for MB on the produced ACs as shown in figure (‎2-3). [10]

Figure ‎2-3 : Freundlich Linear plots of MB on the produced ACs.

- We can also use acetic acid to estimate activated carbon surface area when the adsorption of the adsorbate leads to maximum single molecular layer when the adsorption is complete, then we can calculate the area of the adsorbent that equal the total area of the adsorbed molecules, the number of moles of acid adsorbed per gram adsorbent is independent of chain length the cross suction area Aa of straight-chain acid may be taken to be about 21×10-20m2. The specific area of adsorbent S (m2/g) is then given by:

S=Aa×Na×Ymax			 (2-6-5)

Where:

Na is Avogadro's number, Ymax the amount adsorbed when the surface is just covered with amonomolecular layer of the adsorbate.

- The surface areas of activated carbons are usually measured using the Brunauer-Emmett-Teller (BET) method, which employs the nitrogen adsorption at different pressures at the temperature of liquid nitrogen (77 K). The surface area according to BET is determined by the product of the cross-sectional area of the nitrogen molecule, of the Avogadro's number and of the specific monolayer capacity of nitrogen, which is obtained by an equation proposed by BET with further modifications. For the pore volume determination, the procedure more commonly used also uses nitrogen adsorption isotherm data. The total pore volume is estimated from the amount of nitrogen adsorbed at the highest relative pressure and the micro pore volume is calculated from the nitrogen adsorption isotherms using the Dubinin-Radushkevich equation. In spite of these methods being more used and employed as a reference in the surface area and pore volume determination of porous materials, they are time consuming and require the use of expensive equipment. [10]

Preparation of activated carbon from steam and chemical activation

Activated carbon is made from carbon-based materials like coal or wood that is first heated without oxygen to produce charcoal and tar or pitch, which bubbles out.

The charred material is then heat up with steam or carbon dioxide to above which further erodes and corrodes it to remove everything. The result is an airy, delicate structure that is nearly pure carbon and full of holes, if we continue along period to blow in more steam we have more empty spaces (pores). It is then crush to a powder and mix with binders to form granules of desired size ranges for different filter media.

A series of activated carbons we can prepare from bituminous coal by chemical activation with potassium hydroxide and zinc chloride and also by physical activation with carbon dioxide. [11]

The effect of process variables such as carbonization time, temperature, particle size, chemical agents and method of mixing and impregnation ratio in the chemical activation process will be study to optimize those preparation parameters. Chemical activation will be carried out at low temperature and high temperature conditions.

In low temperature, the sample will be activated by mixing and heating with chemical reagents at low temperatures. ZnCl2, Na2CO3, H3PO4, NaOH and KOH will use as chemical reagents. Impregnation ratio between chemical reagents and precursor will chose, the samples will be stirred continuously in each chemical reagent of a specific percentage solution at known temperature, Then activated sample will filter by vacuum and dry at a specific temperature. After the activation process, the carbonization process applies to the product obtained. During the carbonization process, N2 will introduce to the system by a flow rate. The carbonization processes conduct in a programmable tube furnace. The furnace Programs in such a way that heating rate shall be specific value and after reaching the final temperature it will then remain at that temperature for specific time. At the end of this period the furnace is lifted to cool itself. The carbonized product stirrer with HCl at specific temperature on a heating magnetic stirrer and then it filter. Then it rinse with distillated water several times until the pH of the activated carbon-distillated water mixture has exceeded specific number. Finally, the obtained product will dry and characteristic properties of obtained activated carbon like iodine number (mg/g), BET surface area (m2/g) and pore distribution (micropore, mesopore) (cm3/g) will determine.

At high temperature, the sample will activate by boiling it with chemical reagents of NaOH and KOH, ZnCl2, Na2CO3 and H3PO4. While increasing the carbonization temperature enhances surface area and pore volumes of KOH-activated carbon, it destroys carbon structure in the ZnCl2 carbon series. The sample will put into a volumetric flask with a specific percentage chemical reactive solution so that impregnation ratio between chemical reagents and precursor will find. A condenser will mount to the flask to prevent evaporation. The mixture will boil in an oil bath. At the end of this period, the mixture will be cooled, filtrated by vacuum and then will dry. The carbonization process apply to the sample after the activation process. The effect of temperature on carbonization investigate by selecting furnace final temperature, The furnace programs in such a way that heating rate will find and after reaching the final temperature it will then remain at that specific temperature. At the end of this period the furnace leaves to cool itself. N2introduce to the system during the carbonization process. Then, the carbonized product will be mixed with HCl and the mixture will be heated and stirred in a heating magnetic stirrer and it will filtrate by vacuum. Then they obtained activated carbon will rinse with distillated water several times until the pH of the activated carbon-distillated water mixture has exceeded specific value. The obtained product will be dried Finally, characteristic properties of obtained activated carbon like iodine number (mg/g), BET surface area (m2/g) and pore distribution (micropore, mesopore)(cm3/g) will be determined. [12]

Production of activated carbon

Activated carbon is carbon produced from carbonaceous source materials like nutshells peat, wood, coir, lignite, coal and petroleum pitch. It can be produced by one of the following processes:

- Physical reactivation: The precursor is developed into activated carbons using gases, this is generally done by using one or a combination of the following processes:

- Carbonization: Material with carbon content is pyrolyzed at temperatures in the range 600-900 °C, in absence of air (usually in inert atmosphere with gases like argon or nitrogen (.

- (Activation/Oxidation): Raw material or Carbonized material is exposed to oxidizing atmospheres dioxide, oxygen or steam) at temperatures above 250 °C, usually in the temperature range of (600-1200 °C).

- Chemical activation: Prior to carbonization, the raw material is impregnated with certain chemicals. The chemical is typically an acid strong base, or a salt (phosphoric acid, sodium hydroxide, zinc chloride, respectively). Then, the raw material is carbonized at lower temperatures (450-900 °C). It is believed that the carbonization/activation step proceeds simultaneously with the chemical activation.

Chemical activation is preferred over physical activation owing to the lower temperatures and shorter time needed for activating material. [6]

Carbonaceous matter may be treated with a chemical activating agent such as phosphoric acid or zinc chloride and the mixture carbonized at an elevated temperature, followed by removal of the chemical activating agent by water washing. [5]

Pyrolysis of waste tires

Many years back, incineration (without the recovery value) and landfill were the main and practical means for dealing with the problem of waste tires. However, in light of the overall environmental impact along the drive toward energy and material conservation, more emphasize now has been given to the new disposal options having higher energy recovery values, and also being attractive environmentally.

Pyrolysis is defined as chemical decomposition induced in organic materials by heat in the absence of oxygen. In practice, it is not possible to achieve a completely oxygen-free atmosphere; actual pyrolytic systems are operated with less than stoichiometric quantities of oxygen. Because of some oxygen will be present in any pyrolytic system, the nominal oxidation will be occur. If volatile or semi volatile materials are present in the waste, thermal desorption will also occur.

Pyrolysis transforms hazardous organic materials into gaseous components, small quantities of liquid, and a solid residue (char) containing fixed carbon and ash. Pyrolysis of organic materials produces combustible gases, including carbon monoxide, hydrogen, methane and other hydrocarbons. If the off-gases are cooled, liquids condense producing an oil/tar residue and contaminated water. Pyrolysis typically occurs under pressure and at operating temperatures above 430 °C (800 °F). The pyrolysis gases require further treatment. The off-gases may be treated in a secondary combustion chamber, flared, and partially condensed. Particulate removal equipment such as fabric filters or wet scrubbers are also required. [13,14]

Pyrolysis offers an environmentally attractive method to decompose a wide range of wastes chemically (using system working at high temperature and oxygen free environment), producing lower emission of nitrogen-oxide, sulfur-oxide and side by side valuable reusable products. For example, the oil and gas can be used as fuels within the pyrolysis system or for an adjacent plant such as combined heat and power system. [15]

Application usage of activated carbon

- Water Purification and groundwater contamination.

- Acid rain protection.

- Removes Siloxane.

- Catalytic Deodorizer.

- Volatile organic compound (VOC).

- Garbage incineration. [16]

- Automotive: Activated carbon canisters reduce the hydrocarbon emissions from gasoline-powered automobiles and trucks. Also many cars now include air purification systems that utilize activated carbon in their cabin air filters.

- Food and beverages: Activated Carbon products are used to improve the quality of beverages ranging from water to fruit juices to distilled liquor beverage makers rely on activated carbon to remove bad tastes and odors and help ensure the long-term stability of their products, it is used in:.

- Sugar and Starch.

- Chili and Spices.

- Beer and Wine.

- Caffeine.

- Oil Refining: UCI’s Oil Refining Grade Carbon’s. [16]

- Air purification.

- Water treatment.

- Mining (Gold Processing).

- Agriculture.

- Pharmaceuticals. [4]

- Gas purification.

- Gold purification.

- Metal extraction.

- Medicine.

- Sewage treatment.

- Gas masks. [17]

Activated Carbon Efficiency

- Activated carbon efficiency for removing a given pollutant depends on both its surface chemistry and its adsorption capacity. The activated carbon adsorption capacity is usually attributed to its internal pore volume that may be distributed throughout the solid as pores ranging in width from microspores to macrospores.

- When the pore sizes of the activated carbon are in the size range of the pollutants, adsorption process will be enhanced and is expected to be efficient. Adsorption capacity of the finished activated carbons also depends essentially on the type of the activation methods and on the structural properties of the original precursor material. [18]

Quality assurance and test of activated carbon

Our entire production is tested for the various parameters such as:

- Methylene Blue value.

- Iodine.

- Ash.

- Moisture.

- Fe (Iron) ppm.

- Chlorides and Sulphate.

- Mesh Size.

- Hardness. [16]

Adsorption

Definition of Adsorption

Adsorption is a physical process in which dissolved molecules or small particles are become attached to the surface of something larger according to energy differences and electrical attractive forces, as Vander-Walls forces, cause molecules of the adsorbate to physically fasten and stick onto the adsorbent. In this kind of process we can remove very tiny particles or dissolved contaminants from water such as phenol and lead, some pesticides, viruses and asbestos fibers it used if there are particles in water that are dissolved or are too small and cannot be removed by mechanical filtration. [19]

Adsorption is surface phenomenon which may be defined in terms of an unit operation in the chemical engineering sense and that operation which deals primarily with the utilization of surface forces, and concentration of materials on the surface of solid bodies referred to as adsorption. Alternatively, it may be defined as either partitioning of chemical species between bulk phase and an interface, or accumulation of substances near the interface, an interface has the special properties of adsorption was first theoretically systematized. [20]

Adsorption Mechanisms

Adsorption from solutions is a competitive process where equilibrium is determined by many factors resulted from adsorbents, adsorbates, and solvent properties. The porous structure of a solid, its energetic heterogeneity, and surface chemical properties are the main factors influencing adsorption equilibria. For a given adsorbent, the adsorption of it towards different adsorbates is a function of the solubility, polarity, structure, mass, and size of the adsorbate molecules. [21]

Adsorbed depends on a number of factors including: the degree of attraction, the surface area exposed to mobile particles, the concentration of the contaminants, the pH and temperature of the liquid. Typically, the strongest adsorbents are micro porous or finely divided solids(clays, charcoal, powdered metals) and liquids (fine droplets like aerosols and sprays). [19]

The driving force for adsorption is the reduction in interfacial (surface) tension between the fluid and the solid adsorbent as a result of the adsorption of the adsorbate on the surface of the solid.

The surface or interfacial tension σ, is the change in free energy G, resulting when the area between two phases A is increased.

In the Adsorption process there is two parts mainly:

- Adsorbate or solute the material being adsorbed (e.g., 2,4,6-trichlorophenol).

- Adsorbent the solid material being used as the adsorbing phase (e.g., activated carbon). [22]

Types of Adsorption

Forces of attraction exist between adsorbate and adsorbent. These forces of attraction can be due to Vander-Walls forces of attraction which are weak forces or due to chemical bond which are strong forces of attraction. On the basis of type of forces of attraction existing between adsorbate and adsorbent.

Adsorption can be classified into two types:

- Physical Adsorption or Physisorption

When the force of attraction existing between adsorbate and adsorbent are weak Vander-Walls forces of attraction, the process is called Physical Adsorption or Physisorption. Physical Adsorption takes place with formation of multilayer of adsorbate on adsorbent. It has low enthalpy of adsorption i.e. ΔHadsorption is 20-40 KJ/mol.

It takes place at low temperature below boiling point of adsorbate. As the temperature increases in, process of Physisorption decreases.

Figure ‎3-1 : Physical Adsorption Vs. Temperature graph.

- Chemical Adsorption or Chemisorption:

When the force of attraction existing between adsorbate and adsorbent are chemical forces of attraction or chemical bond, the process is called Chemical Adsorption or Chemisorption. Chemisorption takes place with formation of unilayer of adsorbate on adsorbent. It has high enthalpy of adsorption.

It can take place at all temperature. With the increases in temperature, Chemisorption first increases and then decreases. [23]

Figure ‎3-2 : Chemical Adsorption Vs. Temperature graph.

Energetic Considerations

Physical adsorption versus Chemical adsorptions

- The forces involved in adsorption processes :

- Non-specific forces (physical adsorption) –Vander-Walls forces, electrostatic forces.

- Specific forces (chemisorptions) - Chemical bounds

- Vapor adsorbs on a solid surface is a spontaneous process.

Overall free energy change (△G):Negative, degree of freedom (△S): decrease negative

ΔG = ΔH − TΔS

For △G to be negative △H should be negative, that is adsorption must be an exothermic process.

- The situation may be different in the solid/liquid system.

- Measurement of heat of adsorption, △H -  by Clausius - Clapeyron equation:

(dlnPdT)v = - ∆HadsRT2			(3-3-1)

For physical adsorption, △Hads ≈ heat of condensation

- For example: heat of condensation of N2 = -6 KJ/mole

△Hads of N2 on iron = -10 KJ/ mole

On graphite = -12 KJ/mole

On TiO2 = -14 KJ/mole

Chemisorptions of N2 on iron = -150 KJ/mole

- Physical adsorption: is generally a multilayer process, not limited by the available solid surface area, reversible, more rapid, occurs on almost all solid surface.

- Chemisorptions: limited to the formation of a monomolecular adsorbed layer, has some activation energy, much slower than physical adsorption may not be reversible. [24]

Differentiating physical and chemical adsorption

A solid material usually exhibits a heterogeneous distribution of surface energy. Gas, vapor, or liquid molecules may become bound to the surface if they approach sufficiently close to interact. The solid is called the adsorbent; the gas or vapor molecule prior to being adsorbed is called the adsorptive and while bound to the solid surface, the adsorbate. Physical adsorption is the result of a relatively weak solid-gas interaction. It is a physical attraction resulting from nonspecific, relatively weak Vander Waal's forces and adsorption energy usually not exceeding 80 kJ/mole, with typical energies being considerably less. Physically adsorbed molecules may diffuse along the surface of the adsorbent and typically are not bound to a specific location on the surface. Being only weakly bound, physical adsorption is easily reversed. Adsorption also can result in a surface complex, a union much stronger than a physical bond with heats of adsorption up to about 600 kJ/mole for C-N bonds and 800 kJ/mole for chemical bonds. A chemical bond involves sharing of electrons between the adsorbate and the adsorbent and may be regarded as the formation of a surface compound. Due to the bond strength, chemical adsorption is difficult to reverse. Physical adsorption takes place on all surfaces provided that temperature and pressure conditions are favorable. Chemisorption, however, is highly selective and occurs only between certain adsorptive and adsorbent species and only if the chemically active surface is cleaned of previously adsorbed molecules. Under proper conditions, physical adsorption can result in adsorbed molecules forming multiple layers. Chemisorption, in the typical case, only proceeds as long as the adsorptive can make direct contact with the surface; it is therefore a single-layer process. Exceptions can exist if the adsorptive is highly polar such, NH3 being an example. Both physical and chemical adsorption may occur on the surface at the same time; a layer of molecules may be physically adsorbed on top of an underlying chemisorbed layer. The same surface can display Physisorption at one temperature and chemisorptions at a higher temperature. For example, at liquid nitrogen temperature (77 K) nitrogen gas is adsorbed physically on iron but at 800 K, an energy level too high for physical adsorption bonds, nitrogen is adsorbed chemically to form iron nitride. [25]

Common Adsorbents and it’s applications

There's a variety in adsorbents which have a lot of application and here is the common adsorbents and its applications:

- Activated carbon: Used to absorb nitrogen from air, hydrogen from syngas, 
ethene from methane and hydrogen and vinyl chloride monomer (VCM) from air. Also it’s used as a removal of odors from gases and removal of SOX and NOX, and it’s used to recovery of solvent vapors, and to purification of Helium, and to clean-up of nuclear off-gases and water purification.

- Activated Alumina: Used to drying of gases, organic solvents and transformer oils, also used as a removal of HCl from hydrogen and removal of Fluorine in alkylation process.

- Silica Gel: Used to absorb oxygen from air, also to drying of gasses and drying of refrigerants and organic liquids, it used to removing water from a zeotropes, also to sweetening sour gases and liquids, it used also to purification of hydrogen, also used in separation of ammonia and hydrogen, separation of oxygen and argon, separation of xylenes and ethyl benzene, separation of normal from branched paraffin’s and separation of olefins and aromatics from paraffin’s, it used in recovery of carbon dioxide, recovery of carbon monoxide from methane and hydrogen and recovery of fructose from corn syrup.

- Polymers & Resins: Used in water purification, it also used in recovery and purification of steroids, amino acids, and recovery of proteins and enzymes, it used in separation of fatty acids from water and toluene and separation of aromatics from Aliphatic, and it’s used as a removal of colors from syrups and removal of organics from hydrogen peroxide.

- Clay: Used in treatment of edible oils, also in removal of organic pigments and removal of polychlorinated biphenyls (PCBs) and it used in refining of mineral oils. [19,23]

Factors affecting adsorption

The extent of adsorption depends upon the following factors:

- Nature of adsorbate and adsorbent.

- The surface area of adsorbent.

- Activation of adsorbent.

- Experimental conditions. E.g., temperature, pressure, etc. [20]

Effects of Adsorption on the Nature of the Solid Surface

The resultant effect of surfactant adsorption on the surface character depends on the dominant mechanism of adsorption.

- For a highly charged surface:

- If ion exchange is dominant  electrical natural will not be altered significantly.

- If ion pairing is important  the zeta potential will decrease or even be neutralized. (The solubility of a dispersed system becomes worse).

- When the surface is neutralized by ion pairing of surfactant, the surfaces are hydrophobic, and it is possible for adsorption to continue by dispersion force interaction and leads to reverse of charge and instability.

- For water wetted surface, the adsorption of surfactant reduces the wet ability, and its interaction with non-polar phase (oil, air) is more favorable.

- Application example: froth flotation of mineral ore. [24]

Adsorption at the solid-vapor interface

- Solid characteristics are history-dependent. So, detailed discussion of adsorption onto solid surfaces must include knowledge of “historical” elements.

- Method for a material to reduce surface energy:

Liquid: Reducing the interfacial area (from spherical drop)

Solid: Adsorbing materials heterogeneous in the distribution or excess surface energy, so, the adsorption is not a uniform process. [20]

Isotherms

Adsorption is usually described through isotherms that is, the amount of adsorbate on the adsorbent as a function of its pressure (if gas) or concentration (if liquid) at constant temperature. The quantity adsorbed is nearly always normalized by the mass of the adsorbent to allow comparison of different materials.

Figure ‎3-3 : Basic Adsorption Isotherm.

From the graph, we can predict that after saturation pressure Ps, adsorption does not occur anymore. This can be explained by the fact that there are limited numbers of vacancies on the surface of the adsorbent. At high pressure a stage is reached when all the sites are occupied and further increase in pressure does not cause any difference in adsorption process. At high pressure, adsorption is independent of pressure. [26]

Types of adsorption isotherms

- Freundlich Adsorption Isotherm

Freundlich isotherm postulated base on surfaces that are heterogeneous. Its logarithmic form is expressed as equation(3-8-1):

Logqe=logKf+ 1n logCe		(3-8-1)

With the two constants symbolized as KF and n measuring the adsorption capacity of the adsorbent as well as how the model deviates from linearity, respectively. Generally n>1 suggests favorable adsorption of adsorbate on the adsorbent. The greater the value of n, the more sturdy the adsorption strength.

Temkin model was based on how indirect adsorbent/adsorbate interactions influence the adsorption isotherms. Its linear form is expressed as equation(3-8-2):

qe=  RTb ln A +   RTb ln Ce			(3-8-2)

Where= B (J/mol) and A (L/g) are Temkin constants, which are related to heat of sorption and maximum binding energy, respectively, R is the gas constant (8.31 J/ mol. K) and T (K) is the absolute temperature.

To compare the validity of each model, chi square (χ2) was incorporated since correlation coefficient (R2) may not justify the basis for selecting the best adsorption model because it only signifies the fit between linear forms of the isotherm equations and experimental data and while the suitability between experimental and predicted values of the adsorption capacity is described by chi square (χ2). The lower the χ2 value, the better the fit.

- Langmuir Adsorption Isotherm

Langmuir isotherm is one of the highly popular isotherms for the removal of organic pollutants by adsorption onto activated carbon. The model is explained by Equation (3-8-3)

qe=KLCa0Ce1+ KLCe			(3-8-3)

The isotherm constants associated with adsorption capacity and rate of adsorption were symbolized asQ0a(mg/g) and KL (L/mg) respectively. Equation (3-8-3)was expressed in five different linear forms, as tabulated in Table (3-1), with their major main disparities connected to the distribution of data as well as the parameter determination accuracy.

Table ‎3-1 : Langmuir forms.

| Isotherm | Linear form | Plot |
| --- | --- | --- |
| Langmuir (1) |  |  |
| Langmuir (2) |  |  |
| Langmuir (3) |  |  |
| Langmuir (4) |  |  |
| Langmuir (5) |  |  |

The term describing essential characteristics of the monolayer equation is referred to as dimensionless separation factor (RL), defined as equation (3-8-4)

RL= 11+ KLC0			(3-8-4)

With Co standing for the initial concentration. Unfavorable adsorption is described by RL>1, linear if RL = 1, favorable for 0, (0 <RL<1) as well as irreversible adsorption if RL = 0. [27]

- BET adsorption isotherm

BET equation which was developed for gas phase adsorption to liquid phase adsorption leads to ambiguous and erroneous results. Some cases of misuse of BET equation for liquid phase adsorption have been revisited. By close examination of the development of the classical equation, the causes of misunderstandings were elucidated and the suitable form of the BET equation for liquid phase adsorption was developed. As case studies, the classical form of the BET equation along with the correct form of the equation for liquid phase have been applied for modeling liquid phase adsorption of methyl tert butyl ether (MTBE) on perfluorooctyl alumina, phenol on activated carbon and pentachlorophenol on carbonized bark. It has been shown that direct application of the classical BET isotherm to liquid phase adsorption results in poor and erroneous estimation of the equation parameters.

For example, in aqueous phase adsorption of MTBE on perfluorooctyl alumina, the monolayer adsorption capacity of the adsorbent was calculated as 9.7 mg/g instead of 3.3 mg/g or the saturation concentration of MTBE in water was calculated as 1212 mg/L instead of 42000 mg/L. [28]

Kinetics of  isotherm

For pure gases, experimental physical adsorption isotherms have shapes that are classified into5 types as discussed below. Each of these types is observed in practice but by far the most common are types I, II and IV.

- Type I isotherm :

An inherent property of Type I isotherms is that adsorption is limited to the completion of a single monolayer of adsorbate at the adsorbent surface. Type I isotherms are observed for the adsorption of gases on micro porous solids whose pore sizes are not much larger than the molecular diameter of the adsorbate. Complete filling of these narrow pores corresponds to the completion of a molecular monolayer. An example is the adsorption of oxygen on carbon black at -183oC. Adsorption in all other types do not reach a limit corresponding to the completion of a monolayer.

Figure ‎3-4 : Monolayer adsorption type 1 isotherm.

- The above figure depicts Monolayer adsorption.

- This graph can be easily explained using Langmuir Adsorption Isotherm.

- If BET equation, when P/P0 << 1 and c >>1, then it leads to monolayer formation and Type I Adsorption Isotherm is obtained.

- Examples of Type-I adsorption are Adsorption of Nitrogen (N2) or Hydrogen (H) on charcoal.[29]

- Type II isotherms :

Do not exhibit saturation limit as did Type I. This type of isotherm indicates an indefinite multi-layer formation after completion of the monolayer and is found in adsorbents with a wide distribution of pore sizes. Near to the first point of inflexion (point A) a monolayer is completed, following which adsorption occurs in successive layers. An example is the adsorption of water vapor on carbon black at 30oC.

Figure ‎3-5 : Type II Adsorption isotherm.

- Type II Adsorption Isotherm shows large deviation from Langmuir model of adsorption.

- The intermediate flat region in the isotherm corresponds to monolayer formation.

- In BET equation, value of C has to be very large in comparison to 1.

- Examples of Type-II adsorption are Nitrogen (N2(g)) adsorbed on Iron (Fe) catalyst and Nitrogen (N2(g)) adsorbed on silica gel. [29]

- Type III isotherm:

Is obtained when the amount of gas adsorbed increases without limit as its relative saturation approaches unity. This type of isotherm is obtained when bromine is adsorbed on silica gel at 20oC.

Figure ‎3-6 : Type III Adsorption isotherm.

- Type III Adsorption Isotherm also shows large deviation from Langmuir model.

- In BET equation value if C <<< 1 Type III Adsorption Isotherm obtained.

- This isotherm explains the formation of multilayer.

- There is no flattish portion in the figure which indicates that monolayer formation is missing.

- Examples of Type III Adsorption Isotherm are Bromine (Br2) at 790°C on silica gel or Iodine (I2) at 790°C on silica gel. [29]

- Type IV isotherm:

Is a variation of Type II, but with a finite multi-layer formation corresponding to complete filling of the capillaries. The adsorption terminates near to a relative pressure of unity. This type of isotherm is obtained by the adsorption of water vapor on activated carbon at 30oC.

Figure ‎3-7: Type IV adsorption isotherm.

- At lower pressure region of figure is quite similar to Type II. This explains formation of monolayer followed by multilayer.

- The intermediate flat region in the isotherm corresponds to monolayer formation.

- The saturation level reaches at a pressure below the saturation vapor pressure. This can be explained on the basis of a possibility of gases getting condensed in the tiny capillary pores of adsorbent at pressure below the saturation pressure (PS) of the gas.

- Examples of Type IV Adsorption Isotherm are of adsorption of Benzene on Iron Oxide (Fe2O3) at 500°C and adsorption of Benzene on silica gel at 500°C. [29]

- Type V isotherm :

Is similar variation of Type III obtained when water vapor is adsorbed on activated carbon at 100oC. [26]

Figure ‎3-8 : Type V adsorption isotherm.

- Explanation of Type V figure is similar to Type IV.

- Example of Type V Adsorption Isotherm is adsorption of Water (vapors) at 1000°C on charcoal.

- Type IV and V shows phenomenon of capillary condensation of gas. [29]

Classification of Adsorption Isotherm

The phenomena involved in the process that should be considered in an adsorption model:

- Initial monomolecular adsorption: at low and high coverage.

- Multilayer adsorption.

- Chemisorptions,

- Capillary condensation. [30]

Different modes of operation

There are three modes of operation of adsorptions columns:

  - Batch Mode: In the case neither the solid nor the liquid flows. The rate of adsorption of solute, as controlled by external mass transfer is:

-∂C∂t= K*a*(C- C*)		(3-9-1)

Where C is the concentration of solute in the bulk liquid, C* is the concentration in equilibrium with the loading on the adsorbent, k is the external liquid phase mass transfer coefficient, is the external surface area of the adsorbent per unit volume of liquid.[31]

2. Continuous Mode: In this case both liquid and solids flow continuously through a perfectly mixed vessel. The above equation is converted to an algebraic equation because, as in a perfectly mixed reaction vessel (CSTR), the concentration, c, throughout the vessel, is equal to the exit (outlet) concentration, C out. Thus in terms of the residence time in the vessel:

Cf-Cout Tres=K*a*( C – C*)		(3-9-2)

[32]

Or Rearranging

Cout= Cf+(k*a* Tres *C)1+(K*a*Tres)		(3-9-4)

The Figure below (3-9) showed a typical plot of the ratio of outlet solute concentration to inlet solute concentration in the fluid as a function of time from the start of flow. The S-shaped curve is called the breakthrough curve.

Figure ‎3-9:Breakthrough curve.

Prior to tB, the outlet solute concentration is less than the maximum allowable of 0.05. At tB, this value is reached, and the adsorption step should be discontinued. If the adsorption step were to be continued for t > tB, the outlet solute concentration will rise rapidly, eventually approaching the inlet concentration as entire bed become saturated. The time required to each Cout/CF = 0.95 is designated tE.

The steepness of the breakthrough curve determines the extent to which the capacity of an adsorbent bed can be utilized. Thus, the shape of the curve is very important in determining the length of the adsorption bed. In actual practice, the steepness of the concentration profiles shown previously can increase or decrease, depending on the type of adsorption isotherm involved.

The Figure below showed that for the favorable isotherm of the Langmuir or Freundlich type, the high concentration regions move faster than the low concentration regions, and the wave front steepens with time until a constant pattern front is developed. [33]

Figure ‎3-10: Favorable isotherm of the Langmuir or Freundlich type.

3. Semi continuous Mode: In this case the adsorbent is retained in the vessel, but the feed liquid enters and exits the vessel at a fixed, continuous flow rate. Both concentration C and loading q vary with time. With perfect mixing, the outlet concentration is given by the above equation and c* is related to q in the suspension by an appropriate isotherm (c* = (qk) n). Combining all the above equations we get:

S  dqdt=K *a * ( Cout- C*) * Tres*Q		(3-9-5)

Where S is the batch mass adsorbent in the suspension and Q is the steady volumetric liquid flow rate. [34]

Literature Review

This chapter presents a critical review of various work done on the adsorption of Phenol by activated carbon, together with different theoretical models developed to understand the mechanism of the removal process. Various adsorbents are used for the adsorption having different characteristics such as particle diameter, pore diameter, surface area and adsorption capacities. Activated carbon obtained from different resources as hazelnut, eggshells, olive mill waste and coconut shell.

(Karabacakoğlu et.al. 2008) investigated the Removal of phenol from aqueous solution by adsorption using activated carbon. This study included the adsorption of phenol by activated carbon obtained from hazelnut bagasse activated with ZnCl2. Batch adsorption experiments were carried out at constant pH value under varying experimental conditions of contact time, phenol concentration, temperature and adsorbent dose. Adsorption equilibrium was reached within 300 min. Studies showed that the removal efficiency of phenol increased with increase in adsorbent dose and phenol concentration. Freundlich and Langmuir adsorption isotherms were applied to the experimental data, the adsorption capacities calculated from Langmuir equation were found to be 97.36, 91.32 and 99.27 mg/g for 25, 35 and 45 oC, respectively.

The adsorption kinetics were examined at three different phenol concentrations (300, 400 and 600 mg/L). The adsorption of phenol obeyed pseudo second order rate equation for all concentration range, the present study shows that the activated carbon derived from hazelnut bagasse can be used as low-cost adsorbent for adsorption of phenol. [35]

(Giraldoa et.al. 2014) investigated adsorption of phenol on activated carbons obtained from eggshells. Eggshell activated in inert atmosphere produces materials with a well-developed pore structure and high adsorption capacities. Making it possible to attain surface areas between (58-113 m2 g−1) and pore volumes between (0.54-0.63 0.97cm3 g−1). Activating eggshell membranes generate more solid superﬁcial areas. The same behavior was present for the development of porosity. The exothermic and spontaneous nature of adsorption process on the surface of all samples synthesized. The study revealed that this new adsorbent is inexpensive, indigenous, easily available material and has application for the removal of copper contained in industrial effluents. Finally, the four best-ﬁt three-parameter isotherms Sips, Toth, Radke–Prausnitz and Vieth–Sladek suggest that the sorption capacity of activated carbon of eggshell to uptake phenol is 192 mg/g. For the adsorption studies was applied from aqueous solution Freundlich models, Langmuir and Toth. The phenol adsorption was adjusted to the Langmuir model. The calorimetric results show this technique as promising to follow the adsorption from aqueous solution of such research. [36]

(Sihem et.al. 2012) Showed that cereal by-product, an abundant natural material, can be used effectively and efficiently for the removal of phenol from wastewater. In the work the elimination of phenol from synthesized aqueous solutions was carried out by adsorption onto non activated carbon obtained from calcinations up to 600°C in exclusion air of a local cereal by-product. The adsorption of phenol reached equilibrium in 120 minutes. The results indicate that adsorption capacity of the sorbent was considerably affected by initial phenol concentration, and PH. The adsorption isotherm was also examined where the results showed that at low concentrations, it is of type IV according to the BET (Brunauer, Deming and Teller) classification whereas at high values of concentration the process seemed to be of a multi-layer type.  The results showed that a high retention of the phenol exceeding 70% was achieved for an initial concentration of 20 mg/l, at 20°C, a mean size diameter of 0.1 mm, a mixing velocity of 600 rpm, an adsorbent concentration of  10 g /l, a pH=3  and contact time of 2 hours. [37]

(Arinjay Kumaret.al. 2007) studied the adsorption behavior of phenol and 4-nitrophenol on granular activated carbon from a basal salt medium (BSM) at pH ≈7.1 and temperature ≈30 ◦C, Based on maximum  deviations  and  correlation  coefficients,  Langmuir  gave  the  poorest  fit  for both compounds. Redlich–Peterson, Radke–Prausnitz, and four parameter model of Fritz–Schlunder could represent the data with similar accuracy, however, for phenol, two parameter model of Freundlich may be recommended because of ease in its Parameter estimation and better accuracy. 4-Nitrophenol was found to be more adsorbed than phenol.

The kinetics of the adsorption was found to be intra-particle diffusion controlled with diffusion coefficient values of the order of (10−13 m2/s). Three distinct phases of kinetics rapid, medium, and slow – have been observed in this study. [38]

(Abdelkreem 2013) explored the possibility of using olive mill waste to remove phenol from aqueous effluents.  The removal of phenol was investigated in both batch and continuous processes. Batch mode adsorption studies were performed by varying parameters such as operating time, initial phenol concentration, and solid to solution ratio. Column mode adsorption studies were performed by varying parameters such as initial phenol concentration, bed height, and volumetric flow rate. The rate of adsorption was observed to increase as the phenol initial concentration increases; the solid to solution ratio increases; bed height increases; and volumetric flow rate decreases. The well-known Freundlich, Langmuir, Temkin, and Dubinin-Radushkevich isotherm equations were applied for the equilibrium adsorption data and the isotherm parameters were evaluated. The Dubinin-Radushkevich (D-R) adsorption isotherm was found to have the best fit to the experimental data. The adsorption kinetics can be predicted by pseudo second-order kinetic. From the fixed bed investigations, as the flow rate is increased, the breakthrough curve becomes steeper. The break point time is obtained earlier and effluent phenol concentration ratio increases more rapidly. For smaller bed height, the effluent phenol concentration ratio increases more rapidly than for a higher bed height. The results indicate that olive mill waste can be used as adsorbent material for adsorption of phenol from aqueous solutions. [39]

(Kulkarnia 2013) demonstrated the removal of phenol from waste water in a fluidized bed column using coconut shell activated carbon as an adsorbent. Experimental results agree well with well-known Freundlich adsorption isotherm within 5 percent discrepancy. It is found from the study that percentage saturation increases with increase in initial concentration of phenol and flow rate. Particle size also found to affect the adsorption operation. The inlet concentration of phenol and flow rate has significant effect on the adsorption operation. It is observed that percent saturation decreases with increase in particle size. The flow rate of 4.2l pm yields maximum percent saturation of 46 percent. .In the study particle size of 0.420 mm is found more beneficial. [40]

Experiment work

The experimental work was carried out in series of steps as shown in Figure (5-1) :

Figure ‎5-1: The steps that was followed in this work.

Preparation of pyrolyzed carbon

We prepared a pyrolyzed carbon washed with water and another with HCl.

Preparation of  pyrolyzed carbon washed with HCl

- Heating: heat at a temperature of 600○C for 2hr (in BIFA LABORATORY FURNACES) to make sure the pyrolysis process is completed and to avoid the presence of impurities in it.

- Washing was done in three steps:

- Washing with de ionized water to remove fine powder then was dried (by  ari j. levy oven) at 100 ○C for 24 hr.

- Washing with 1 M HCl.

- Washing with de ionized water to removed residual of HCl.

- Drying: drying (in BIFA LABORATORY FURNACES) at a temperature of 600-700 ○C for 30-40 min.

- Finally, it was sieved into particular size of 4 mm<x<2 mm and 2mm<x<0.425 mm, the solid material obtained was stored in desiccators for use.

Preparation of  pyrolyzed carbon washed with water:

- Heating: heat at a temperature of 600○C for 2 hr (in BIFA LABORATORY FURNACES) to make sure the pyrolysis process is completed and to avoid the presence of  impurities in it.

- Washing: washing with de ionized water to remove fine powder then drying (by ari j. levy oven) at 100 ○C for 24 hr.

- Drying: drying (in BIFA LABORATORY FURNACES) at a temperature of 600-700 ○C for 30-40 min.

- Finally, it was sieved into particular size of (4<x<2) mm and (2<x<0.425) mm, the solid material obtained was stored in desiccators for use.

The activation

The activation process creates or increases porosity on the activated carbon surface as illustrated in Figure 5-2. There are two main activation process; chemical activation and physical activation, but in our project we did chemical activation with KOH for carbon washed with HCl with a particle size of 2mm < x < 0.425 mm.

Figure ‎5-2 : Two-dimensional representation of carbon activation.

    - Chemical activation with KOH

- It was dried (by in ari j. levy oven) at 100 ○C and was mixed with a solution of 1 M KOH (1:1 by weight).

- A sample of this mixture was heated in THERMOLYNE tube furnace  to 550 ○C (heating rate 5○C/min) for 120 min in an inert N2 atmosphere (flow rate 150 ml/min).

- The material was allowed to cool in the same atmosphere and was washed with de ionized water to remove the remaining KOH and any reaction products that might block the pores of the resulting activated carbon (AC-K).

- The AC-K was then washed by stirring with 5 M HCl for 12 hr. This suspension was then centrifuged (SiGmA 2-5) at 3900 rpm for 15 min before washing several times de ionized water; this step was repeated four times.

- The samples were finally dried in an oven (by ari j. levy oven) at 100 ○C for 3 days.

Phenol adsorption

Phenol preparation

- Phenol was prepared from liquid phenol (91 wt%), the phenolic solution was produced with different concentrations  (5, 10, 20, 30, 40, 50) ppm   .

- The water used for the preparation of the solutions of phenol was de ionized water.

Batch adsorption

Isotherm

- We put in contact 0.1 g of carbon with 10 ml of  the phenol solutions.

- Agitation at 100 rpm during 120 minutes at a temperature of 25 0C (in LabTech shaker).

- Equilibrium was assumed to have been reached after 120 min.

- Centrifuged (SiGmA 2-5) at 3900 rpm for 45 min then filtration of the solutions by Sartorius filter 0.45 Mm.

- Analysis the new solutions by Spectrophotometer (Lambda 25 UV/VIS Spectrometer ) directly after filtration.

- Determination of the adsorption capacity.

Kinetic

- The kinetic experiment was done by adding 250 ml (30 ppm) phenol solution and 0.5g of carbon, this solution was put in the shaker (in LabTech shaker) at 100 rpm and  25˚ C.

- A sample of 10 ml was taken every certain time for a period of approximately 3 days.

- The phenol samples filtration by Sartorius filter 0.45 Mm then the concentration  was measured by spectrophotometer (Lambda 25 UV/VIS Spectrometer ).

- The concentration and adsorption capacity is then calculated to have the calibration curve.

Surface area measurement

    - Acetic acid

We used acetic acid to estimate activated carbon surface area when the adsorption of the adsorbate leads to maximum single molecular layer when the adsorption was complete, then we calculated the area of the adsorbent that equal the total area of the adsorbed molecules.

- We prepared a series of acetic acid solution (0.5, 1, 1.5, 2) M.

- Then weighted 0.1 g of carbon.

- The 0.1 g of carbon was added to 10 ml of each solution

- Put the tubes in shaker (in LabTech shaker)  at 100 rpm and 25 ○C for 30 hrs.

- The solutions was Filtered (by Sartorius filter 0.45 Mm) and titrated with standard 0.1 M sodium hydroxide and phenolphthalein was used as indicator.

The number of moles of acid adsorbed per gram adsorbent is independent of chain length, the cross suction area Aa of straight-chain acid may be taken to be about 21×10-20m2. The specific area of adsorbent S (m2/g) is then given by:

S=Aa×Na×Ymax			 (2-6-5)

Where:

Na is Avogadro's number, Ymax the amount adsorbed when the surface is just covered with a monomolecular layer of the adsorbate.

Result and Discussion

Calibration Curve

In analytical chemistry, calibration curve is a plot that shows how the analytical signal of an analytical instrument changes with the concentration of an analyte. It is a general method used to determine the concentration of an unknown sample solution by comparing its absorbance to a set of standard samples of known concentrations. A series of concentrations in the range of expected concentrations of the analyte in the unknown solutions were prepared and their concentrations noted. Their absorbance were taken with the aid of a UV-Vis spectrophotometer and recorded. A plot of their absorbance was plotted against their concentrations which showed a linear relationship as shown in Figure (6-2).

Figure ‎6-1: Calibration Curve of phenol solution.

Using the calibration curve, the concentrations of the unknown solutions were extrapolated from the calibration curve after their response (absorbance) has been taken.

Equilibrium study

Adsorption isotherms are mathematical models that describe the distribution of the adsorbate species among liquid and adsorbent, based on a set of assumptions that are mainly related to the heterogeneity/homogeneity of adsorbents, the type of coverage and possibility of interaction between the adsorbate species. Adsorption data are usually described by adsorption isotherms, such as Langmuir, Freundlich and Temkin isotherms. These isotherms relate metal uptake per unit mass of adsorbent qe , to the equilibrium adsorbate concentration in the bulk fluid phase Ce.

The Langmuir isotherm

The Langmuir model  is based on the assumption that the maximum adsorption occurs when a saturated monolayer of solute molecules is present on the adsorbent surface, the energy of adsorption is constant and there is no migration of adsorbate molecules in the surface plane. The Langmuir isotherm is given by equations (6-2-1) and (6-2-2) :

1qe=1qm+1qm kL Ce                         (6-2-1)

OR

Ceqe=Ceqm+1qm kL                            (6-2-2)

where qm and KL are the Langmuir constants, representing the maximum adsorption capacity for the solid phase loading and the energy constant related to the heat of adsorption respectively. We have done the isotherm adsorption for carbon washed by water and HCl for two particles size and for activated carbon was washed with HCl of ( 0.425 – 2mm) particles size.

It can be seen from Figure (6-2) that the isotherm data for carbon of two particles size washed with water fits the Langmuir equation (6-2-1) well with R2 =0.999 for particle size (0.425 – 2 mm) and R2=0.979 for particle size (2 – 4 mm).

The values of qm and KL for particle size (0.425 – 2 mm) and particle size (2 – 4 mm) were determined from the figure,  qm found to be 1.889 mg/g and 1.7006 mg/g respectively and KL found to be 0.02085 L/mg and 0.1137 L/mg, respectively.

Figure ‎6-2: Langmuir Adsorption Isotherm for phenol adsorption on carbon washed by water for two particles size.

It can be seen from Figure (6-3) that the isotherm data for carbon of two particles size washed with HCl fits the Langmuir equation well with R2 =0.976 for particle size (0.425 – 2 mm) and R2= 0.983 for particle size (2 – 4 mm).

The values of qm and KL for particle size (0.425 – 2 mm) and particle size (2 – 4 mm) were determined from the figure,  qm found to be 3.937 mg/g and 3.597 mg/g respectively and KL found to be 0.8355 L/mg and 0.722 L/mg, respectively.

Figure ‎6-3: Langmuir Adsorption Isotherm for phenol adsorption on carbon washed by HCl for two particles size.

It can be seen from Figure (6-4) that the isotherm data for activated carbon that washed by HCl of (0.425 - 2 mm) particle size fits the Langmuir equation well with R2 =0.904. The values of qm and KL were determined from the figure found to be 4.281 mg/g and 0.911 L/mg, respectively.

Figure ‎6-4: Langmuir Adsorption Isotherm for phenol adsorption on activated carbon washed by HCl for particle size (0.425 – 2 mm).

The Freundlich isotherm

The Freundlich isotherm model is an empirical relationship describing the adsorption of solutes from a liquid to a solid surface and assumes that different sites with several adsorption energies are involved. Freundlich adsorption isotherm is the relationship between the amounts of nickel adsorbed per unit mass of adsorbent qe , and the concentration of the nickel at equilibrium Ce.

The logarithmic form of the Freundlich isotherm is given by equation (6-2-3):

Logqe=logKf+1nLogCe            (6-2-3)

where Kf and n are the Freundlich constants, the characteristics of the system. Kf and n are the indicators of the adsorption capacity and adsorption intensity, respectively.

Table ‎6-1 : Langmuir phenol adsorption and Freundlich phenol adsorption isotherm.

| Freundlich adsorption isotherm |  |  | Langmuir adsorption isotherm |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Kf(mg/g) | n | R2 | Kl(L/mg) | qm(mg/g) | R2 |  |
| 0.629 | 0.1798 | 0.979 | 0.02085 | 1.889 | 0.99 | Washed by water (0.425 – 2 mm) |
| 0.282 | 0.9057 | 0.937 | 0.1137 | 1.7006 | 0.979 | Washed by water (2 - 4 mm) |
| 1.566 | 2.653 | 0.618 | 0.8355 | 3.937 | 0.976 | Washed by HCl (0.425 - 2 mm) |
| 1.339 | 2.604 | 0.651 | 0.722 | 3.597 | 0.983 | Washed by HCl (2 - 4 mm) |
| 0.769 | 1.4023 | 0.863 | 0.911 | 4.281 | 0.957 | A.C (0.425 - 2 mm) |

From data showed in table (6-1), it was noticed that Langmuir adsorption isotherm model yields very good straight lines (correlation coefficient, R2 > 0.95) as compared to the Freundlich adsorption isotherm. The Langmuir adsorption isotherm constants Kl were in the range of 0.02085 to 0.911 L mg-1 and qm  were in the range of 1.7006 and 4.281 mg g-1.

As shown in figure (6-5) the amount of phenol adsorption for carbon of particle size (0.425 –2mm) is  greater than the amount of phenol adsorption for the particle size (2 - 4 mm), so the adsorption for small particles is better due to increase surface area.

Figure ‎6-5 : Effect of particles size on isotherm adsorption of phenol on carbon washed by water.

We can see from figure (6-6) the amount of phenol adsorption for carbon of particle size (2-0.425 mm) is  better than the amount of phenol adsorption for the particle size (4-2 mm), so the adsorption for small particles is better due to increase surface area.

Figure ‎6-6: Effect of particles size on isotherm adsorption of phenol on carbon washed by HCl.

When we compare between the amount of phenol adsorption on carbon for particle size (0.425 -2 mm) and for the particle size (2 - 4 mm) for carbon washed by water and HCl in figures (6-7 and 6-8), we see the washing solution has no effect on adsorption.

Figure ‎6-7: Effect of washed solution on isotherm adsorption of phenol for particle size of (2-0.425 mm).

Figure ‎6-8: Effect of washed solution on isotherm adsorption of phenol for particle size of  (2 - 4 mm).

By the activation , the amount of phenol adsorption for carbon of particle size (2-0.425 mm ) is better compared with the non activated carbon washed by HCL  and water, we can see that from figure (6-9).

Figure ‎6-9: Effect of washed solution on isotherm adsorption of phenol on carbon washed by HCl, water and A.C for particle size of (2-0.425 mm).

Kinetic  Study

In order to investigate the controlling mechanism of adsorption processes such as mass transfer and chemical reaction, the pseudo-first-order and pseudo-second order equations are applied to model the kinetics of phenol adsorption by activated carbon. The pseudo-first-order rate equation is as given in equation (6-3-1):

Logqe-qt= Logqe-Kad2.303t              (6-3-1)

where qt and qe are the amount adsorbed (mg/g) at time t, and at equilibrium respectively and kad is the rate constant of the pseudo-first-order adsorption process (min-1). Straight line plots of log(qe - qt) against t were used to determine the rate constant kad, and correlation coefficients, R2 for different phenol concentrations.

Pseudo second order equation can be given by equation (6-3-2):

tqt=1K2qe2+1qe t            (6-3-2)

Here, k2 is the rate constant of second order adsorption (g mg-1min-1). The plot t/qt versus t should give a straight line if pseudo-second-order kinetics is applicable and qe and kad can be determined from the slope and intercept of the plot, respectively. We have done the isotherm adsorption for carbon washed by water and HCl for two particles size and for activated carbon was washed with HCl of ( 0.425 – 2mm) particles size.

In figure (6-10) pseudo second order for carbon of two particles size washed by water fits the pseudo second order equation well with R2=0.998 for particle size (0.425 – 2 mm) and R2= 0.992 for particle size (2 – 4 mm).

The values of qe and Kad for particle size (0.425 – 2 mm) and particle size (2 – 4 mm) were determined from the figure,  qe found to be 7.634 mg/g and 7.194 mg/g respectively and Kad found to be 0.001978 g mg-1min-1 and 0.0006786 g mg-1min-1, respectively.

Figure ‎6-10: Pseudo second order for phenol adsorption on carbon washed by water for two particles size.

In figure (6-11) pseudo second order for carbon of two particles size washed by water fits the pseudo second order equation well with R2=0.994 for particle size (0.425 – 2 mm) and R2= 0.982 for particle size (2 – 4 mm).

The values of qe and Kad for particle size (0.425 – 2 mm) and particle size (2 – 4 mm) were determined from the figure,  qe found to be 8.0645 mg/g and 6.6667 mg/g respectively and Kad found to be 0.0007582 g mg-1min-1 and 0.0006878 g mg-1min-1, respectively.

Figure ‎6-11: Pseudo second order for Pseudo second order for phenol adsorption on carbon washed by HCl for two particles size.

It can be seen from Figure (6-12) that the pseudo second order for activated carbon washed by HCl of (2-0.425 mm) particle size fits  pseudo second order well with R2 =0.993. The values of qe and Kad were determined from the figure found to be 9.091 mg/g and 0.000587 g mg-1min-1, respectively.

Figure ‎6-12: Pseudo second order for phenol adsorption on activated carbon washed by HCl for particle size (0.425 – 2 mm).

Table ‎6-2: Pseudo first order and pseudo second order of phenol kinetic adsorption.

| Pseudo second order |  |  | pseudo-first-order |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| K2(g mg-1min-1) | qe(mg/g) | R2 | Kad(m-1) | qe(mg/g) | R2 |  |
| 0.001978 | 7.634 | 0.998 | 0 | 2.971 | 0.555 | Washed by water (0.425 - 2 mm) |
| 0.0006786 | 7.194 | 0.992 | 0.002303 | 6.6069 | 0.932 | Washed by water (2 - 4 mm) |
| 0.0007582 | 8.0645 | 0.994 | 0 | 4.742 | 0.706 | Washed by HCl (0.425 - 2 mm) |
| 0.0006878 | 6.6667 | 0.982 | 0 | 4.325 | 0.591 | Washed by HCl (2 - 4 mm) |
| 0.000587 | 9.091 | 0.993 | 0 | 5.445 | 0.717 | A.C (0.425 - 2 mm) |

From data showed in table (6-2), it was noticed that pseudo second order model yields very good straight lines (correlation coefficient, R2 > 0.98) as compared to the pseudo-first order. The pseudo-second-order rate constants were in the range of 0.000587 to 0.001978 g mg-1 min-1 and qe  were in the range of 6.6667 and 9.091 mg g-1.

We can see from figure (6-13 and 6-14), when the washing solution is constant and the particle size is varies the concentration of phenol after equilibrium for the particle size (0.425 - 2 mm) is  less than the concentration of phenol after equilibrium for the particle size (2 - 4 mm) for the same type of washing solution, which is means higher amount adsorption of phenol, so the adsorption for small particles is better due to increase surface area.

Figure ‎6-13: Effect of particles size on kinetic adsorption of phenol on carbon washed by water.

Figure ‎6-14: Effect of particles size on kinetic adsorption of phenol on carbon washed by HCl.

When we compare between the concentration of phenol after equilibrium for the particle size (2-0.425 mm) and for the particle size (4-2 mm) for carbon preparation by water and HCl in figures (6-15) and (6-16), find out that the equilibrium concentration in HCl is less than water in the two sizes, but in a small different which is means the washing solution has no effect on adsorption of phenol.

Figure ‎6-15: Effect of washed solution on kinetic adsorption of phenol for particle size of (2-0.425 mm).

Figure ‎6-16: Effect of washed solution on kinetic adsorption of phenol for particle size of (2 -4 mm).

By the activation, the concentration of phenol after equilibrium for the particle size (2-0.425 mm) is less compared with the non activated carbon prepared by HCL  and Water, which means higher amount of phenol adsorption by activated carbon because of high surface area, we can see that from figure (6-17).

Figure ‎6-17: Effect of washed solution on kinetic adsorption of phenol on carbon washed by HCl, water and A.C for particle size of (2-0.425 mm).

Surface area measurement

From our experimental data we find the isotherm adsorption of acetic acid is Freundlich isotherm and the adsorption is in a multilayer, because of that the surface area measurement is hard to predict by acetic acid. May be it can done by other method such as: Methylene blue number (MBN), gas adsorption or by surface area measurement devices:

- Sub sieve- sizer device.

- Blaine device.

- Friederich permeability device.

Conclusion

The adsorption of phenol from aqueous solution using activated carbon derived from the pyrolysis of waste tires was investigated. Results indicate that adsorption capacity was considerably affected by type of washing solution and particle size. Phenol adsorption increased with carbon washed by HCl solution and with the decrease of particle size of activated carbon. Phenol adsorption on the carbon washed by HCl is roughly the same of carbon washed by water, but the carbon washed by HCl has a slightly larger amount phenol adsorbed by carbon washed by water because the HCl is reaches deeper places in the pore which leads to an increase in the pore’s surface area.

Kinetic experiments carried out with different particle sizes showed that the smaller the particle size, the faster was the diffusion of phenol into adsorption sites of adsorbent. Kinetics results of phenol adsorption were examined using the pseudo-first-order, pseudo-second-order models. The results obtained show that the pseudo-second order model was the best to describe adsorption kinetic data for phenol. Equilibrium data were fitted to Langmuir and Freundlich isotherms and the best fit was given by the Langmuir isotherm model, the acetic acid adsorption was Freundlich isotherm so it is a multilayer adsorption which means the surface area measurement is very hard to measured. Thus indicates that activated carbon derived from the pyrolysis of waste tires is suitable to be used as an adsorbent material for adsorption of phenol from aqueous solution it may also be effective in removing other harmful species such as heavy metals.

Recommendations

- Ultimate analysis of carbon must be tested.

- The activation can be carried out by physical activation.

- At the activation process by tube furnace must use high temperature reaches to about 8500C, but in this project we used 550 oC  because the type of tube furnace ,that we have, can’t bear this high temperature.

- The surface area must be carried by surface area analyzer to measure the surface area instead of using acetic acid method.

Reference

- Li Li, Shuangxi Liu, Tan Zhu, Application of activated carbon derived from scrap tires for adsorption of Rhodamine B, Journal of Environmental Sciences 22(8) (2010) 1273–1280.

- F.A. López, T.A. Centeno, O. Rodríguez, and F.J. Alguacil, Preparation and characterization of activated carbon from the char produced in the thermolysis of granulated scrap tires, Journal of the Air & Waste Management Association, 63:5 (2013) 534-544.

- Lopez G., Olazar M., Artetxe M., Amutio M., Elordi G., Bilbao J., 2009b, Steam activation of pyrolytictyre char at different temperatures, Journal of Analytical and Applied Pyrolysis, 85, 539-543.

- Adrián Barroso Bogeat, María Alexandre Franco, Carmen Fernández González, and Vicente Gómez-Serrano, Activated carbon surface chemistry: Changes upon impregnation with Al (III), Fe (III) and Zn (II)-metal oxide catalyst precursors from NO3− aqueous solutions, Arabian Journal of Chemistry 2016.

- Prepared by the 37th JECFA (1990), published in FNP 52 (1992) superseding specifications prepared at the 31st JECFA (1987), and published in FNP 38 (1988). Metals and arsenic specifications reviewed at the 61st JECFA (2003). No ADI was established at the 31st JECFA (1987).

- Casmir E. Gimba, Odike Ocholi, Peter A. Egwaikhide, Turoti Muyiwa and Emmanuel E. Akporhonor, New raw material for activated carbon. I. Methylene blue adsorption on activated carbon prepared from Khayasenegalensis fruits, Cienciae Investigacion Agrria 36 (1) (2009)107-114.

- Ann Lemley, Linda Wagenet and Barbera Kneen, Activated Carbon Treatment of Drinking Water, Water Treatment NOTES, Fact sheet 3 December 1995.

- Teresa J. Bandosz, Activated carbon surfaces in environmental remediation, Chapter: Types of carbon adsorbents and their production, ELSEVIER, pp.1-48.

- Patil Pragya, Singh Sripal and Yenkie Maheshkumar, Preparation and Study of Properties of Activated Carbon Produced from Agricultural and Industrial Waste Shells, Research Journal of Chemical Sciences3(12) December (2013) 12-15.

- Alaa H. Jalil, Surface Area Determination of Activated Carbons Produced from Waste Tires Using Adsorption from Solution, Tikrit Journal of Pure Science 17 (2) (2012) 1813 - 1662 .

- Ahmad pour, D.D. Do, the preparation of active carbons from coal by physical activation, science Direct 34 (1996) 471-479.

- Dilek Cuhadaroglu and Oznur Aydemir Uygun, Production and characterization of activated carbon from a bituminous coal by chemical activation, African Journal of Biotechnology 7 (20) (2008) 3703-3710.

- Innovative Remediation Technologies:  Field Scale Demonstration Project in North America, 2nd Edition, Abstracts of Remediation Case Studies, Volume 4,  June, 2000, EPA 542-R-00-006.

- Shah, J.K., T.J. Schultz, and V.R. Daiga, 1989. "Pyrolysis Processes." Section 8.7 in Standard Handbook of Hazardous Waste Treatment and Disposal, ed. H.M. Freeman. McGraw-Hill Book Company, New York, NY.

- Nurulhuda Binti Amri, Preparation Of Activated Carbons From Waste Tires Char Impregnated With Potassium Hydroxide And Carbon Dioxide Gasification, Universiti Sains Malaysia (2008).

- David C. Sands, John L. Mcintyre, and Gerald S. Walton, Use of Activated Charcoal for the Removal of Patulin from Cider, Applied and Environmental Microbiology 32 (3) (1976) 388-391.

- Sustainable wastewater treatment of temporary events: the Dranouter Music Festival case study". Water Science and Technology 58 (8) (2008) 1653–7.

- Joana M. Dias, J.Rivera Utrilla and Manuel Almeida, ENVIRONMENTAL Management, waste materials for activated carbon, Pub Med 85 (2007) 833-846.

- Czepirski, L.; Balys, M. R.; Komorowska-Czepirska, "Some generalization of Langmuir adsorption isotherm". Internet Journal of Chemistry 3 (14) (2000) 1099-8292.

- S. Lata, P. K. Singh, S. R. Samadder, Regeneration of adsorbents and recovery of heavy metals: a review, International Journal of Environmental Science and Technology 12 (4) (April 2015) 1461-1478.

- WU Zhi-jian and LEE Kangtaek, Adsorption Mechanisms of Mesoporous Adsorbents in Solutions, Chem. Res. Chinese U. 2004 20 (2) (2004) 185-187.

- Guggenheim, E. A. and Adam, N. K., The thermodynamics of adsorption at the surface of solutions Proc. R. Soc. London, 139 (1933) 218–236.

- A. Da˛browski, Adsorption from theory to practice, Advances in Colloid and Interface Science 93 (2001) 135 -224.

- A K .Bajpai and M .rajpoot, adsorption techniques – A Review, Journal of scientific& industrial research 58 (1999) 844-860.

- Paul A. Webb, Introduction to Chemical Adsorption Analytical Techniques and their Applications to Catalysis, MIC Technical Publications, January 2003.

- Czepirski, L.; Balys, M. R.; Komorowska-Czepirska, "Some generalization of Langmuir adsorption isotherm". Internet Journal of Chemistry 3 (14) (2000) 1099-8292.

- Afidah Abdul Rahim, Zaharaddeen N. Garba, Efficient adsorption of 4-Chloroguiacol from aqueous solution using optimal activated carbon: Equilibrium isotherms and kinetics modeling, Journal of the Association of Arab Universities for Basic and Applied Sciences, Available online 29 November 2015.

- Amanollah Ebadi, Jafar S. Soltan Mohammad zadeh, Anvar Khudiev, What is the correct form of BET isotherm for modeling liquid phase adsorption?, Adsorption, 15(1) (February 2009) 65-73.

- Physical Chemistry - Peter Atkins, Julio dePaula, vlab.amrita.edu. (2011). Adsorption Isotherm.

- Charles H. Giles and David Smith, A General Treatment and Classification of the Solute Adsorption Isotherm, Department of Mathematics, University of Strathdyde, Glasgow G1, Scotland ,Received May 6, 1973 .

- B. Wayane Bequette, “Process Dynamics Modeling, Analysis and Simulation”, Prentice Hall PIR, New Jersey (1998).

- Donald R. Coughnowr, ”Process System Analysis and Control”, McGraw-Hill, Inc, International Edition (1991).

- George Stephanopoulos, “Chemical Process Control”, Prentice Hall of India Private Ltd, New Delhi (1990).

- William L. Luyben, ”Process Modeling Simulation and Control For Chemical Engineers”, McGraw-Hill International Editions (1990).

- Belgin Karabacakoğlu, Fatma Tümsek, Hakan Demiral and İlknur Demiral, Liquid Phase Adsorption of Phenol by Activated Carbon Derived From Hazelnut Bagasse, , J. Int. Environmental Application & Science, 3 (5) (2008) 373-380.

- Liliana Giraldo and Juan Carlos Moreno-Piraján, Study of adsorption of phenol on activated carbons obtained from eggshells, Journal of Analytical and Applied Pyrolysis 106 (2014) 41–47.

- Arris Sihem, Bencheikh Lehocine M and, Miniai H.A, Batch Adsorption of Phenol from Industrial Waste Water Using Cereal By-Products asa New Adsorbent. Energy Procedia 18 ( 2012 ) 1135 – 1144

- Arinjay Kumara, Shashi Kumara, Surendra Kumara and Dharam V. Guptab, Adsorption of phenol and 4-nitrophenol on granular activated carbon in basal salt medium: Equilibrium and kinetics, Journal of Hazardous Materials 147 (2007) 155–166.

- M. Abdelkreem, Adsorption of Phenol from Industrial Wastewater Using Olive Mill Waste, APCBEE Procedia5  ( 2013 )  349 – 357

- Sunil J.Kulkarni, Ravi W.Tapre, Suhas V. Patil, Mukesh B.Sawarkar, Adsorption of Phenol from Waste water in Fluidized Bed Using Coconut Shell Activated Carbon, Procedia Engineering 51 ( 2013 ) 300 – 307.

Appendix

| C(ppm) | Absorbance |
| --- | --- |
| 0 | 0 |
| 5 | 0.0633 |
| 10 | 0.1329 |
| 20 | 0.2834 |
| 30 | 0.4227 |
| 40 | 0.5606 |
| 50 | 0.73 |

Table 4: Calibration data of Phenol concentration.

| Ce (ppm) | C0(ppm) | Time(min) |
| --- | --- | --- |
| 30.647 | 30.679 | 0 |
| 27.82 | 30.679 | 5 |
| 27.548 | 30.679 | 15 |
| 26.718 | 30.679 | 30 |
| 24.231 | 30.679 | 50 |
| 23.192 | 30.679 | 80 |
| 21.87 | 30.679 | 110 |
| 19.308 | 30.679 | 150 |
| 18.752 | 30.679 | 190 |
| 18.032 | 30.679 | 250 |
| 17.667 | 30.679 | 370 |
| 17.425 | 30.679 | 500 |
| 17.349 | 30.679 | 800 |
| 16.883 | 30.679 | 1100 |
| 16.54 | 30.679 | 1300 |
| 16.133 | 30.679 | 1420 |
| 15.965 | 30.679 | 1600 |
| 15.869 | 30.679 | 1780 |
| 15.473 | 30.679 | 2950 |

Table 5: Kinetic adsorption phenol data adsorbed on carbon washed by water of (0.425 – 2 mm) particle size.

| Ce (ppm) | C0(ppm) | Time(min) |
| --- | --- | --- |
| 30.614 | 30.614 | 0 |
| 27.82 | 30.614 | 5 |
| 27.548 | 30.614 | 15 |
| 26.718 | 30.614 | 30 |
| 24.231 | 30.614 | 50 |
| 23.192 | 30.614 | 80 |
| 21.87 | 30.614 | 110 |
| 19.308 | 30.614 | 150 |
| 18.752 | 30.614 | 190 |
| 18.032 | 30.614 | 250 |
| 17.667 | 30.614 | 370 |
| 17.425 | 30.614 | 500 |
| 17.349 | 30.614 | 800 |
| 16.883 | 30.614 | 1100 |
| 16.54 | 30.614 | 1300 |
| 16.133 | 30.614 | 1420 |
| 15.965 | 30.614 | 1600 |
| 15.869 | 30.614 | 1780 |
| 15.473 | 30.614 | 2950 |

Table 6: Kinetic adsorption phenol data adsorbed on carbon washed by water of ( 2 – 4  mm) particle size.

| Ce (ppm) | C0(ppm) | Time(min) |
| --- | --- | --- |
| 30.825 | 30.825 | 0 |
| 30.415 | 30.825 | 5 |
| 29.169 | 30.825 | 15 |
| 27.798 | 30.825 | 30 |
| 27.531 | 30.825 | 50 |
| 25.346 | 30.825 | 80 |
| 24.314 | 30.825 | 110 |
| 23.277 | 30.825 | 150 |
| 22.836 | 30.825 | 190 |
| 21.761 | 30.825 | 250 |
| 19.262 | 30.825 | 370 |
| 18.454 | 30.825 | 500 |
| 17.792 | 30.825 | 800 |
| 17.629 | 30.825 | 1100 |
| 17.487 | 30.825 | 1300 |
| 16.742 | 30.825 | 1420 |
| 16.571 | 30.825 | 1600 |
| 15.665 | 30.825 | 1780 |
| 15.11 | 30.825 | 2950 |

Table 7: Kinetic adsorption phenol data adsorbed on carbon washed by HCl of ( 0.425 – 2  mm) particle size.

| Ce (ppm) | C0(ppm) | Time(min) |
| --- | --- | --- |
| 29.567 | 29.567 | 0 |
| 27.987 | 29.567 | 5 |
| 27.545 | 29.567 | 15 |
| 27.175 | 29.567 | 30 |
| 26.632 | 29.567 | 50 |
| 26.17 | 29.567 | 80 |
| 25.52 | 29.567 | 110 |
| 25.434 | 29.567 | 150 |
| 24.856 | 29.567 | 190 |
| 24.012 | 29.567 | 250 |
| 22.564 | 29.567 | 370 |
| 21.365 | 29.567 | 500 |
| 19.917 | 29.567 | 800 |
| 19.214 | 29.567 | 1100 |
| 18.562 | 29.567 | 1300 |
| 17.952 | 29.567 | 1420 |
| 17.306 | 29.567 | 1600 |
| 17.116 | 29.567 | 1780 |
| 17.043 | 29.567 | 2950 |

Table 8: Kinetic adsorption phenol data adsorbed on carbon washed by HCl of ( 2 – 4  mm)  particle size.

| Ce (ppm) | C0(ppm) | Time(min) |
| --- | --- | --- |
| 30.37 | 30.37 | 0 |
| 29.8 | 30.37 | 5 |
| 28.74 | 30.37 | 15 |
| 26.78 | 30.37 | 30 |
| 26.54 | 30.37 | 50 |
| 24.91 | 30.37 | 80 |
| 24.44 | 30.37 | 110 |
| 23.2 | 30.37 | 150 |
| 22.06 | 30.37 | 190 |
| 21.41 | 30.37 | 250 |
| 20.12 | 30.37 | 370 |
| 18.71 | 30.37 | 500 |
| 15.47 | 30.37 | 800 |
| 14.25 | 30.37 | 1100 |
| 14.9 | 30.37 | 1300 |
| 14.71 | 30.37 | 1420 |
| 14.53 | 30.37 | 1600 |
| 13.856 | 30.37 | 1780 |
| 13.156 | 30.37 | 2950 |

Table 9: Kinetic adsorption phenol data adsorbed on activated carbon washed by HCl of ( 0.425 – 2 mm) particle size.

| C0(ppm) | Ce(ppm) |
| --- | --- |
| 0 | 0 |
| 5 | 1.5482 |
| 10 | 2.426 |
| 20 | 3.944 |
| 30 | 5.1269 |
| 40 | 6.1646 |
| 50 | 7.6775 |

Table 10: Isotherm  adsorption phenol data adsorbed on carbon washed by water of (0.425 – 2 mm) particle size.

| C0(ppm) | Ce(ppm) |
| --- | --- |
| 0 | 0 |
| 5 | 1.258 |
| 10 | 2.468 |
| 20 | 4.67 |
| 30 | 7.0606 |
| 40 | 8.9089 |
| 50 | 10.2036 |

Table 11: Isotherm adsorption phenol data adsorbed on carbon washed by water of ( 2 – 4  mm) particle size.

| C0(ppm) | Ce(ppm) |
| --- | --- |
| 0 | 0 |
| 5 | 0.3349 |
| 10 | 0.3319 |
| 20 | 0.3409 |
| 30 | 1.562 |
| 40 | 8.251 |
| 50 | 12.944 |

Table 12: Isotherm  adsorption phenol data adsorbed on carbon washed by HCl of ( 0.425 – 2  mm) particle size.

| C0(ppm) | Ce(ppm) |
| --- | --- |
| 0 | 0 |
| 5 | 0.4004 |
| 10 | 0.4572 |
| 20 | 0.5296 |
| 30 | 2.44 |
| 40 | 10.185 |
| 50 | 16.28 |

Table 13: Isotherm  adsorption phenol data adsorbed on carbon washed by HCl of ( 2 – 4  mm)  particle size.

| C0(ppm) | Ce(ppm) |
| --- | --- |
| 0 | 0 |
| 5 | 1.362 |
| 10 | 1.654 |
| 20 | 4.28 |
| 30 | 4.475 |
| 40 | 6.615 |
| 50 | 9.242 |

Table 14: Isotherm  adsorption phenol data adsorbed on activated carbon washed by HCl of ( 0.425 – 2 mm) particle size.

| Ce(M) | VNaOH(ml0 | C0(M) |
| --- | --- | --- |
| 0 | 0 | 0 |
| 0.4 | 12 | 0.5 |
| 0.8 | 24 | 1 |
| 1.396667 | 41.9 | 1.5 |
| 1.876667 | 56.3 | 2 |

Table 15:  Acetic acid adsorption data adsorbed on carbon washed by water of ( 0.425 – 2 mm) particle size.

| Ce(M) | VNaOH(ml0 | C0(M) |
| --- | --- | --- |
| 0 | 0 | 0 |
| 0.466667 | 14 | 0.5 |
| 0.873333 | 26.2 | 1 |
| 1.466667 | 44 | 1.5 |
| 1.936667 | 58.1 | 2 |

Table 16: Acetic acid adsorption data adsorbed on carbon washed by water of ( 2 – 4 mm) particle size.

| Ce(M) | VNaOH(ml0 | C0(M) |
| --- | --- | --- |
| 0 | 0 | 0 |
| 0.32 | 9.6 | 0.5 |
| 0.756667 | 22.7 | 1 |
| 1.166667 | 35 | 1.5 |
| 1.406667 | 42.2 | 2 |

Table 17: Acetic acid adsorption data adsorbed on carbon washed by HCl of (0.425 – 2 mm) particle size.

| Ce(M) | VNaOH(ml0 | C0(M) |
| --- | --- | --- |
| 0 | 0 | 0 |
| 0.333333 | 10 | 0.5 |
| 0.78 | 23.4 | 1 |
| 1.313333 | 39.4 | 1.5 |
| 1.576667 | 47.3 | 2 |

Table 18: Acetic acid adsorption data adsorbed on carbon washed by HCl of ( 2 – 4 mm) particle size.

| Ce(M) | VNaOH(ml0 | C0(M) |
| --- | --- | --- |
| 0 | 0 | 0 |
| 0.233333 | 7 | 0.5 |
| 0.483333 | 14.5 | 1 |
| 0.533333 | 16 | 1.5 |
| 0.733333 | 22 | 2 |

Table 19: Acetic acid adsorption data adsorbed on activated carbon washed by HCl of ( 0.425 – 2 mm) particle size.