## Slide 1: An Najah N. University Faculty of Engineering Building Engineering Department
Graduation project 2
"The effect of adding waste materials to the concrete mixture"
Prepared by:
Sadeq Abu Al Haraden
Momen Khdeash
Supervisor : Dr. Mohammad Dwaikat
2011 / 2012

## Slide 2: Presentation Outlines
Introduction.
Objective.
Process.
Materials added.
Results.
Recommendations

## Slide 3: Introduction
In our life much of the material is destroyed and throw it in nature, if we took advantage of materials with the mixture of concrete and we saw the results that can happen there is a difference in the concrete, where we will see in this project the effect of some material on the concrete mix
The components of concrete are:
Cement.
Aggregate.
Sand.
Water.
Admixture.

## Slide 4: Objective
The main objective is:
• Developing a new unit construction material of high strength and a good quality.
By adding waste materials to concrete mixture.

## Slide 5: Materials added
1- Human Hair.
2- Glass.
3- CD’s.
4- Wood paneling
5- Hay.
6- Peat(olive extract).

## Slide 6
7-Coal ash.
8- Plastic.

## Slide 7: Process
To achieve strength of concrete equal 250 kg/cm2, we used a mixture of concrete contains of :
12% cement (2.6 kg).
30% sand(6.5 kg).
58% aggregate (12.5kg).
And the W/C is (0.5-0.7) and in this project used W/C = 0.65.
Bu using this components we got strength of concrete equal 242- 248 kg/cm2 after testing.
cubic (10x10x10)cm is used.

## Slide 8: Primary Results
Three problems in the preparation of concrete mixture,
the first problem mixture ratio of 1: 2: 3 (Cement, aggregate, sand),
The type of sand in the laboratory was not an appropriate,
The type of aggregate used in the first small batch size.

## Slide 9: Table shown the primary results
strength concrete (kN/cm2) | Sample
84 | Concrete Standard
did not give strength | Hay
86 | peat (olive extract)
94 | Ash
102 | Glass + ash
104 | human hair
124 | Glass

## Slide 10: The Results
Human hair is used:
20 grams gave concrete strength 263 kg/cm2.
15 grams gave concrete strength 257 kg/cm2.
10 grams gave concrete strength 251 kg/cm2.

## Slide 12: CD's
CD's is used:
4 CD’s are broken gave concrete strength 285 kg/cm2.
5 CD’s gave concrete strength 290 kg/cm2.

## Slide 14: Glass
150 g gave concrete strength 280 kg/cm2.
300 g gave concrete strength 310 kg/cm2.

## Slide 16: Coal Ash
100 g given concrete strength 264 kg/cm2.
150 g given concrete strength 270 kg/cm2.

## Slide 18: peat (olive extract):
100 g gave concrete strength 120 kg/cm2.
150 g gave concrete strength 100 kg/cm2.
200 g gave concrete strength 94 kg/cm2.
Concrete sample containing 100 g of peat (olive extract)

## Slide 20: Wood Paneling
Smooth :
50g gave concrete strength 77 kg/cm2.
100g gave concrete strength 45kg/cm2.
Strength of concrete Kg/cm2
Material added g
Chart: 
| 45 | 77
 | 50 | 100

## Slide 21: Wood Paneling
Rough :
50g gave concrete strength 84kg/cm2.
100g gave concrete strength 34kg/cm2.
Chart: 
| 34 | 84
 | 50 | 100
Strength of concrete Kg/cm2
Material added g

## Slide 22
Concrete sample with added straw (hay ground) 15 grams per cubic.
Concrete sample containing 150 grams of rough wood shavings

## Slide 23
Concrete samples containing 4 CD’s broken.
Concrete samples containing 75 g of glass and 150 g ash
Concrete samples containing 150 grams of powdered glass

## Slide 24
Concrete sample containing 2.6 kg cement and 6.5 kg of sand and 12.5 kg aggregate and the strength of concrete is 248kg/cm2

## Slide 25: Recommendations
There are a lot of human waste which is a barrier in the natural life, for example if we look at the size of the CD's damaged, we have exploited in the production concrete mixture, concrete will give us strength and a lower cost of concrete available in the market at the same quality. These materials are used in the experiments gave strength concrete terms will reduce the cost of concrete.

## Slide 26
Thank You
Thank You
SADEQ & MOEMEN