## Slide 1: An-Najah National University Faculty of Engineering & IT Mechanical Engineering Department
Prepared by
Waleed Najjar
Khaled Jawabreh
Jehad Shamlouli
Supervisor
Dr. Ahmad Al-Ramahi
2014-2015
Design and Fabrication Creep Testing Apparatus

## Slide 2
Outline
Introduction
Design
Manufacturing
Results.
Conclusion .

## Slide 3
Introduction
Creep Definition .
Creep Theory
Objectives of project

## Slide 4
Problem definition
The creep phenomena : is an important phenomena to be studied
This phenomena happens under high temperature and

## Slide 5
Objectives of project
the apparatus will be designed to test plastic specimens and study their creep behaviors under different types of loading and temperatures
In our project, the added value is the ability to perform creep test under different types of loading (tension ,torsion and combined load ),however ,in the literature most testing devices dedicated on one type of loading only .

## Slide 6
Creep Theory.
When designing a structural component that operation at high temperature for specified long time it's essential to obtain on the creep properties of this part, and also to determine the creep characteristics of this part the creep test or stress rupture test must be conducted to obtain on these properties and characteristics.
Creep test measure the amount of creep strain as a function of time to obtain the creep rate.

## Slide 7
Creep curve .
- Primary Creep .
- Secondary Creep .
- Tertiary Creep .

## Slide 9
The idea of CTA comes from the ASTM D1043.
This device used to determine the modulus of rigidity
Design of Creep Testing Apparatus (CTA)

## Slide 10
Graphical Design
Isometric View.
Sectional View.
Exploded View.
Bill Of Material (BOM ).

## Slide 11
Isometric View.
Sectional View.
Graphical Design

## Slide 12
Graphical Design
Other Views
(Front and Side View)

## Slide 13
ITEM NO. | PART NUMBER | QTY.
1 | Inside Column | 3
2 | Plate for Vertical Pulley | 2
3 | Vertical Pully | 1
4 | Deep GroovBall Bearing | 1
5 | Specimen | 1
6 | Axial Shaft | 1
7 | Mass stud | 1
8 | Fixing Column | 2
9 | Connecting Shaft Plate | 1
10 | NUT | 1
11 | Socket Set Screw | 2
12 | Socket Set Screw | 2
13 | Shaft of Bottom Chuck | 1
14 | Chuck | 2
15 | Grips | 1
16 | Upper Palte | 1
17 | Torsional Bearing Holder | 1
18 | Needle Bearing | 1
19 | Shaft of Upper Chuck | 1
20 | Hoeizantol Pully | 1
21 | Thrust Bearing | 1
22 | Vertical Pin | 1
23 | Frame of Axial Shaft | 1
24 | Linear Motion Ball Bearing | 2
25 | Internal Retaining Ring | 2
26 | Base | 1
27 | Flask | 2
28 | Plate for Flask | 2
29 | Heater | 1
30 | Lower Part of Table | 1
31 | Outside Column | 3
32 | Mufeh | 1
33 | Wheel of Machine | 4

## Slide 14
Specimen
The test specimen, is made from plastic
  High density Polyethylene (HD).
  Polypropylene.
  The Mechanical Proprieties of these material :
Specimen | Melting temperature °C | modules of elasticity Gpa | Ultimate tensile strength MPa | Elongation %
Polyethylene HD | 130-137 | 0.8 | 15 | 500
Polypropylene | 160-180 | 1.9 | 40 | 100

## Slide 15
Specimen
Specified dimensions of selected specimen on the CTA.
As shown in the dimension of the free length is selected to be 200mm, the remaining length is for the clamping of the specimen by two-30 mm for chucks.

## Slide 16
Fixing the Specimen
The Drill Chuck was used to Fix the specimen for different reasons:
  The Weight of the chucks (low)
  The Price of the chucks (low)

## Slide 17
Load on the Specimen
Pure Axial Load
Pure Torsional Load
Combined Load (Axial & Torsional)

## Slide 18
Load on the Specimen Pure Axial Load

## Slide 19
Load on the Specimen Pure Torsional Load
T
Fixed

## Slide 20
Load on the Specimen Combined Load
T
F

## Slide 21
Type of Applied Load
There are many types of forcing systems that can be used. However, in the CTA case the most practical way to applying the load is to use Dead Weight. Figure shown sample of dead weights.

## Slide 22
Bearing Design
In the CTA there are three types of bearing used:
  - Thrust Ball Bearing - Needle Roller Bearing.

## Slide 23
Bearing Design
In the CTA there are three types of bearing used:
  - Deep Groove Ball Bearing. - Linear Motion Ball Bearing.

## Slide 24
Flask
It is made from poly acrylic material. While acrylic softens at higher temperatures, it does not actually melt until it reaches 320 °F (160 °C),

## Slide 25
Heater
The heater is used to heat the water by conduction.
The capacity of the used heater was specified from the haters available in the market (2500 Watt).
It was needed to calculate the time required to heat the amount of required water as following.

## Slide 26
Heater
Energy required to increase the temperature of water by using the following equation:

## Slide 27
Energy losses from the side and the surface of the heater
=70-20= 50

## Slide 28
Electrical System
    Aurduino

## Slide 29
Electrical System
    Ultrasonic Ranging sensor
- This sensor was used to measure the axial deformation in the case of axial Load on the specimen.
- Ultrasonic ranging module HC - SR04 provides 2cm - 400cm non-contact measurement function.
- The ranging accuracy can reach to 3mm.
- The modules includes ultrasonic transmitters, receiver and control circuit.

## Slide 30
Electrical System
    Digital Thermometer
- This sensor was used to measure the temperature of the water and give the microcontroller the signs when its work before reach to the desired temperature, and when it’s stop after achieve the desired temperature.
It has an operating temperature range of -55°C to +125°C
it is accurate to ±0.5°C, over the range of -10°C to +85°C

## Slide 31
Electrical System
    Keypad
- Used to enter the value of the required temperature, this process will be achieved by microcontroller that received the input required value and give a command to the heater to work until to reach the specified temperature.

## Slide 32
Electrical System
    LCD Screen
This screen was used to give the value of the running temperature, the value of the axial deformation that comes from the ultra-sonic sensor, and the value of the angular deflection that comes from potentiometer.

## Slide 33
Manufacturing and Assembly of CTA
The manufacturing process to each part can’t be explained because there is no enough time to that ,
Assembly process is explained by using SolidWorks program.

## Slide 34
Manufacturing and Assembly of CTA
We used different joining and assembling process to achieve the assembly process parts together as following:

## Slide 35
Load
a- The fixed column was joined with lower plate by welding process

## Slide 36
Load
b- The wheel was joined with lower plate by welding process

## Slide 37
Load
c- The Flask part was joined together

## Slide 38
Load
d- The flask was joined with lower plate after that the heater was joined

## Slide 39
Load
e- The needle bearing was joined with torsional shaft holder while the linear motion bearing was joined with axial shaft holder

## Slide 40
Load
f- The torsional shaft holder and the axial shaft holder was joined with upper plate

## Slide 41
Load
g- Horizontal pulley was joined with the shaft

## Slide 42
Load
g- The shaft was joined with the chuck and the pin was used to prevent pulley motion

## Slide 43
Load
g- The shaft was joined with the chuck and the the pin was used to prevent pulley motion

## Slide 44
Load
h- The upper plate was joined with the sliding column

## Slide 45
Load
i- Axial shaft and it’s components

## Slide 46
Load
j- Axial shaft was connected with upper part

## Slide 47
Load
k- Upper part connected with lower part

## Slide 48
Load
l- Vertical pulley was connected as shown

## Slide 50
Results & Discussion
Pure Torsional load .
T: applied torque on specimen (N.mm).
F: the applied dead weight (N)
R: radius of the horizontal pulley (mm)
→

## Slide 51
Results & Discussion

## Slide 52
Results & Discussion

## Slide 53
Results & Discussion

## Slide 54
Results & Discussion
Chart: Time(min)

## Slide 55
Results & Discussion
Chart: Time(min)

## Slide 56
Results & Discussion
Results for pure axial load experiment :

## Slide 57
Results & Discussion

## Slide 58
Results & Discussion
Combined Load Test
There is no enough time to achieve this type of test.

## Slide 59
Results & Conclusion

## Slide 61
Conclusion
We were hope getting the best results through our project but we encountered some problems that we talked about previously ,we solved some of these but other did not solve.