## Slide 1: An-Najah National University Chemical Engineering Department Graduation Project(2) Recycling and Rreinforcing of PP from White Board Markers Prepared by: Fedaa Jitawi Hidaya Shaker Ismaiel Manasrah Mays Shadeed Supervisor: Eng. Shadi Sawalha 2011

## Slide 2: Presentation Topics
Problem
Objectives
Introduction
Methodology
Result and Discussion
Conclusion and Recommendation

## Slide 3: Problem
The problem comes from highly amount of consumed white board markers inside educational centres. These markers occupied large volume because they are not biodegradable due to their nature.

## Slide 4: Objectives
Recycling of White Board Markers and use its constituents as composite component in order to produce a stronger polymer which could be used in other applications.

## Slide 5: Introduction

## Slide 6: White Board Markers
PP
PET
HDPE

## Slide 7: Composite
Fiber composite technology is based on taking advantage of the high strength and high stiffness of fibers, which are combined with matrix materials of similar/ dissimilar natures in various ways, creating inevitable interfaces.
Most composites have two constituent materials: a binder or matrix, and reinforcement.
The reinforcement is usually much stronger and stiffer than the matrix, and gives the composite its good properties.

## Slide 8: Composite
Factors affect the composite strength:
Interfacial bonding
Influence of Fiber Length
Influence of Fiber Orientation
Reinforcements basically come in three forms: particulate, discontinuous fiber, and continuous fiber.

## Slide 9: Glass Fiber
Glass Fiber-reinforced Plastic (GFRP), is a fiber reinforced polymer made of a plastic matrix reinforced by fine fibers made of glass.
Glass fibers reinforced polymer matrix composites are manufactured by open mold processes, closed mold processes and Pultrusion method.
Properties of glass fiber:
High strength-to-weight ratio.
High modulus of elasticity-to-weight ratio.
Good corrosion resistance.
Good insulating properties.
Low thermal resistance.
But it is weak in compression.

## Slide 10: Methodology

## Slide 11
Information collection
Raw material collection
Statistical survey.
questionnaire
Material type determination
Methodology
Statistical survey.
questionnaire
University decision for WBM collection
DSC test was performed to every part of the marker

## Slide 12: Methodology
Raw material preparation
processing
Using thermal press
Testing and Analysis
Using tensile test
Cleaning
grinding
Produce 6 of reinforced sheet
Modulus of elasticity, tensile strength and Ke were calculated
Sorting
Using tensile test
Modulus of elasticity, tensile strength and KE were calculated
  Using thermal press
Produce 6 series of reinforced sheet
  Using tensile test
Sorting
Cleaning
Grinding
  Modulus of

## Slide 13: Result and Discussion

## Slide 14
Statistical Survey
The number of the markers
38810
Weight (Kg)
670

## Slide 15: DSC Test Results

## Slide 16
Body, cap , and plug samples
Figure (2): The DSC test result for the body of the white board marker.

## Slide 17
Holder sample
Figure (3): The DSC test result for the fibre holder of the white board marker.

## Slide 18
Fibers sample
Figure (4): The DSC test result for the fibers of the white board marker.

## Slide 19: Tensile Test Results

## Slide 20: Polypropylene and glass fiber composite at different composition
Chart: Wt%
| 0 | 5 | 10 | 15 | 20 | 25 | 30
modulus | 445.9 | 831.5 | 900.6667 | 1058 | 761.33 | 623 | 559.75
Chart: Wt%
| 0 | 5 | 10 | 15 | 20 | 25 | 30
yield strength | 20.53 | 25 | 28.3 | 32.301 | 32 | 31.69 | 29.167
Figure (5): Relationship between modulus of elasticity and yield strength with glass fiber content at constant temperature 220˚C.

## Slide 21: Polypropylene and glass fiber composite at different composition
Chart: Wt%
| 5 | 10 | 15 | 20 | 25 | 30
Gc | 0.19157 | 0.12188 | 0.11808 | 0.037548 | 0.012792 | 0.0052665
Figure (6): Relationship between ke versus weight percent of glass fiber

## Slide 22: Polypropylene and glass fiber composite at different temperature
Chart: Temperature (˚C)
| 200 | 220 | 240 | 260 | 280 | 300
modulus | 557.5 | 900.6667 | 461.6168 | 403.7978 | 402.9167 | 332.8317
Chart: Temperature (˚C)
| 200 | 220 | 240 | 260 | 280 | 300
Yield strength | 17.7752 | 28.3 | 20.6804 | 22.9157 | 23.5675 | 23.0803
Figure (7): Relationship between modulus of elasticity and yield strength with temperature at constant composition 10 wt% glass fiber.

## Slide 23: Polypropylene (PP) and Recycled polyethylene teraphthalate fibers (rPETFs) composite at different composition.
Chart: Wt%
| 2 | 4 | 6 | 8 | 10 | 15 | 20 | 25
PET | 665.107 | 737.864 | 793.432 | 842.25 | 863.248 | 848.735 | 769.2287 | 595.9061
Chart: Wt%
| 2 | 4 | 6 | 8 | 10 | 15 | 20 | 25
PET | 16.8781 | 22.3215 | 22.5403 | 28.0696 | 28.4846 | 22.6188 | 23.623 | 19.2611
Figure (8): Relationship between modulus of elasticity and yield strength with weight percentage of PET fiber at constant temperature 220˚C.

## Slide 24: Polypropylene (PP) and Recycled polyethylene teraphthalate fibers (rPETFs) composite at different composition
Chart: Wt%
| 2 | 4 | 6 | 8 | 10 | 15 | 20 | 25
Pet c | 0.97075 | 0.93648 | 0.85887 | 0.79989 | 0.70248 | 0.47469 | 0.29198 | 0.10532
Figure (9): Relationship between Ke versus weight percent of PET fibre

## Slide 25: Polypropylene (PP) and Recycled poly ethylene terephthalate fibers (rPETF) composite at different temperature.
Chart: Temperature (˚C)
| 200 | 220 | 240 | 260 | 280 | 300
modulus | 548.3119 | 911.9395 | 485.347 | 433.9174 | 790.5564 | 464.6704
Chart: Temperature (˚C)
| 200 | 220 | 240 | 260 | 280 | 300
yield strength | 27.0687 | 30.0514 | 25.4 | 19.3041 | 22.0633 | 18.4377
Figure (10): Relationship between modulus of elasticity and temperature at constant composition 8wt% PET fiber.

## Slide 26: Comparison between glass fiber/PP composite and rPETf/PP composite
Figure (11): Comparison between the modulus of elasticity tensile strength of glass fibre/PP composite and rPETf/ PP.
Chart: Wt%
| 0 | 5 | 10 | 15 | 20 | 25 | 30
Glass fiber | 445.9 | 831.5 | 900.6667 | 1058 | 761.33 | 623 | 559.75
PET | 445.9 | 665.107 | 737.864 | 793.432 | 842.25 | 863.248 | 848.735 | 769.2287 | 595.9061
Chart: Wt%
| 0 | 5 | 10 | 15 | 20 | 25 | 30
Glass fiber | 20.53 | 25 | 28.3 | 32.301 | 32 | 31.69 | 29.167
PET | 20.53 | 16.8781 | 22.3215 | 22.5403 | 28.0696 | 28.4846 | 22.6188 | 23.623 | 19.2611

## Slide 27
Chart: Wt%
| 2 | 4 | 6 | 8
modulus | 1045.8 | 1310.3333 | 1256.6667 | 674
Chart: Wt%
| 2 | 4 | 6 | 8
yeild strength | 25.55 | 34.85 | 26.818 | 17.5 | 26.36
Figure (12): Relationship between yield strength and weight percent of PET composite with 10wt% of glass fiber and PP at 220˚C.
Three composite component (rPETFs and PP)/GF at different composition

## Slide 28
Chart: Temperature (˚C)
| 200 | 220 | 240 | 260 | 280 | 300
modulus | 677.0585 | 733.01 | 762.29 | 786.8106 | 829.8404 | 741.7256
Chart: Temperature (˚C)
| 200 | 220 | 240 | 260 | 280 | 300
Yield strength | 26.0118 | 26.9176 | 29.1162 | 36.8878 | 41.998 | 34.3333
Figure(13): Relationship between modulus of elasticity and weight percentage of PET fiber at constant temperature 220˚C.
Glass fibre (mat) and Polypropylene composite at different temperature.

## Slide 29: Conclusion
The PP content is 66% from the hole marker
The optimum GF composition in r-PP/GF was 15% at processing temperature of 220 (˚C).
The material of WBM consist of PP ,HDPE, and PET fibers

## Slide 30
The optimum composition of rPETFs in Composite of r-PP/rPETFs is 10%, at temperature of 220 (˚C)
The optimum processing temperature for r-PP/GF (E-class mat) composite is 280 (˚C)
The optimum compositions of rPETFs and short GF where 4% and 10% respectively in rPETFs and GF/r-PP composite at processing temperature 220 (˚C).

## Slide 31: Problem objective
The problem is the high amount of consumed white board markers
The objective is to recycle these markers and to produce a new product by composite .
A three component composite 4%PET and 10%GF

## Slide 32: Thank You For Coming And Listening Any Question?

## Slide 33
1
2
Polypropylene (PP) and Recycled poly ethylene terephthalate fibers (rPETF) composite at different temperature.
5
Glass fibre (mat) and Polypropylene composite at different temperature.
Polypropylene and glass fiber composite at different composition
4
3
6
Three composite component (rPETFs and PP)/GF at different composition
Polypropylene (PP) and Recycled polyethylene teraphthalate fibers (rPETFs) composite at different composition.
Polypropylene and glass fiber composite at different temperature

## Slide 34: Polypropylene (PP):
PP is a versatile polymer used in applications from films to fibers.
PP is synthesized by the polymerization of propylene, a monomer derived from petroleum products.
With a density of 0.905 g/cm3.
The melting temperature is 165 to 170˚C.

## Slide 35: Polyester (PETF):
Resin is used in several key products; a large part of the polyester is converted into fibers
Condensation polymer made from terephthalic acid and ethylene glycol.
Density :1.3-1.4 gm\cm3.
Melting temperature: 212-265 ˚C.

## Slide 36: High density polyethylene (HDPE):
High-density polyethylene has the simplest structure and is essentially made of long virtually unbranched chains of polymer.
PE is synthesized by the polymerization of ethylene, a monomer derived from petroleum products.
With density in the range of 0.941–0.965 g/cm3).
The melting temperature 130˚C.

## Slide 37
Figure (13): Comparison between the modulus of elasticity tensile strength of glass fibre/PP composite and rPETFs/ PP.
Comparison between glass fiber/PP composite and rPETFs/PP composite

## Slide 38
Chart: Temperature (˚C)
| 200 | 220 | 240 | 260 | 280 | 300
modulus | 557.5 | 900.6667 | 461.6168 | 403.7978 | 402.9167 | 332.8317
Polypropylene and glass fiber(10wt% glass fiber) composite at different temperature
Chart: Temperature (˚C)
| 200 | 220 | 240 | 260 | 280 | 300
Yield strength | 17.7752 | 28.3 | 20.6804 | 22.9157 | 23.5675 | 23.0803
Figure (7): Relationship between modulus of elasticity and yield strength with temperature at constant composition 10 wt% glass fiber.

## Slide 39
Figure (4): The DSC test result for the fibers of the white board marker.