## Slide 1
Graduation Project 2
Prepared by Abdullah aghbar Ameer Hendiya Mahmoud Ziad
Supervisors: Dr. Osayd Abdul Fattah
The Effect of Adding Pyrolysis Carbon Black On Concrete At Different Particle Size

## Slide 2
Agenda - Objective. - Introduction. - Material. - Experimental Work. - Methodology. - Conclusion. - Recommendation.

## Slide 3
Objective We are continuing the work done by Ayman Nassar, under Dr. Osayd Abdul Fattah supervisor which is the effect on mechanical properties of concrete when pyrolysis carbon black is added but we focused on the adding of particle size.

## Slide 4
Concrete:
Concrete is the most widely used in construction material in the world. It is obtained by mixing cementitious materials, water and aggregates in required proportions.
Introduction

## Slide 5
Concrete consists of

## Slide 6
Concrete admixture
Additives are used in concrete for several purposes are (plasticizers, retarders, accelerators, Shrinkage-reducing and air entraining agents).

## Slide 7
Concrete Additives

## Slide 8
Advantage of concrete
1. Concrete components are easily available. 2. Concrete is free of defects unlike natural stones. 3. Concrete strength can be controlled with economy. 4. The durability of concrete is very high. 5. Easy to form concrete for the desired shape.

## Slide 9
Dis advantage of concrete 1. The tensile strength of the concrete is low. 2. Concrete is high brittle. 3. Its weight is high compared to its strength. 4. Concrete contains soluble salts which affect their properties. 5. Concrete contains pores.

## Slide 10
Pyrolysis carbon black:
Waste tire is one of the most important problems that face many countries in the world, especially with the growth of the auto-related industries.
Carbon black produce from waste tire by pyrolysis.

## Slide 11
Pyrolysis is produce

## Slide 13
Experimental Work Program
Materials:
1.Cement: Cement acts mostly as a binding agent between coarse aggregate (gravel), fine aggregate (sand) and provides strength to concrete on setting and hardening

## Slide 14
3. Aggregate: Is coarse aggregates increases the crushing strength of concrete, makes concrete solid hard mass, reduce cost of concrete by occupying major volume in concrete.
2. Sand: Is fine aggregate reduces shrinkage and cracking, fills voids present in coarse aggregates and helps in hardening of cement

## Slide 15
4.Water: Its act as one of the component in concrete mix for reaction with cement which result in hard cement after drying, but increase water to cement ratio reduce concrete strength. Water to cement ratio is 50%
Note: High w/c ratio due to reduce strength of concrete.
5.Super G7: is a plasticizers substance which can be added to concrete to increase the workability of concrete when mixing concrete ingredients together
Super cement ratio is 2%

## Slide 16
6. PCB

## Slide 17
Instruments and characterizations

## Slide 18
Methodology
In order for the concrete to be designed, the type has to be identified along with the properties, proportions involved in the preparation of the concrete and those things the typical standard normally used in buildings in the market of Palestine.
Mix 1Kg Cement, 2.3Kg Sand, 4.03Kg Aggregate
40g PCB and B300 type of concrete.
And we will have 3 type of tests :

## Slide 19
Compression Test

## Slide 20
Water Adsorption Test

## Slide 21
Slump Test

## Slide 22: Results : 1- Compression Test Compression Test at 7 days
Ratio PCB% | Age (Days) | Weight (gm) | Density (g/ | Compression Test (KN) | Pressure MPa | Pressure (Kg/c
0% | 7 | 2379 | 2.379 | 212 | 21.2 | 216.2
4% Random | 7 | 2369 | 2.369 | 284.6 | 28.4 | 290.3
4% at 600 µm | 7 | 2407.6 | 2.407 | 297.3 | 29.7 | 303.2
4% at 300µm | 7 | 2454.3 | 2.454 | 236.6 | 23.6 | 241.3
4% at 150µm | 7 | 2383 | 2.383 | 246 | 24.6 | 250.8
4% at 75µm | 7 | 2417.3 | 2.417 | 263.3 | 26.3 | 268.5
Ratio PCB% | Age (Days) | Weight (gm) |  | Compression Test (KN) | Pressure MPa | 
0% | 7 | 2379 | 2.379 | 212 | 21.2 | 216.2
4% Random | 7 | 2369 | 2.369 | 284.6 | 28.4 | 290.3
4% at 600 µm | 7 | 2407.6 | 2.407 | 297.3 | 29.7 | 303.2
4% at 300µm | 7 | 2454.3 | 2.454 | 236.6 | 23.6 | 241.3
4% at 150µm | 7 | 2383 | 2.383 | 246 | 24.6 | 250.8
4% at 75µm | 7 | 2417.3 | 2.417 | 263.3 | 26.3 | 268.5

## Slide 23
Chart: Compression Test At 7 days
| 0% | 4% Random | 600 µm | 300 µm | 150 µm | 75 µm
 | 21.2 | 28.4 | 29.7 | 23.6 | 24.6 | 26.3
Compression Test at 7 days Continue ..

## Slide 24
Error for Compression Test at 7 days
Ratio PCB% | Error%
0% | ± 2.83
4% Random | ± 2.455
4% at 600 µm | ± 1.68
4% at 300µm | ± 2.535
4% at 150µm | ± 1.12
4% at 75µm | ± 3.795

## Slide 25
Error for Compression Test at 7 days Continue ..
Chart: Error at 7 days
| 0% | 4% Random | 600 µm | 300 µm | 150 µm | 75 µm
 | 2.83 | 2.455 | 1.68 | 2.535 | 1.12 | 3.795

## Slide 26
Compression Test at 28 days
Ratio PCB% | Age (Days) | Weight (gm) | Density (g/ | Compression Test (KN) | Pressure MPa | Pressure (Kg/c
0% | 28 | 2395.6 | 2.3956 | 295.3 | 29.5 | 301.1
4% Random | 28 | 2392.6 | 2.3926 | 341.3 | 34.1 | 348.1
4% at 600 µm | 28 | 2494.3 | 2.4943 | 354.6 | 35.4 | 361.6
4% at 300µm | 28 | 2251.6 | 2.2516 | 376.6 | 37.6 | 384.1
4% at 150µm | 28 | 2374 | 2.374 | 405.3 | 40.5 | 413.3
4% at 75µm | 28 | 2421.3 | 2.4213 | 424 | 42.4 | 432.3
Ratio PCB% | Age (Days) | Weight (gm) |  | Compression Test (KN) | Pressure MPa | 
0% | 28 | 2395.6 | 2.3956 | 295.3 | 29.5 | 301.1
4% Random | 28 | 2392.6 | 2.3926 | 341.3 | 34.1 | 348.1
4% at 600 µm | 28 | 2494.3 | 2.4943 | 354.6 | 35.4 | 361.6
4% at 300µm | 28 | 2251.6 | 2.2516 | 376.6 | 37.6 | 384.1
4% at 150µm | 28 | 2374 | 2.374 | 405.3 | 40.5 | 413.3
4% at 75µm | 28 | 2421.3 | 2.4213 | 424 | 42.4 | 432.3

## Slide 27
Compression Test at 28 days Continue ..
Chart: Compression Test At 28 days
| 0% | 4% Random | 600 µm | 300 µm | 150 µm | 75 µm
 | 29.5 | 34.1 | 35.4 | 37.6 | 40.5 | 42.4

## Slide 28
Error for Compression Test at 28 days
Ratio PCB % | Error %
0% | ± 3.385
4% Random | ± 1.755
4% at 600 µm | ± 1.97
4% at 300µm | ± 2.65
4% at 150µm | ± 1.97
4% at 75µm | ± 2.12

## Slide 29
Error for Compression Test at 28 days Continue..
Chart: Error at 28 days
| 0% | 4% Random | 600 µm | 300 µm | 150 µm | 75 µm
 | 3.385 | 1.755 | 1.97 | 2.65 | 1.97 | 2.12

## Slide 30
Water Adsorption (%) | Average Weight concrete Dry (gm) | Average Weight concrete Wet (gm) | Ratio PCB%
6.01 | 2251.221 | 2386.354 | 0
4.83 | 2326.333 | 2439.453 | 4% Random
4.89 | 2319.748 | 2433.765 | 4% at 600 µm
4.78 | 2179.519 | 2284.534 | 4% at 300µm
4.46 | 2256.983 | 2357.618 | 4% at 150µm
4.14 | 2262.158 | 2355.124 | 4% at 75µm
2- Water Adsorption Test

## Slide 31
Chart: Water Adsorption
| 0 | 4% Random | 600 µm | 300µm | 150µm | 75µm
 | 6.01 | 4.83 | 4.89 | 4.78 | 4.46 | 4.14
Water Adsorption test Continue ..

## Slide 32
3- Slump Test
Slump (cm) | 4% PCB at different particle size
4.3 | 0
6.7 | 4% Random
5.1 | 75 µm
6.4 | 150 µm
7.3 | 300 µm
7.9 | 600 µm

## Slide 33
Slump Test Continue ...
Chart: Slump Test
| 0 | 4% Random | 75 µm | 150 µm | 300 µm | 600 µm
 | 4.3 | 6.7 | 5.1 | 6.4 | 7.3 | 7.9

## Slide 34
Slump Test Continue ...
Placing Conditions | Blinding concert; Shallow sections; Pavement using pavers | Mass concrete; Lightly reinforced Sections in slab, beams, walls, columns, floor | Heavily reinforced, sections in slab, beams, walls, columns; Slipform work; pumped concrete | Trench fill; in site piling | Termite concrete
Degree of workability | Very low | Low | Medium | high | Very high
Slump (mm) | <25 | 25 – 75 | 50 - 100 | 75 – 100 | 100 – 150

## Slide 35
Conclusion
The PCB of waste automobile tires may be one of the most desirable techniques for the economic and environmental stand point.
Lastly, a PCB content of 4% of the weight of concrete mix will be recommended to use at 75 µm particle size to give desirable compressive strength after 28 days.

## Slide 36
First of all adding water to concrete must be very careful so water amount that should be added must be studied and weighed carefully.
About dealing with cement it is not preferable to use cement from an opened left pocket.
Another recommendation which is dealing with pyrolysis carbon black should be in very careful way and this is due to the light weight of the PCB
Recommendation

## Slide 37
Thank you 