## Slide 1: Graduation Project ( 2 ) Remediation of Wastewater Containing Divalent Heavy Metals using Silica-Embedded Metal Oxide Nanoparticles
By: Saqr Abuhatab
Hana Hamdan
Wessal Ziad
Under the supervision of Dr. Amjad El-Qanni
May 20, 2019

## Slide 2: Outlines
Synthesis of Silica-Embedded NiO -MgO NanoParticles .
pH, Isotherm and Kinetics Adsorption Experiments.
Coexisting Ions effect.
Reusability of NiO -MgO SBNs.
Adsorption of Cr2+from real wastewater sample.
Cost estimation for synthesizing NiO-MgO SBNs.
Conclusion and Recommendations.

## Slide 3: Synthesis of NPs.
1
NiO-MgO SBNs
Colloidal Silica
Deionized water
Nickel nitrate
Magnesium nitrate
Sucrose
Nitric acid
Step1: Mixing

## Slide 4: Afterward, the glass beaker was then placed in the oven at 100 ᵒC for 48 h to evaporate the water. After 48 h, dried solid materials looking like sponge cakes were obtained. These solid materials were placed in the oven at 250 ᵒC for 12 h.
2
Step2: Drying
Step3: Calcination
The obtained powder was milled until it become homogenous, then it was calcined in the oven at 800 ᵒC for 3 h in a flow of air.

## Slide 5: pH Effect
3
The effect of solution pH on the adsorption performance was investigated by varying it from about 3 to 11.
The removal uptakes of the metal ions have been found to be strongly pH dependent for Cu2+, while slightly dependent for Zn2+ and Cr2+.

## Slide 6: Adsorption Isotherms.
4
Adsorption isotherms for Zn2+, Cu2+, and Cr2+ metal ions onto NiO-MgO SBNs were conducted by varying the initial concentration of the metal ions from 50 to 400 mg/L at 25 ℃ and pH of around 5.5.
The adsorption uptakes (molecules per surface area) of SBNs was determined based on a mass balance analysis.
The adsorption of Cu2+ and Zn2+ onto NiO-MgO SBNs were described using the non-linear Sips model, while the adsorption of Cr2+ ions was perfectly described by the non-linear BET model.
Sips model parameter |  |  |  | 
Heavy metal |  |  |  | 
Zn2+ | 7.234 | 0.322 | 0.99 | 0.0823
Cu2+ | 13.76 | 0.007 | 0.59 | 0.0074
BET model parameter |  |  |  | 
Heavy metal |  |  |  | 
Cr2+ | 38.35 | 0.00037 | 0.00188 | 0.0459
Sips model parameter |  |  |  | 
Heavy metal |  |  |  | 
Zn2+ | 7.234 | 0.322 | 0.99 | 0.0823
Cu2+ | 13.76 | 0.007 | 0.59 | 0.0074
BET model parameter |  |  |  | 
Heavy metal |  |  |  | 
Cr2+ | 38.35 | 0.00037 | 0.00188 | 0.0459

## Slide 7
Cu2+
Zn2+
5
Surface of SBNs
Surface of SBNs
(Sips Model)

## Slide 8
Cr2+
Surface of SBNs
6

## Slide 9: Adsorption Kinetics
7
The adsorption kinetics of Zn2+, Cu2+, and Cr2+ metal ions onto NiO-MgO SBNs were only affected by the film diffusion, of which it can be considered as the rate-limiting step in the kinetics study.
The adsorption kinetics of Zn2+, Cu2+, and Cr2+ metal ions onto NiO-MgO SBNs were conducted in single solutions by fitting the obtained experimental data to the external mass transfer model.
Heavy metal | Cr2+ | Cu2+ |  | Zn2+
Equilibrium Isotherm model | BET | Sips |  | 
(mg/g) |  |  |  | 
External mass transfer model |  |  |  | 
a (1/min) | 0.65 | 0.21 | 0.101 | 
Needed time to reach equilibrium (min) | 2 | 40 | 60 | 
Heavy metal | Cr2+ | Cu2+ |  | Zn2+
Equilibrium Isotherm model | BET | Sips |  | 
 | 0.65 | 0.21 | 0.101 | 
Needed time to reach equilibrium (min) | 2 | 40 | 60 | 

## Slide 10
Zn2+
Cu2+
Cr2+
8
Estimated time: 60 min
Estimated time: 40 min
Estimated time: 2 min

## Slide 11: Coexisting ions effect
The data in Figure below shows the obtained experimental data of the coexisting metal ions experiment. It was found that the total adsorption capacity of Zn2+, Cu2+, and Cr2+ onto the NiO-MgO SBNs in multi-component system increases.
9

## Slide 12: Reusability of NiO-MgO SBNs
10
The regeneration of the commercial available adsorbents, e.g. activated carbon, is energy intensive, costly, time-consuming process and environmentally unfriendly
The Figure below, shows the removal efficiency (R%), of single Zn2+, Cu2+, and Cr2+ metal ions after two adsorption cycles onto the NiO-MgO SBNs. It is obvious from the results that the used NiO-MgO SBNs are reusable sustainable for the adsorptive of these metal ions.
The regeneration of the Zn2+- (NiO-MgO) SBNs consumed the largest amount of HNO3 and DI water until no any metal ions were found in the washing water, followed by Cu2+-(NiO-MgO) SBNs and finally by Cr2+- (NiO-MgO) SBNs

## Slide 13: Adsorption of Cr2+ ions from real wastewater sample
11
The leather tanning wastewater sample before (the left side) and after adsorption (the right side).

## Slide 14: Cost estimation for synthesizing NiO-MgO SBNs .
12
Material | Commercial cost (USD) | Used amount | Cost (USD)
Colloidal Silica | 58.2 USD/ 1L | 5.1g | 0.229
Nickel nitrate | 306.4 USD/ 100g | 9.9g | 30.3
Magnesium nitrate | 337 USD/ 50g | 9.1g | 61.3
Sucrose | 1 USD/ 1 kg | 15g | 0.015
Nitric acid | 235 USD/ 475mL | 1.5mL | 0.742
Total Cost |  |  | 92.59 USD/ 5g NPs

## Slide 15: Cost comparison of the in-house prepared NiO-MgO SBNs with common metal oxides nanoadsorbents
Metal Oxide NPs | Commercial cost (USD) | Cost for 1 g (USD)
NiO | 76.3 USD/ 25g | 3
MgO | 125 USD/ 5g | 25
NiO-MgO SBNs | 92.59 USD/ 5g | 18.5
13

## Slide 16: Recommendations
14
Our project can be extended to further work details:
Working on further divalent heavy metal such lead and cadmium in signle, binary, and ternary systems.
Studying the efficiency of single NiO or MgO SBNs for the removal of heavy metal ions.
Scalling up the process by first studying the hydraulic design of a packed bed column.
Perform recrystallization experiments for the heavy metals after the adsorption.

## Slide 17: Thanks for Listening and for your time. Any Questions?
The end…
15