## Slide 1: Synthesis of Nitrogen-Doped Carbon Nanodots from Ethylene Amine
Graduation Project-1 (10626591)
Supervised by: Dr. Shadi Sawalha
Prepared by: Ansam Zedan
Anhar Azizeh

## Slide 2: Problem statment Scope of work Carbon nanodots 01 02 03
TABLE OF CONTENTS
N-Doped
04
Methodology
Results and discussion
Prospective and Recommendations
05
06
07
Conclosion
08

## Slide 3: 01 Problem Statement

## Slide 4: Problem Statement
Different properties of CNDs are affected by the choice of precursor. Due to their differences, they can be used in a variety of applications, including biomedicine and advanced materials depending on the different properties that characterize each CND configuration depending on the source and its compatibility with the specific application.

## Slide 5: Scope of work 02

## Slide 6: Scope of work
To synthesize N-doped CNDs from Penta ethylene hexamine and triethylenetetramine by chemical oxidation method. Furthermore, To study the effect of the oxidizing agent (H2O2)on their properties.

## Slide 7: Carbon nanodots 03
Synthesis, application, and property

## Slide 8: Bottom-up 02
Synthesis and source
Top-down
Microwave pyrolysis
Hydrothermal
solvothermal treatment
01
chemical oxidization laser ablation arc discharge
Bottom-up
Microwave pyrolysis
Hydrothermal
solvothermal treatment
02

## Slide 9: CNDs properties
Resistance to photobleaching
Low cost
Low cytotoxicity
Ease of functionalization
02
01
03
04
05
Good biocompatibility

## Slide 10: 04 N-Doped
Source and property

## Slide 11: Element surface doping
Nitrogen
Phosphorus
sulfur
Good stability
Structure defects
Electrochemical activity
High conductivity
Specific surface area

## Slide 12: 5 Methodology
Materials and Synthesis of CNDs

## Slide 13: Chemical Materials
Penta ethylene hexamine (PEHA)
Triethylenetetramine (TETA)

## Slide 14: Synthesis of CNDs
0.5 ml PEHA with H2O2
(0-1.5 ml)
black Residue
CNDs
solution
cenrifuge and filter
heating at 220 C

## Slide 15: 6
Results
and Dissection

## Slide 16: Synthesis mechanism

## Slide 17
Compilation time
Catalyst Compilation time (min)
H2O2 PEHA TETA
0 25 10.5
0.25 22 9
0.5 22 8
1 16 7.5
1.5 11 7

## Slide 18
product yield
catalyst product yield %
H2O2 TETA PEHA
0 3.5 14.8
0.25 4.7 23.7
0.5 5.2 40.6
1 5.6 46

## Slide 19: Morphology and Surface functional group

## Slide 20: AFM for TETA
(a) AFM image of TETA. (b) height profile of TETA.

## Slide 21: AFM for PEHA
((c) AFM image of PEHA. (d) height profile of PEHA.

## Slide 22: FTIR spectra of synthesized CNDs from PEHA
ζ-potential
10.83 to
0.59.

## Slide 23: FTIR spectra of synthesized CNDs from TETA
ζ-potential
11
to
2.27

## Slide 24
XPS for PEHA
(a) XPS survey of PEHA. (b) High resolution of C 1s core.
(c) High-resolution O 1s cores. (d) High-resolution N 1s cores.

## Slide 25
XPS for TETA
(a) XPS survey of TETA. (b) High resolution of C 1s core.
(c) High-resolution O 1s cores. (d) High-resolution N 1s cores.

## Slide 26
Optical property

## Slide 27: UV-Vis for PEHA
(a)The absorption spectra of synthesized CNDs from PEHA
(b)Tauc plot of PEHA
Bandgap
2.9 eV

## Slide 28: UV-Vis for TETA
(a)The absorption spectra of synthesized CNDs from TETA
(b)Tauc plot of TETA
Bandgap
3.12-3 eV

## Slide 29: Fluorescence spectra
(a) Fluorescence spectra at different excitation wavelengths for PEHA
(b) Fluorescence spectra at different excitation wavelengths for TETA
Maximum emission
Maximum emission
PEHA
TETA
430 nm
436 nm

## Slide 30: Quantum Yield
Catalyst | Quantum Yield | 
H2O2(ml) | PEHA(0.5ml) | TETA(0.5ml)
0 | 9.5 | 14.8
0.25 | 9.2 | 12.27
0.5 | 8.8 | 9.8
1 | 6.4 | 7.7

## Slide 31: 7
Prospective and Recommendations

## Slide 32: Prospective and Recommendations
CNDs from N-doped CNDs can be used for several applications including LED for the reason CNDs that were produced from PEHA and TETA have a high fluorescence, especially for TETA so it’s suitable to produce LED from these CNDs. Furthermore, Other applications could be proposed as antibacterial, and anti-cancer and could be good candidates for bioimaging.

## Slide 33: 8 conclusion

## Slide 34: conclusion
In this project, CNDs were synthesized from PEHA and TETA with the presence of various amounts of H2O2 from 0 to 1.5 by using the chemical oxidation method. The resulting high-efficiency N-doped CNDs gives a wide variety of different characteristics in particle size, but PEHA gave a larger size than TETA, and this in turn affects the band gap in the opposite way, as the band gap of TETA is relatively large compared to PEHA.
The N-doped CNDs possess distinct fluorescent properties that appeared when they were irradiated with a 360 nm UV lamp. In addition, they behave with excellent absorption in the UV region, and the tail extends into the visible region which is characteristic of most synthesized CNDs.
Moreover, a thorough analysis of the nitrogen, carbon, and oxygen contents in both materials revealed strikingly identical amounts. This consistency supports the claim that carbon nanodots with comparable compositions from TETA and PEHA sources were successfully synthesized by the synthesis technique.

## Slide 36: Our team
Ansam Shdad Zedan
Anhar Yousef Azizeh