## Slide 1: Incorporating Nano Titanium Dioxide in Water Based Emulsion for Photo-Degradation of VOCs
Prepared by:
Jenan Kamal
Mariam Harah
Remaa` Yasser
Thar`a Mabrouk
Supervisor: Eng. Maryam Hmoudah

## Slide 2: Outline:
Brief introduction about( VOCs, Naphthalene, TiO2)
Preparation of water-based emulsion and tests.
Synthesis of in -houseTiO2 NPs.
Characterization of TiO2 NPs.
Incorporation TiO2 NPs with paint and tests.
Set up of photo-degradation of naphthalene.
Photo-degradation of naphthalene solution.
Conclusion

## Slide 4: Brief introduction:
Volatile organic compounds (VOCs) are emitted as gases from certain solids or liquids. VOCs include a variety of chemicals, some of which may have short- and long-term adverse health effects. Concentrations of many VOCs are consistently higher indoors (up to ten times higher) than outdoors.

## Slide 5: Naphthalene

## Slide 6: Nano titanium dioxide
Titanium nanoparticles are particles of titanium dioxide (TiO2) with diameters less than 100 nm.

## Slide 7: Preparation of water-based emulsion
The raw materials of P2
 | Ingredients | Percentage (wt. %)
1 | Water | 34.0
2 | Cellulosic thickener | 0.4
3 | Dispersing agent | 0.6
4 | Bactercide | 0.45
5 | Titan | 12.0
6 | Carbonate | 20.0
7 | Talc | 4.0
8 | Styrene acrylic | 16.0
9 | Coalescent agent | 0.6
10 | Anti-foaming agent | 0.7
11 | Wetting agent | 0.5
12 | Silicate | 4.0
 | Total | 93

## Slide 8: Result of P2 before storage.
Acceptance | Permitted Limit (Palestinian Standards Institution) | Result | The test
√ | 25◦C | 24 ◦C | Temperature
√ | 5-22 poise | 15 poise | Viscosity
√ | 1.4-1.6g/ml | 1.38 g/ml | Density
√ | 7-10 | 8 | pH
√ | 55-70 % | 58.5% | Solid content
√ |  | 4.5 | Gloss
√ |  | 0.949 | Opacity

## Slide 9: Result of P2 after storage.
Acceptance | Permitted Limit (Palestinian Standards Institution) | Result | The test
√ | 25◦C | 24 ◦C | Temperature
√ | 5-22 poise | 16 poise | Viscosity
√ | 1.4-1.6g/ml | 1.41 g/ml | Density
√ | 7-10 | 8 | pH
√ | 55-70 % | 58.5% | Solid content
√ |  | 4.5 | Gloss
√ |  | 0.949 | Opacity

## Slide 10: Synthesis of TiO2 NPs by sol-gel method
There are many different synthetic routs of TiO2 NPs.
Sol-gel method is widely used to assemble various metal oxides due to many reasons, so sol-gel is the simplest and most developed method among different methods.

## Slide 11: Synthesis process:
TTIP
Isopropyl alcohol
After 20min of stirred DIW will be added
Heating 80˚C,5hr
Cooled at room temp.
NaOH
pH
Sol
1 day,25°C
Gel
Filtering and washing
Rinse with ethanol
Drying @100°C,12hr
Calcination @800,2hr

## Slide 12: Characterization of TiO2 NPs
The main devices used to characterize TiO2 NPs:
X-ray diffraction (XRD): is a rapid analytical technique primarily used for phase identification of a crystalline material and can provide information on unit cell dimensions.
Scanning electron microscopy (SEM): was performed to study the surface morphology of TiO2 NPs . To view the morphology of the samples. A very small quantity of each powdered sample was placed over a carbon tape sample holder and it was tapped to release the excess and loose particles

## Slide 13: XRD analysis

## Slide 14: SEM analysis
(a)
(b)
a) SEM image for in-house nano by sol gel method. b) SEM image for purchase

## Slide 15: Incorporation TiO2 NPs with paint
incorporated with paint at the last stage of paint manufacturing.
The ratio of TiO2 NPS to paint equally 1%.
Speed of mixer approximately 166 rpm for 15 min.

## Slide 16: Result of incorporating 6g TiO2 NPs with 600g P2.
Acceptance | Permitted Limit (Palestinian Standards Institution) | Result | The test
√ | 25◦C | 24 ◦C | Temperature
√ | 5-22 poise | 17 poise | Viscosity
√ | 1.4-1.6g/ml | 1.38 g/ml | Density
√ | 7-10 | 8.7 | pH
√ | 55-70 % | 60.7 % | Solid content
√ |  | 4.5 | Gloss
√ |  | 0.949 | Opacity

## Slide 17: Set up of photo-degradation of naphthalene
Wooden box
Painted cube
Magnetic
Hotplate
Led light

## Slide 18: calibration curve
  AfterPhoto-degradation of naphthalene experiment, quantitative analysis was established by UV-Vis spectrophotometer then a calibration curve was constructed and then used to determine the final concentration values of naphthalene solution after photo degradation.
Chart: 
| 0 | 0.1 | 0.2 | 0.25 | 0.4
calibration curve | 0 | 1.582 | 2.774 | 2.805 | 2.867
Calibration curve of naphthalene solutions

## Slide 19
final concentrations for the S1 (in-house TiO2 NPs ), S2 (pure paint) and S3 (purchased TiO2 NPs) effectiveness on naphthalene solution of 0.28M in first trial .
Trial 1 with LED | Concentration [M] | % of remove the naphthalene
Original solution 0.28M | 0.318 | -
S1 | 0.314 | 1.26%
Re-generation S1 | 0.311 | 2.2%
S2 | 0.324 | -
S3 | 0.322 | -

## Slide 20
final concentrations for the S1(TiO2 NPs ), S2 (pure paint) and S3(purchased TiO2 NPs) effectiveness on naphthalene solution of 0.28M in second trial.
Trial 2 with LED | Concentration [M] | % of remove the naphthalene
S1:in-house TiO2 NPs | 0.299 | 5.97%
S2 :pure paint | 0.306 | -
S3 :purchased TiO2 NPs | 0.304 | 4.4%

## Slide 21
Effectiveness of in-house TiO2 NPs compared with the original solution

## Slide 22
Effectiveness of pure paint compared with original solution

## Slide 23
Effectiveness of purchased TiO2 NPs compared with original solution

## Slide 24: conclusion
TiO2 NPs have been synthesized by the sol-gel method producing anatase phase. TiO2 has been successfully applied as a catalyst for photo-degradation of naphthalene by using led light. The led light has also improved the photo-catalytic properties of the paint and through the re-generation TiO2 NPs. In-houseTiO2 NPs were characterized by two methods X-RD and SEM, the crystal size of the TiO2-anatase-phase was determined to be 3.1 nm, the surface structure and morphology of TiO2 NPs were cubic and agglomerated surface.
. The efficiency of photo degradation of naphthalene were compered between in-house TiO2 NPs and the purchased TiO2 NPs, the results as %removal of naphthalene for purchased after regeneration it was 4.4%. However, the %Removal of naphthalene with the in-house TiO2 NPs was 1.26% and after regeneration it was 5.97%. These results indicate the in-house TiO2 NPs more effective than the purchased TiO2 NPs