## Slide 1
An-Najah National University
Chemical Engineering Department
Graduation Project
Modification and Testing the Performance of Floor Surface Cleaning Gel
Supervisor:
Prof.Amer El-Hamouz
Prepared by:
Azza Abu-Asab
Doaa’ Al-Shiekh
Ola Abdelhadi

## Slide 2: Contents
4
Introduction
1
2
3
5
Goals and objectives
Methodology
Experimental Work
Results and Discussion
6
Conclusions and Recommendations
6

## Slide 3: Introduction
This project is based on a previous project “ The Preparation of Palestinian Standard for Floor Cleaning Gel”.
The rapid increase in the cost of the pine oil.
There's no practical scientific method to test the performance of the gel.
Study Problem
The actual market volume is approximately 6700 tons per year.

## Slide 4
Main Goals
Testing the performance of the gel using surface activity concept and standard tests
Can we produce a cleaning gel with low cost and higher efficiency?!

## Slide 5
2
Modification of floor cleaning gel by adding abrasive materials and modifying the formula.
1
Production of a gel in the lab by different pine oil concentration.
3
Finding and using a method to evaluate the cleaning efficiency and performance of the gel by using contaminated soil and determine the amount of contamination absorbed for each
Evaluate the cleaning efficiency and performance of the gel for contaminated soil tile using a straight line apparatus and the surface tension of cleaning gel solution.
Objectives

## Slide 6
4
New formula of cream cleaning product
5
Designing an apparatus to evaluate the cleaning efficiency
1
Questionnaire
Txt in here
ThemeGallery is a Design Digital Content & Contents mall developed by Guild Design Inc.
2
Performing gel samples with abrasive material.
3
Standard quality tests
Methodology

## Slide 7: Experimental Work Materials

## Slide 8: Customer Concern
Chart: 
| cleaning | foaming | viscosity | effect of temp | smell | cost | mildness
1 | 2 | 8 | 16 | 10 | 5 | 22 | 3
2 | 5 | 13 | 22 | 14 | 3 | 13 | 5
3 | 4 | 28 | 13 | 21 | 10 | 13 | 7
4 | 49 | 11 | 9 | 15 | 42 | 12 | 35
The results of the survey

## Slide 9: The characteristics of the gel preferred by the consumer were in the following order :
Moderate to high foam volume
Moderate viscosity
Acceptable fragrant smell
4
1
2
3
5
Mild to the skin.
High cleaning efficiency

## Slide 10
Minimum number of experiments needed were 12 to get the most acceptable gel sample.The most important ones are as in the following table
Sample No. | Pine oil (Wt%) | Abrasive (Wt%) | CMC (Wt%) | Texapone (ETA) (Wt%)
1 | 5 | - | - | -
4 | 3 | 10 Sand | - | -
6 | 3.5 | 5 CaCO3 | - | -
12 | 2.5 | 2.85 CaCO3 | 0.5 | 1
Results
Gel Preparation

## Slide 11: Standard tests
pH
viscosity
foam volume (shake volume test)

## Slide 12: Results of measured viscosity, foam and pH tests
Sample no. | Viscosity (cp) | Foam volume (mm) | pH
1 | 26000 | 40 | 6.5
4 | 25261 | 30 | 7.24
6 | 25219 | 30 | 6.88
12 | 32600 | 70 | 6.92
13(commercial) | 25712 | 65 | 6.85
Results
Standard tests

## Slide 13: Cost of the best sample in this project and in the a previous project
Ingredient | Cost of one Kg of the ingredient (NIS) | Weight of ingredient of 1L sample of the previous project (g) | Weight of ingredient of 1L sample of this project (g) | Cost of 1L sample of the previous project (NIS) | Cost of 1L sample of this project (NIS)
LABS | 10 | 120 | 120 | 1.2 | 1.2
NaOH | 4 | 15 | 15 | 0.06 | 0.06
Pine oil | 35 | 25 | 50 | 0.87 | 1.75
CaCO3 | 8 | 28.5 | - | 0.23 | -
CMC | 12 | 5 | - | 0.06 | -
ETA | 9 | 10 | - | 0.09 | -
Total cost |  |  |  | 2.51 | 3.01
Results
The percentage of saving is about 17%

## Slide 14
Testing the performance of gel using surface activity concept:
It was done according to the American Standard Testing Method (ASTM), ASTM D4488-95
Soil preparation
The soil was prepared by blending a melt vegetable oil, animal grease, and carbon black
.
Soil application
left for 24 hours at ambient temperature.
Cleaning test
Surface tension measurements

## Slide 15: Results Finding the “cmc” of the gel

## Slide 16
Chart: Surfactants Concentration(ppm)
| 4960 | 2480 | 1240 | 620 | 409.2 | 310 | 137.63999999999999 | 71.92 | 37.200000000000003 | 19.096000000000004 | 9.61 | 4.8236000000000008 | 2.3559999999999977 | 0.60511999999999999
 | 30.2 | 31.22 | 31.4 | 31.9704 | 34.163 | 28.393 | 33.009 | 33.7014 | 34.163 | 34.3938 | 35.5478 | 42.241 | 48.011 | 60.705
In order to find the critical micelle concentration “cmc” of the gel, 14 samples of gel with different diluted concentrations in the range between 4*10-4 to 4 ml gels in 125 ml water were prepared

## Slide 17
Pine oil concentration
1%
2.5%
3.5%
commercial
1:125
0.25:125
0.06:125
0.004:125
0.002:125

## Slide 18
Results
Effect of time (cleaning cycles) on surface tension
Chart: No. cycles
| 0 | 5 | 10 | 15 | 20 | 25
1/125 | 33.7591 | 33.586 | 31.278 | 33.009 | 32.432 | 30.701
0.25:125 | 33.6437 | 30.701 | 33.2398 | 32.7782 | 33.586 | 33.9322
0.06:125 | 33.586 | 33.0667 | 34.163 | 34.9708 | 34.2207 | 34.5669
0.004:125 | 44.0297 | 41.9525 | 43.7989 | 42.241 | 43.5104 | 40.0484
0.002:125 | 47.0878 | 36.2979 | 39.356 | 43.6258 | 42.0102 | 33.8745
Effect of time (cleaning cycles) on surface tension for the 2.5% pine gel/soil solution at different concentrations of gel

## Slide 19: Results Effect of pine oil concentration on surface tension
For a 5 cycles cleaning application
Chart: ml gel: 125 ml water
| 2.0000000000000052E-3 | 6.0000000000000032E-2 | 0.25 | 1
2.5% pine oil | 36.2979 | 33.0667 | 30.701 | 33.586
1% pine oil | 35.9517 | 30.2971 | 30.701 | 33.6437
commercial | 33.6437 | 29.547 | 33.6437 | 32.7782
3.5% pine oil | 38.2597 | 35.317 | 33.586 | 34.3938

## Slide 20: Results Effect of pine oil concentration on surface tension
For 10 cycles cleaning application
Chart: ml gel: 125ml water
| 2.0000000000000052E-3 | 6.0000000000000032E-2 | 0.25 | 1
2.5% pine oil | 39.356 | 34.163 | 33.2398 | 31.278
1% pine oil | 47.434 | 34.2784 | 30.1817 | 35.0285
commercial | 36.8749 | 29.7778 | 28.97 | 28.2776
3.5%pine oil | 40.7985 | 34.163 | 26.5466 | 33.4129

## Slide 21: Results Effect of pine oil concentration on surface tension
For 15 cycles cleaning application
Chart: 15 cycles
| 2.0000000000000052E-3 | 6.0000000000000032E-2 | 0.25 | 1
2.5%pine oil | 43.6258 | 34.9708 | 32.7782 | 33.009
1% pine oil | 46.4531 | 34.163 | 34.0476 | 34.8554
commercial | 40.9716 | 30.4702 | 28.6815 | 28.1045
3.5% pine oil | 50.319 | 35.2016 | 34.0476 | 34.163

## Slide 22: Conclusions and Recommendations
The concentration of the pine oil was reduced to a half of its value in the previous project (from 5wt% to 2.5 wt% )
.
A measurement of the critical micelle concentration ‘cmc’ of the gel was found to be 310 ppm
This work result of pine oil concentration is in line with the published data. Pine oil preferably in amount of up to( 0.01-2.5% by weight),
but most preferably in amount of between (0.75-1.5%) pine oil by weight
Germicidal Pine Oil Composition

## Slide 23
Comparison of surface tension of prepared sample with a commercial gel sample was carried out. Results show that the surface tension measurements of the commercial one were less than that of other samples. Although, the commercial gel sample contains concentration of LABS lower than that used of our work.
What pine oil and other constituents’ concentration in the commercial sample is?

## Slide 24: Recommendations
New Recommended Recipe
pine oil concentration of 1.5%.
pine oil solubilizing agent (5%)
viscosity promoter
The New Recommended Recipe should include:

## Slide 25: Thank You!