## Slide 1
An-Najah National University Faculty of Engineering Chemical Engineering Department
Graduation Project ( 2 )
Effect of processing techniques and conditions on properties of composite polymeric film.
Prepared by:
Ahed Zabadi
Muna Sleem
Salam Sa'ad
We'am Dweikat
Supervisors:
Dr. Hassan Sawalha
Eng. Shadi Sawalha

## Slide 2
Outline
Introduction.
About Linear-low density Polyethylene.
Objectives.
Experimental work.
Materials.
Processing techniques.
Characterization.
Results and discussion
Conclusion

## Slide 3
Introduction

## Slide 4: Different types of PE products
Figure (1): polyethylene bags.
Figure (2): polyethylene pipes
Figure (3): polyethylene gloves.
Figure (4): polyethylene terephthalate bottles

## Slide 5
  Polyethylene
Polyethylene (PE) is the simplest of all polymers.
Linear low – density polyethylene (LLDPE), is a type of PE has low density and crystallinity, formed under low temperature and pressure polymerization conditions.

## Slide 6
  Improvement of the properties LLDPE
Optimizing the mechanical and thermal properties by operation conditions (cooling rate and pressing temperature).
Use additive with different concentration and study its effect on the mechanical and thermal properties by measure it.

## Slide 7
  Objectives:
The first objective of this project was to study the effect of processing techniques and conditions on the properties of polyethylene film.
Preparation method:
Thermal method.
Cold method.

## Slide 8
The second objective was to study the effect of biological food waste –at different concentrations-on the mechanical and thermal properties of composite polyethylene film.

## Slide 9
The properties will be measured by using:
Differential Scanning Calorimetry (DSC).
Tensile Testing Machine.
Melt flow index (MFI).

## Slide 10
Experimental work

## Slide 11
  Material:
Borstar®FB2230 is an enhanced polyethylene. It contains antioxidant and low content anti blocking agent.
Food waste materials:
Figure(5): pistachio shell

## Slide 12
Figure(6): olive kernel
Figure(7): almond shell
Figure(8): avocado seed

## Slide 13
Figure(9): press molding device.
  Processing methods
Thermal press molding.
1-Pressing.
2- Heating.
3- Cooling.

## Slide 14
polyethylene
xylene
xylene
Non-solvent
Non-solvent
Solidification
Cold method (polymer dissolution):
LLDPE put in xylene with 2% concentration and the solution was heated at hot plate.
2. The solution was casted then put in to non-solvent.
3. Solidification for the polymer film.

## Slide 15: Preparation of composites film:
Grinding
Screening
Blending the polymer with the flour
extrusion
Press molding

## Slide 16
  Characterization
Mechanical Properties:
The modulus of elasticity, yield and ultimate strength and elongation at break of the films were measured using Universal Material Tester 50 kN.
Samples were cut from the films into a dog-bone shape.

## Slide 17
Figure (10): Universal Material Tester 50 kN
Notes: لما نحكي عن طريقة عمل الجهاز لازم نحكي السرعة =50 mm/min

## Slide 18: Thermal Properties:
Range of melting temperature and enthalpy of melting were measured using differential scanning calorimetry.
Figure(11): differential scanning calorimetry.

## Slide 19: Chemical Properties:
Melt flow index was measured using melt flow indexer.
Figure(12): melt flow indexer.
Notes: Film samples were cut into small pieces and tested using melt flow index device with a capacity of 6 g. The test was done under loud of 5000g and 190 °C. After the sample processed in the device the material was taken after a period of 10min and weighted.

## Slide 20
Results and discussion

## Slide 21: Analysis of stress-strain diagram
Modulus = Stress /Strain (0.001)
Notes: نحط stree-strian diagram من الرسمة القديمة تطبيق على السامبل اللي بالمشروع

## Slide 22: Results of mechanical properties:
Chart: 160 °c
air | 4033.3333
water | 3550
ice | 3410
Chart: 180 °c
air | 2270
water | 4983.333
ice | 1550
Figure (13): Elastic modulus at different cooling rate for temperatures 160 and180 °C.

## Slide 23
Chart: 180 °c
air | 21.3592
water | 20.9142
ice | 19.0845
Chart: 200 °c
air | 21.749
water | 19.7471
ice | 19.3472
Figure (14): Ultimate strength at different cooling rate for temperatures 180, 200°C.

## Slide 24
Chart: 180 °c
air | 15.2575
water | 16.1262
ice | 12.713
Chart: 200 °c
air | 16.1871
water | 15.1277
ice | 13.8625
Figure (15): maximum yield strength at different cooling rate for temperatures 180, 200°C.

## Slide 25
Chart: 160 °C
air | 2.5479
water | 3.2109
ice | 3.4141
Chart: 200 °C
air | 3.1339
water | 3.031
ice | 3.3976
Figure (16): Elongation at different cooling rate for temperatures 160, 200°C.

## Slide 26
Chart: air
T160 | 4033.3333
T180 | 2270
T200 | 3960
Figure (17): Elastic modulus at different temperatures cooled by air.

## Slide 27: Analysis of DSC diagram:
Figure(18): results of DSC device.

## Slide 28: DSC results
 | Tmp | Tms | sample
 | 119.6 | 108.4 | LLDPE
 | 122.82 | 112.77 | TA180
51.86 | 122.9 | 110.6 | TW180
47 | 121.49 | 108.48 | TI180
 | 121.94 | 106.5 | CA
117.2 | 118.77 | 102.68 | CE.A
 | Tmp | Tms | sample
 | 119.6 | 108.4 | LLDPE
 | 122.82 | 112.77 | TA180
51.86 | 122.9 | 110.6 | TW180
47 | 121.49 | 108.48 | TI180
 | 121.94 | 106.5 | CA
117.2 | 118.77 | 102.68 | CE.A
20.31
43.01
106.1
Table (1): comparison between processing method.

## Slide 29
 | Tmp | Tms | Sample
20.31 | 119.6 | 108.4 | LLPPE
29.41 | 122 | 110.8 | TW160
 | 128.9 | 110.6 | TW180
43.3 | 121.7 | 111.57 | TW200
 | Tmp | Tms | Sample
20.31 | 119.6 | 108.4 | LLPPE
29.41 | 122 | 110.8 | TW160
 | 128.9 | 110.6 | TW180
43.3 | 121.7 | 111.57 | TW200
Table (2): comparison between different pressing temperatures.
51.86

## Slide 30: Melt flow index results:
Thermal method: no change in the melt flow index.
Cold method:
Melt flow index g/10 min | Sample
1.23 | Ethyl acetate
1.08 | Ethanol
1.38 | Air
Table (3): Melt flow index for Cold method samples.

## Slide 31
Part two:
Composite films

## Slide 32: Results of mechanical properties.
Chart: olive kernel pistachio shell almond shell avocado seed
15 | 1300 | 1450 | 690 | 1390
5 | 0 | 6900 | 5050 | 4950
pure | 4983.333 | 4983.333 | 4983.333 | 4983.333
Figure (19): Elastic modulus for composite films.

## Slide 33
Chart: olive kernel pistachio shell almond shell avocado seed
15 | 14 | 10 | 5 | 3.39
5 | 0 | 15.6 | 11.7 | 13
pure | 16.1262 | 16.1262 | 16.1262 | 16.1262
Figure (20): Maximum yield strength for composite films.

## Slide 34
Chart: olive kernel pistachio shell almond shell avocado seed
15 | 13.75 | 7.3 | 5.1 | 3.3333
5 | 0 | 15.5556 | 11.6667 | 12.8571
pure | 20.9142 | 20.9142 | 20.9142 | 20.9142
Figure (21): Ultimate strength for composite films.

## Slide 35
Figure (22): Elongation for composite films.
Chart: olive kernel pisachio shell almond shell avokado seed
15 | 0.22693 | 0.35995 | 0.15499 | 0.25162
5 | 0 | 0.23857 | 0.52229 | 0.29595
pure | 2.932 | 2.932 | 2.932 | 2.932
Notes: elongation

## Slide 36: DSC results.
 | Tmp | Tms | sample
51.86 | 128.9 | 110.6 | TW180 (pure)
44.66 | 122.96 | 111.9 | Pistachio shell (5%)
40.59 | 122.64 | 110.9 | Almond shell (5%)
44.6 | 161.01 | 110.61 | avocado seed (5%)
38.54 | 121.24 | 110.6 | Olive kernel (5%)
40.79 | 120.87 | 110.37 | Almond shell (15%)
 | Tmp | Tms | sample
51.86 | 128.9 | 110.6 | TW180 (pure)
44.66 | 122.96 | 111.9 | Pistachio shell (5%)
40.59 | 122.64 | 110.9 | Almond shell (5%)
44.6 | 161.01 | 110.61 | avocado seed (5%)
38.54 | 121.24 | 110.6 | Olive kernel (5%)
40.79 | 120.87 | 110.37 | Almond shell (15%)
Table (4): comparison between pure and composite films.

## Slide 37: Melt flow index results.
5% | 15% | samples
No result | 0.97 | Olive kernel
0.92 | 1.12 | Pistachio shell
0.499 | 0.36 | Almonds shell
0.91 | 1.09 | Avocado seed
Table (5): Melt flow index for composite samples (g/10 min).

## Slide 38: Conclusion
The films cooled by quenching in ice have the lowest elastic modulus, maximum yield and ultimate strength.
Increasing the pressing temperature increases the elastic modulus.

## Slide 39
MFI of solution-casting samples have higher MFI values than those prepared with thermal press-molding.
The pistachio shell (with 5% concentration) showed better mechanical properties than other food additives.