## Slide 1: Synthesis and characterization of metal oxide nanoparticles (MON): cases of MgO and FeO
Prepared by:
Hala Odeh
Safia Kahla
Shiraz Hussein
Supervisor:
Dr.Hamdallah Bearat

## Slide 2: Objectives
Overview
Introduction
Synthesis and characterization
Results and discussion
Errors and difficulties
Conclusion
Recommendations

## Slide 3: Overview
The first stage of research concerns about synthesis of two metal oxides: (I) magnesium oxide (MgO) through thermal methods starting from the carbonate (MgCO3) , (ii) ferric iron oxide (Fe­2O3) through thermal or hydrothermal decomposition of iron oxyhydroxid (FeO.OH).
While in the second stage, the product is analyzed as powders for particle size and particle size distribution using the following technique: X-ray powder diffraction (XRD).

## Slide 4: Introduction
The project focus on synthesis and characterization of MgO and FeO
Where the Characterization part include checking and testing the samples available by different devices like XRD , SEM , TEM , UV and etc . But the device that was chosen to check the size of the samples is XRD , as it’s the only device available in our country specifically in Arab American University – Jenin .

## Slide 5: What is X-Ray Diffraction?
X-ray powder diffraction (XRD) is a rapid analytical technique used for phase identification of a crystalline material ,provide information on unit cell dimensions, and for determining the mean size of Nano crystallites. Both phases of MgO & Feo demonstrates very sharp peak . As shown later in results

## Slide 6: Synthesis OF MgO and FeO
Preparation of MgO
Dry Magnesium carbonate in oven at 90C ⸰
MgCO3∆→MgO+CO2
Weigh a sample of 1g MgO
Heat it at different temperature using electric furnace
Preparation of FeO
Dry iron oxide in oven at 90C ⸰
2FeO.OH∆→Fe2O3 + H2O
Weigh a sample of 0.5g Fe₂O ₃
Heat it at different temperature using electric furnace

## Slide 7: Characterization
XRD TEST:
Different samples were chosen to apply them for the test, the steps were:
Preparation of powder samples
Put the sample on the specified glass for the device.
Insert the sample inside the device for the test by closing on it.
Insert the wanted data like speed, range of angle and etc on the software.
The Miniflex program starts drawing the graph of 2θ versus intensity.

## Slide 8: Results and Discussion
The best samples were taken to test them in the XRD. As mentioned earlier that the range of diameter of a Nano particle is from (0-100) nm, and the diameter of the samples didn’t exceed 50nm .When the temperature increase the size of the diameter increase, it was noticed also that as the temperature rise the width of the peak get narrower.

## Slide 9
Sample temp. © | Diameter(nano meter)
600 | 2.602733
700 | 2.954923
800 | 3.751513
Table (1):MgO temperature series at 10min and 2deg per min

## Slide 10
Chart: temp.series for Mgo
Figure(1):MgO temperature series @10min and 2deg per min

## Slide 11
Sample time (min) | Diameter (nano meter)
5 | 2.679652
10 | 2.602733
20 | 1.210166
Table(2): MgO time series at 600 c and 2deg per min

## Slide 12
Chart: MgO time series
Figure(2):MgO time series @600 c and 2deg per min

## Slide 13
Sample temp. © | Diameter(nano meter)
750 | 9.820033
850 | 8.119393
950 | 8.469314
Table(3): FeO temperature series at 10min and 2deg per min

## Slide 14
Chart: temperatrue series
Figure(3):FeO temperature series at10min and 2deg per min

## Slide 15
Sample time (min) | Diameter(nano meter)
5 | 11.45671
10 | 9.820033
Table(4):FeO time series at 750 c and 2deg per min

## Slide 16
Chart: TIME SERIES FOR FeO
Figure(4):FeO time series at750 C and 2deg per min

## Slide 17: Errors and Difficulties
The accuracy of the balance while weighting the samples.
It have been discovered the all ceramic crucible’s were used shows high percentage of error.
There was some human error, which make us do more trials for each sample.
Long time to do XRD test for each sample

## Slide 18: Conclusion
The preparation of metal oxide in this project was synthesized by hydrothermal method.
There was a theoretical loss that was calculated.
Samples were tested in XRD, then Miniflex draw the result to find later its diameter. The results of our samples in general for MgO were from (1.2 – 3.7) nm , As for the FeO the results were (8.1-11.4)nm .
Finally our goal have been achieved, as the assumption that was made become real , Nano size exist in the samples .

## Slide 19: Recommendation
1- There should be X-Ray Diffraction device in An-Najah University
2- Safety tools should be available , with better quality due to dealing with high temperature .
3- special crucible material should available , it result in the product quality .

## Slide 20
The end