## Slide 1
Production and Utilization of Biochar from Municipal Solid Waste
Department of Chemical Engineering
Department of Civil Engineering
Supervisors: Dr. Abdelrahim Abusafa
Dr. Abdelhaleem Khader

## Slide 2
Content
01
02
03
04
05
INTRODUCTION
Municipal Solid Waste Disposal Methods
BIOCHAR
METHODOLOGY
CONCLUSION & Recommendation
Rustle & Discussion
06

## Slide 3
INTRODUCTION
The Problem statements
01
02
Objective

## Slide 4
Solid waste management is a significant concern in Palestine, posing environmental and health challenges due to the accumulation of waste. One potential solution involves converting municipal solid waste into biochar through pyrolysis.
The Problem statements

## Slide 5
Reviewing the Literature regrading biochar production.
Objectives
Investigate the pyrolysis process of biochar using cooked rice as the feedstock.
Explore the impact of varying pyrolysis temperatures and residence times on biochar yield and quality.
Analyze the physical and chemical properties of the produced biochar.
Study the adsorption capacity of biochar for methylene blue (MB) dye.

## Slide 6
Municipal Solid Waste Disposal Methods
01
02
03
04
LANDFILLING
Composting
Incineration
Pyrolysis

## Slide 7
Pyrolysis
Pyrolysis is the heating of an organic material in the absence of oxygen.
Biomass pyrolysis is usually conducted at 400°C and 450 °C .
pyrolysis of produces three products:
  syngas
  BIO-OIL
  BIOCHAR

## Slide 8
Biochar Objectives
Production
Characterization
Applications

## Slide 9
Production
Collect &Separate Solid Waste
Pre-drying
Chop Dried
Materials
Prepare the Reactor
Enter Biomass into the Oxygen-Free Reactor
Steps
Post Pyrolysis Cooling in Biochar Production
Place Biochar in Special Bags
Biochar is a charcoal-like material that is produced by burning organic waste through a process called pyrolysis.
BIOCHAR

## Slide 10
BIOCHAR
In this project, rice was used to produce biochar It is a carbon-rich product that is manufactured at temperatures ranging from 350 to 700 ° C.
400 ° C
450 ° C
300 ° C

## Slide 11
Characterization
  PH
  Biochar pH varies from slightly acidic to alkaline, influenced by factors like organic material source, initial acidity, and pyrolysis conditions.
The ash content and composition of biochar are critical factors, often expressed on a dry basis, excluding water. Understanding biochar's ash content is vital as it influences potential applications.
Ash Content:
Chemical
Physical
The surface area property of biochar refers to the total area of the external and internal surfaces within its structure.
Surface Area:
  Water Holding Capacity
Water Holding Capacity (WHC) is a key property of biochar that impacts soil moisture, irrigation needs, and plant growth.
  Adsorption
indicating its ability to adsorb pollutants, is influenced by factors like biomass type, pyrolysis temperature, activation method, solution pH, and adsorbate properties. while higher pyrolysis temperatures and activation methods increase surface area and porosity.

## Slide 12
Methodology
Ash content:
prepare the samples 1 g by drying and grinding the original materials
place them in a high-temperature furnace 750c for the incineration process for 7-10 min
Once cooled, measure the weight of the remaining ash using a precision balance.

## Slide 13
Methodology
PH:
2 g of the sample were added to 50 ml distilled water then the pH was measured using a pH meter.

## Slide 14
Methodology
Water Holding Capacity:
A 5-gram from crushed biochar was placed in a funnel
addition of 30 milliliters of water.
Test Method:
Percolation

## Slide 15
Methodology
The biochar was dried in the oven at 105 C for one-hour
acetic acid solution (0.1 M) was prepared with known concentration and NaOH solution (0.1 M) for titration was prepared
1 g of biochar was weighted and 50 mL of the acetic acid solution were moved to the flask
The 1 g biochar was moved to the flask and left in the solution for 24 hours closed in the shaker
After 24 hours the acetic acid solution was filtered and titrated with NaOH prepared solution (0.1 M)
Surface area:

## Slide 16
Methodology
Adsorption:
A stock solution of methylene blue (200 mg/L) was prepared and diluted to concentrations of 5, 10, 15, 20, and 25 mg/L.
0.2 gram of crushed biochar was weighed using a sieve and placed in a 10 ml tube containing a solution (distilled water with methylene blue dye) for all concentrations that were diluted.
The solutions were centrifuged at 200 rpm for 24 h in a shaker.

## Slide 17
  Results and Discussion

## Slide 18
Production
Results Production Biochar
Sample | Temperature (°C) | Duration (h) | Initial weight(g) | Final weight(g) | Difference
1 | 300 | 1 | 109.81 | 93.63 | 16.18
2 | 300 | 2 | 104.69 | 78.68 | 26.01
3 | 400 | 1 | 97.53 | 79.75 | 17.78
4 | 400 | 2 | 99.53 | 68.82 | 30.71
5 | 400 | 3 | 104.02 | 72.69 | 31.33
6 | 450 | 1 | 113.13 | 81.88 | 31.25
7 | 450 | 2 | 110.44 | 73.51 | 36.89
8 | 450 | 1.5 | 108.21 | 72.06 | 36.15
The samples at 300°C did not undergo complete pyrolysis and were therefore completely disregarded
Temperatures of 400°C and 450°C were used to obtain the best sample for studying its characterization and application.

## Slide 19
PH
The results range between 7.36−5.46 for biochar samples and 9.72 for the commercial activated carbon.
Sample | PH
2 hr-400c | 7.09
1hr-450c | 5.46
2hr-450c | 7.28
3hr-400c | 7.28
1.5hr-450c | 7.36
Activated | 9.72
The samples were weighted before and after incinerating and no ash had appeared.
Ash Content

## Slide 20
WHC
Surface Area
Sample | Weight(g) | Volume 1 | volume 2 | v2-v1 | WHC%
1 hr-450c | 5 | 30 | 21 | 9 | 180
1.5hr-450c | 5 | 30 | 25 | 5 | 100
2hr -450c | 5 | 30 | 26 | 4 | 80
Activated carbon | 5 | 30 | 22 | 8 | 160
Sample name | surface area(m2)
2h (400) | 109.79
3h (400) | 307.40
1.5h (450) | 219.57
2h (450) | 285.45
activated carbon | 1,317.45

## Slide 21
calibration curve
Chart: Empty
| 0 | 5 | 10 | 15 | 20 | 25
 | 0 | 0.442 | 1.1 | 1.236 | 1.668 | 2.322
Adsorption

## Slide 22
Adsorption
Chart: 2 hour 400 oC
| 0 | 1.3863636363636365 | 2.875 | 3.5340909090909092 | 8.295454545454545 | 11.090909090909092 | 28.19318181818182 | 110.90909090909092 | 160
 | 0 | 0.18068 | 0.35625 | 0.5733 | 0.58523 | 0.69545 | -0.5
Chart: 1.5 hour 450 oC
| 0 | 1.3522727272727273 | 3.2840909090909092 | 5.9659090909090917 | 11.897727272727273 | 11.215909090909092 | 38.93181818181818 | 59.431818181818187 | 390.4545454545455
 | 0 | 0.18239 | 0.3358 | 0.4517 | 0.40511 | 0.6892
Chart: 2 hour 450 oC
| 0 | 3.4772727272727275 | 3.6363636363636367 | 5.2500000000000009 | 8.875 | 10.022727272727273 | 47.727272727272727 | 213.63636363636363 | 244.54545454545456
 | 0 | 0.076136 | 0.31818 | 0.4875 | 0.55625 | 0.74886
Chart: 3 hour 400 oC
| 0 | 1.6477272727272727 | 6.4659090909090908 | 9.3409090909090917 | 13.931818181818182 | 43.56818181818182 | 117.72727272727273 | 153.18181818181819
 | 0 | 0.16761 | 0.1767 | 0.75 | 0.53295 | 0.55341
Chart: commercial activated carbon
| 0 | 1.1477272727272729 | 1.2613636363636365 | 1.9090909090909094 | 1.9431818181818183 | 2.7613636363636362 | 9.954545454545455 | 59.772727272727273 | 54.88636363636364
 | 0 | 0.19261 | 0.43693 | 0.65455 | 0.90284 | 1.1119

## Slide 23
to select the best biochar sample, it is essential to perform Isothermal Adsorption calculations
Isothermal Adsorption
Freundlich
Chart: Langmuir and Freundlich isothermaol adsorption 3h 400 c
| 0.60689655172413792 | 0.15465729349736379 | 0.1070559610705596 | 7.1778140293637854E-2
langmuir | 5.9661 | 5.6592 | 1.8763 | 1.807
freun | -0.77569 | -0.75275 | -0.27331 | -0.25695
Chart: Langmuir and Freundlich isothermaol adsorption AC
| 0.87128712871287117 | 0.79279279279279269 | 0.52380952380952372 | 0.51461988304093564 | 0.36213991769547327
lang | 5.1917 | 2.2887 | 1.5278 | 1.1076 | 0.89934
freun | -0.71531 | -0.35959 | -0.18406 | -0.044389 | 0.046078

## Slide 24
Isothermal Adsorption
Langmuir
Chart: Langmuir and Freundlich isothermaol adsorption 1.5h 450 c
| 0.73949579831932777 | 0.30449826989619377 | 0.16761904761904758 | 8.4049665711556823E-2 | 8.9159067882472132E-2
langmuir | 5.4829 | 2.978 | 2.2138 | 2.4684 | 1.4509
freundlich | -0.73901 | -0.47393 | -0.34515 | -0.39242 | -0.16165
Chart: Langmuir and Freundlich isothermaol adsorption 2h 400 c
| 0.72131147540983598 | 0.34782608695652173 | 0.28295819935691319 | 0.12054794520547946 | 9.0163934426229497E-2
langmuir | 5.5346 | 2.807 | 1.7443 | 1.7087 | 1.4379
freun | -1.3457 | -2.2309 | -4.1387 | -4.2978 | -6.3399
Chart: Langmuir and Freundlich isothermaol adsorption 2H 450 c
| 0.27499999999999997 | 0.19047619047619044 | 0.11267605633802817 | 9.9773242630385478E-2
langmuir | 3.1429 | 2.0513 | 1.7978 | 1.3354
freundlich | -0.49732 | -0.31203 | -0.25473 | -0.1256

## Slide 25
Data Analysis
Following our characterization study, the biochar was selected to be chemically and physically activated at 450°C for 2 hours.
Physical activation The prepared biochar samples were heated at 450 °C for 2 h using an oven at 750 °C for 1 h.
The biochar's surface area increased from 285.45 m² to 807.47 m² after physical activation.
Chemical activation Phosphoric acid was used to activate biochar prepared at 450°C for 2 hours. Two grams of biochar were immersed in 50 mL of 0.1 M phosphoric acid solution and stirred for 24 hours. The biochar was then washed to adjust the pH to 5.73 and dried at 105°C for 2 hours to remove residual moisture.
The biochar's surface area increased from 285.45 m² to 346.06 m² after chemical activation.

## Slide 26
  APPLICATION

## Slide 27
2.Soil:
Biochar, derived from biomass pyrolysis, enhances soil by:
Improving physical properties and aeration.
Retaining nutrients and preventing water contamination.
Providing habitat for microorganisms, enhancing soil quality.
Adjusting pH and increasing Cation Exchange Capacity.
Removing heavy metals, contributing to soil remediation.
Sequestering carbon, reducing greenhouse gas emissions.
Increasing water retention, nutrient availability, and reducing soil erosion
1.Water Purification

## Slide 28
Recommendation
Experiments may have errors due to using a single sample; at least three are needed for reliability.
Higher pyrolysis temperatures (e.g., 800°C) improve biochar's water holding capacity (WHC).
Physical activation significantly increases surface area compared to chemical activation and is recommended for better adsorbent and catalyst performance.
Further studies should examine the effect of pyrolysis temperature on pH.
Explore alternative chemical activation agents (e.g., KOH, NaOH, ZnCl2, H2SO4) and control activation parameters.
Applying biochar to soil can enhance soil health and crop yield.

## Slide 29
Conclusion

## Slide 30
Team Members
Eng.Fatima Abujash
Thank you
Eng.Suzan Shnity
Eng.Dima Shnity
Eng.Dana Qamhiyeh