## Slide 1: Building with Sand
An-Najah National University
Faculty of Engineering & Information Technology
Department of Civil Engineering
Graduation Project ll
Prepared by: Supervisor:
Ahmad Sarrawi Dr. Mohammad Ghazal
Ahmad Assas
Qasem Albayda

## Slide 2: Contents of Presentation
Case study
Our work
Results
Conclusion
References

## Slide 3: CASE STUDY
Tests conducted on mixtures consisting of loam with a specific percentage of added cement:

## Slide 4: OUR WORK
Making a mixture of sand and cement and studying the mechanical properties of the resultant mix by conducting two tests:

## Slide 5: OUR WORK
1. Direct shear
Studied percentages:
Pure sand
15% cement
20% cement
25% cement

## Slide 6: RESULTS
Direct Shear
Soil Description: Sand
Ф = 28.3 degrees
Load (kg) | Max H.Load (KN) | Sigma (Kpa) | Shear (Kpa)
18 | 0.22 | 49.1 | 61.1
36 | 0.287 | 98.1 | 79.7
72 | 0.5 | 196.2 | 138.9

## Slide 7: RESULTS
Direct Shear
Soil Description: Sand + 15% cement
Ф = 29.45 degrees
Load (kg) | Max H.Load (KN) | Sigma (Kpa) | Shear (Kpa)
18 | 0.216 | 49.1 | 60.0
36 | 0.28 | 98.1 | 77.8
72 | 0.508 | 196.2 | 141.1

## Slide 8: RESULTS
Direct Shear
Soil Description: Sand + 20% cement
Ф = 32.6 degrees
Load (kg) | Max H.Load (KN) | Sigma (Kpa) | Shear (Kpa)
18 | 0.176 | 49.1 | 48.9
36 | 0.29 | 98.1 | 80.6
72 | 0.515 | 196.2 | 143.1

## Slide 9: RESULTS
Direct Shear
Soil Description: Sand + 25% cement
Ф = 34.3 degrees
Load (kg) | Max H.Load (KN) | Sigma (Kpa) | Shear (Kpa)
18 | 0.178 | 49.1 | 49.4
36 | 0.254 | 98.1 | 70.6
72 | 0.53 | 196.2 | 147.2

## Slide 10: OUR WORK
2. Compressive strength test (Molds):
Studied percentages:
15% cement
20% cement
25% cement

## Slide 11: RESULTS
Compressive Strength

## Slide 12: RESULTS
Compressive strength
After 7 days:
Percentage of cement in the block | Load
15% | 25KN
20% | 50KN
25% | 80KN

## Slide 13: RESULTS
After 28 days:
Percentage of cement in the block | Load
15% | 33KN
20% | 91KN
25% | 98KN

## Slide 14: CONCLUSION
Mixtures showed increasing angle of friction as the percentage of cement increased
Mixtures showed a considerable compressive strength:
Up to 8 Mpa after 7 days
Up to 9.8 Mpa after 28 days

## Slide 15: References
Building with earth, Gernot minke
Minke, Earth Construction Handbook. Southampton, Great britian 2000.
Minke, Building with Straw.Basel, Berlin, Boston, Germany 2005.
McCann, J.: clay and cop building. Aylesbury, Great britian 1983.
Soil Mechanics,7th Edition, Braja M. Das.